Undirected C-H Bond Activation in Aluminium 
Hydrido Enaminonates

Chijioke Kingsley Amadi, Ufuk Atamtürk, Andreas Lichtenberg, Aida Raauf and Sanjay Mathur *

Institute of Inorganic Chemistry, Department of Chemistry, University of Cologne, Greinstr. 6, 50939 Cologne, Germany; camadi@smail.uni-koeln.de (C.K.A.); ufuk.atamtuerk01@gmail.com (U.A.); andreas.lichtenberg@uni-koeln.de (A.L.); ajamil@uni-koeln.de (A.R.).

*	Correspondence: sanjay.mathur@uni-koeln.de (S.M.)

Figure S1: 1H NMR Spectrum of (ETFB) in CDCl3 at RT with schematic and arbitrary numbering.....................................................................................................................................................................2

Figure S2: 19F NMR Spectrum of (ETFB) in CDCl3 at RT with schematic and arbitrary numbering………...3

Figure S3: 1H NMR Spectrum of (H-TFB-TBA) in CDCl3 at RT with schematic and arbitrary numbering…..................................................................................................................................................................4

Figure S4: 19F NMR Spectrum of (H-TFB-TBA) in CDCl3 at RT with schematic and arbitrary numbering......................................................................................................................................................................5

Figure S5: 1H NMR spectra of complex 3 recorded in C6D6. Inset shows a magnified portion of the spectrum of (3) to illustrate the signal due to hydride ligands attached to aluminium…………………………………...6

Figure S6: 19F NMR spectra of complex 3 recorded in C6D6....................................................................................7

Figure S7. 19F NMR spectra of 4b and 4b´ recorded in C6D6 at room temperature…………………………….8

Figure S8. 13C NMR spectra of 4b and 4b´ recorded in C6D6 at room temperature……………………………..8

Figure S9. 1H−13C heteronuclear multiple bond correlation (HMBC) spectra of 4b and 4b´ at room temperature………………………………………………………………..…………………………………………..9

Figure S10. 1H−13C Heteronuclear multiple quantum coherence (HMQC) spectra of 4b and 4b´ at room temperature……………………………………………………………………….…………………………………...9

Figure S11: Solution 27Al NMR spectra of complex 3 recorded in C6D6 at room temperature………………...10

Figure S12: Solution 27Al NMR spectra of complexes 4b and 4b´ recorded in C6D6 at room temperature………………………………………………………………………………………….....…………….10

Figure S13. FT-IR spectra of the enaminone ligand (black), compound 3 (red) and compound (blue)…………………………………………………………………………………………………………………11

Figure S14: Obtained XRD pattern of the residue 3 and 4a after TG…………………….……….……………11

Figure S15. Representative SEM images of post/annealed thin films deposited using 4 as precursor in a CVD process.…………………………………………………………………………………………………………...….12

1

2

3

4

5

6

6-H

5-H

4-H

3-H

ppm

Figure S1: 1H NMR Spectrum of ETFB 1 in CDCl3 at RT with schematic and arbitrary numbering.

1

2

3

4

5

6

ppm

1-F

1-F

Figure S2: 19F NMR Spectrum of ETFB 1 in CDCl3 at RT with schematic and arbitrary numbering.

ppm

1

2

3

4

5

NH

5-H

4-H

3-H

Figure S3: 1H NMR Spectrum of H-TFB-TBA 2 in CDCl3 at RT with schematic and arbitrary numbering.

ppm

1

2

3

4

5

1-F

Figure S4: 19F NMR Spectrum of H-TFB-TBA 2 in CDCl3 at RT with schematic and arbitrary numbering.

Figure S5. 1H NMR spectra of complex (3) recorded in C6D6. Inset shows a magnified portion of the spectrum of (3) to illustrate the signal due to hydride ligands attached to aluminium.

ppm

3

5

4

1

1-F

2

Figure S6. 19F NMR spectra of complex (3) recorded in C6D6.

Figure S7. 19F NMR spectra of 4b and 4b´ recorded in C6D6 at room temperature.

Figure S8. 13C NMR spectra of 4b and 4b´ recorded in C6D6 at room temperature.

Figure S9. 1H−13C heteronuclear multiple bond correlation (HMBC) spectra of 4b and 4b´ at room temperature.

Figure S10. 1H−13C Heteronuclear multiple quantum coherence (HMQC) spectra of 4b and 4b´ at room temperature.

Figure S11: Solution 27Al NMR spectra of complex 3 recorded in C6D6 at room temperature

Figure S12: Solution 27Al NMR spectra of complexes 4b and 4b´ recorded in C6D6 at room temperature

Al-H

4b 4b´

Ligand

3

Wavenumber (cm-1)

Figure S13. FT−IR spectra of the enaminone ligand (black), compound 3 (red) and compound 4b and 4b´ (blue).

Figure S14: Obtained XRD pattern of the residue of 3 and 4a after TG.

Figure S15. Representative SEM images of post-annealed thin films deposited using 4a as precursor in a CVD process.