## Slide 1
Surface Modification of Ga-LLZO(Li7La3Zr2O12) by Addition of PAN for the Electrochemical Stability of Solid-State Battery

## Slide 2
Supplementary Materials

## Slide 3
Figure S1. Nyquist impedance plots of LiTFSI/ SCN(PCE) with various ratios of concentration.

## Slide 4
Figure S2. The schematic image and the real image of LGLZO particle that is protected by the cyclized PAN.

## Slide 5
SPE+LGLZO
Blade
SPE+PAN+LGLZO
80℃
2h
mixing
Blade
Coating
Blade
Coating
80℃
2h
mixing
Figure S3. Images of (a) SPE/LGLZO and (b) SPE/PAN/LGLZO slurry before and after 80oC, 2h mixing and the image of aged slurry after fabrication
(a)
(b)

## Slide 6
Figure S4. The cross-section SEM image of g-PPCE and the corresponding EDS mappings of N, F and La
N
F
La

## Slide 7
50㎛
(221)
(200)
(420)
(332)
(422)
(510)
(521)
(321)
(400)
Figure S5. SEM image of LGLZO and XRD pattern of LGLZO
50㎛

## Slide 8
Figure S6. XRD graphs of LGLZO green sheet, SPE, impregnated green sheet and g-PPCE samples

## Slide 9
Figure S7. FT-IR analysis

## Slide 10
Figure S8. TGA graphs of LGLZO green sheet, SPE, g-PPCE and g-PPCE samples

## Slide 11
Figure S9. Nyquist impedance plots of SSllg-PPCEllSS with different percent of PAN

## Slide 12
Figure S10. Nyquist impedance plot and the image of the LGLZO pellet(inset), and the conductivity of LGLZO pellet
 | LGLZO pellet
Conductivity (mS/cm) | 1.4

## Slide 13
Figure S11. Nyquist impedance plot of SPE

## Slide 14
Figure S12. Cyclic voltammetry curves of g-PPCE

## Slide 15
Figure S13. Nyquist impedance plots of a LFP||g-PPCE||Li-metal cell before and after galvanostatic cycling at 1C and 25 °C.
 | R1(Ω) | R2(Ω) | R3(Ω)
before cycle | 5.3 | 77 | 
after cycle | 9.8 | 98 | 92.5

## Slide 16
before cycle
after 100 cycles
Figure S14. The equivalent circuits of Nyquist impedance plots of a LFP||g-PPCE||Li-metal cell before and after galvanostatic cycling at 1C and 25 °C.