Supporting Information (SI)

for

Synthesis and Luminescence of Optical Memory Active Tetramethylammonium Cyanocuprate(I) 3D Networks

Aaron D. Nicholas1*, Rebeka M. Bullard1, Amelia M. Wheaton2, Michaela Streep2, Victoria A. Nicholas1, Robert D. Pike2, and Howard H. Patterson1

1Department of Chemistry, University of Maine, Orono, ME, 04469 and 2Department of Chemistry, College of William and Mary, Williamsburg, VA, 23185

# *Corresponding Author: 	aaron.d.nicholas@maine.edu

TABLE OF CONTENTS

Figure S1.	Unit cell diagram of 1 viewed along the b-axis	01

Figure S2.	Unit cell diagram of 2 at 298 K viewed between the a- and c-axes.	02

Figure S3.	Unit cell diagram of 2 at 100 K viewed along the a-axis	03

Figure S4.	Unit cell diagram of 3 at 100 K viewed along the b-axis	04

Table S1.	Select bond lengths of 1	05

Table S2.	Selected bond angles of 1	06

Table S3.	Select bond length of 2 at 296 K	10

Table S4.	Selected bond angles of 2 at 296 K	11

Table S5.	Selected bond lengths of 2 at 100 K	12

Table S6.	Selected bond angles of 2 at 100 K	14

Figure S5.	Vibrational infrared spectra of solid samples of 1 and 2 at 298 K	17

Figure S6.	Luminescence spectrum of (left) 1 and (right) 2 at 78 K and 298 K	18

Figure S7.	Lifetime measurements of 1 at (left) 298 K (𝜆em = 522 nm) and (right) 78 K	19

Figure S8.	Lifetime measurements of 2 at (left) 298 K (𝜆em = 420 nm) and 
	(right) 78 K (𝜆em = 440 nm)	20

Table S7.	DFT ground state parameters of 1 compared to experimental values	21

Table S8.	DFT ground state parameters of 2 compared to experimental values	21

Figure S9.	M06/CEP-31G(d) ground state structure of 1 (left) and 2 (right)	22

Table S9.	M06/CEP-31G(d) TD-DFT calculation excited state transitions for 1 at 300 nm	23

Table S10.	M06/CEP-31G(d) TD-DFT calculation excited state transitions for 2 at 330 nm	23

Figure S10.	Uncorrected optical memory results of (left) 1 and (right) 2	24

# Figure S1. Unit cell diagram of 1 viewed along the b-axis, 30% ellipsoids. Disordered atom positions and hydrogen atoms omitted.

# Figure S2. Unit cell diagram of 2 at 296 K viewed between the a- and c-axes, 30% ellipsoids. Disordered atom positions and hydrogen atoms omitted.

# Figure S3. Unit cell diagram of 2 at 100 K viewed along the a-axis, 30% ellipsoids. Disordered atom positions and hydrogen atoms omitted.

# Figure S4. Unit cell diagram of 3 at 100 K viewed along the b-axis, 30% ellipsoids. Disordered atom positions and hydrogen atoms omitted.

# Table S1. Select bond lengths of 1.

| Cu(1)-N(1B) | 1.960(4) | C(10)-H(10A) | 0.9800 |
| --- | --- | --- | --- |
| Cu(1)-C(1A) | 1.960(4) | C(10)-H(10B) | 0.9800 |
| Cu(1)-N(8) | 1.963(4) | C(10)-H(10C) | 0.9800 |
| Cu(1)-C(8) | 1.963(4) | C(11)-H(11A) | 0.9800 |
| Cu(1)-C(4)#1 | 2.089(4) | C(11)-H(11B) | 0.9800 |
| Cu(1)-C(3)#2 | 2.236(4) | C(11)-H(11C) | 0.9800 |
| Cu(1)-Cu(3)#2 | 2.5146(8) | N(10)-C(14) | 1.487(8) |
| Cu(3)-N(7) | 1.987(4) | N(10)-C(13)#8 | 1.492(5) |
| Cu(3)-C(7) | 1.987(4) | N(10)-C(13) | 1.492(5) |
| Cu(3)-C(3) | 2.007(4) | N(10)-C(12) | 1.497(7) |
| Cu(3)-N(2) | 2.023(4) | C(12)-H(12A) | 0.9800 |
| Cu(3)-C(4)#3 | 2.077(4) | C(12)-H(12B) | 0.9800 |
| Cu(3)-Cu(1)#4 | 2.5146(8) | C(12)-H(12C) | 0.9800 |
| Cu(4)-N(5) | 1.905(5) | C(13)-H(13A) | 0.9800 |
| Cu(4)-C(5) | 1.905(5) | C(13)-H(13B) | 0.9800 |
| Cu(4)-N(4) | 1.913(4) | C(13)-H(13C) | 0.9800 |
| Cu(4)-N(3) | 1.923(4) | C(14)-H(14A) | 0.9800 |
| N(2)-C(2) | 1.145(6) | C(14)-H(14B) | 0.9800 |
| C(2)-Cu(2B) | 1.934(15) | C(14)-H(14C) | 0.9800 |
| C(2)-Cu(2A) | 2.037(6) | N(11)-C(16) | 1.433(11) |
| C(2)-Cu(2A)#5 | 2.299(9) | N(11)-C(18) | 1.451(16) |
| N(3)-C(3) | 1.151(6) | N(11)-C(15) | 1.458(12) |
| C(3)-Cu(1)#4 | 2.236(4) | N(11)-C(17) | 1.595(17) |
| N(4)-C(4) | 1.152(6) | C(15)-H(15A) | 0.9800 |
| C(4)-Cu(3)#6 | 2.077(4) | C(15)-H(15B) | 0.9800 |
| C(4)-Cu(1)#1 | 2.089(4) | C(15)-H(15C) | 0.9800 |
| Cu(2A)-C(6) | 1.981(6) | C(16)-H(16A) | 0.9800 |
| Cu(2A)-N(1A) | 2.005(6) | C(16)-H(16B) | 0.9800 |
| Cu(2A)-C(2)#5 | 2.299(9) | C(16)-H(16C) | 0.9800 |
| Cu(2A)-Cu(2A)#5 | 2.436(12) | C(17)-H(17A) | 0.9800 |
| N(1A)-C(1A) | 1.161(6) | C(17)-H(17B) | 0.9800 |
| C(5)-C(5)#1 | 1.137(10) | C(17)-H(17C) | 0.9800 |
| C(6)-C(6)#7 | 1.180(8) | C(18)-H(18A) | 0.9800 |
| C(7)-C(7)#8 | 1.167(8) | C(18)-H(18B) | 0.9800 |
| C(8)-C(8)#8 | 1.151(8) | C(18)-H(18C) | 0.9800 |
| Cu(2B)-N(6) | 1.910(11) | N(12)-C(21) | 1.475(9) |
| Cu(2B)-C(1B) | 1.912(13) | N(12)-C(20)#8 | 1.491(5) |
| Cu(2B)-Cu(2B)#5 | 3.03(8) | N(12)-C(20) | 1.491(5) |
| C(1B)-N(1B) | 1.161(6) | N(12)-C(19) | 1.498(9) |
| N(5)-N(5)#1 | 1.137(10) | C(19)-H(19A) | 0.9800 |
| N(6)-N(6)#7 | 1.180(8) | C(19)-H(19B) | 0.9800 |
| N(7)-N(7)#8 | 1.167(8) | C(19)-H(19C) | 0.9800 |
| N(8)-N(8)#8 | 1.151(8) | C(20)-H(20A) | 0.9800 |
| N(9)-C(10) | 1.489(8) | C(20)-H(20B) | 0.9800 |
| N(9)-C(9) | 1.496(8) | C(20)-H(20C) | 0.9800 |
| N(9)-C(11)#7 | 1.499(5) | C(21)-H(21A) | 0.9800 |
| N(9)-C(11) | 1.499(5) | C(21)-H(21B) | 0.9800 |
| C(9)-H(9A) | 0.9800 | C(21)-H(21C) | 0.9800 |
| C(9)-H(9B) | 0.9800 | O(1)-H(1W) | 0.82(2) |
| C(9)-H(9C) | 0.9800 | O(1)-H(2W) | 0.82(2) |

# Table S2. Selected bond angles of 1.

| N(1B)-Cu(1)-N(8) | 114.59(15) | N(9)-C(10)-H(10B) | 109.5 |
| --- | --- | --- | --- |
| C(1A)-Cu(1)-C(8) | 114.59(15) | H(10A)-C(10)-H(10B) | 109.5 |
| N(1B)-Cu(1)-C(4)#1 | 111.26(16) | N(9)-C(10)-H(10C) | 109.5 |
| C(1A)-Cu(1)-C(4)#1 | 111.26(16) | H(10A)-C(10)-H(10C) | 109.5 |
| N(8)-Cu(1)-C(4)#1 | 113.11(15) | H(10B)-C(10)-H(10C) | 109.5 |
| C(8)-Cu(1)-C(4)#1 | 113.11(15) | N(9)-C(11)-H(11A) | 109.5 |
| N(1B)-Cu(1)-C(3)#2 | 111.54(16) | N(9)-C(11)-H(11B) | 109.5 |
| C(1A)-Cu(1)-C(3)#2 | 111.54(16) | H(11A)-C(11)-H(11B) | 109.5 |
| N(8)-Cu(1)-C(3)#2 | 103.14(16) | N(9)-C(11)-H(11C) | 109.5 |
| C(8)-Cu(1)-C(3)#2 | 103.14(16) | H(11A)-C(11)-H(11C) | 109.5 |
| C(4)#1-Cu(1)-C(3)#2 | 102.21(16) | H(11B)-C(11)-H(11C) | 109.5 |
| N(1B)-Cu(1)-Cu(3)#2 | 124.97(11) | C(14)-N(10)-C(13)#8 | 109.7(3) |
| C(1A)-Cu(1)-Cu(3)#2 | 124.97(11) | C(14)-N(10)-C(13) | 109.7(3) |
| N(8)-Cu(1)-Cu(3)#2 | 119.91(11) | C(13)#8-N(10)-C(13) | 109.3(5) |
| C(8)-Cu(1)-Cu(3)#2 | 119.91(11) | C(14)-N(10)-C(12) | 110.2(5) |
| C(4)#1-Cu(1)-Cu(3)#2 | 52.66(11) | C(13)#8-N(10)-C(12) | 108.9(3) |
| C(3)#2-Cu(1)-Cu(3)#2 | 49.56(11) | C(13)-N(10)-C(12) | 108.9(3) |
| N(7)-Cu(3)-C(3) | 110.75(16) | N(10)-C(12)-H(12A) | 109.5 |
| C(7)-Cu(3)-C(3) | 110.75(16) | N(10)-C(12)-H(12B) | 109.5 |
| N(7)-Cu(3)-N(2) | 105.75(15) | H(12A)-C(12)-H(12B) | 109.5 |
| C(7)-Cu(3)-N(2) | 105.75(15) | N(10)-C(12)-H(12C) | 109.5 |
| C(3)-Cu(3)-N(2) | 113.45(17) | H(12A)-C(12)-H(12C) | 109.5 |
| N(7)-Cu(3)-C(4)#3 | 106.79(16) | H(12B)-C(12)-H(12C) | 109.5 |
| C(7)-Cu(3)-C(4)#3 | 106.79(16) | N(10)-C(13)-H(13A) | 109.5 |
| C(3)-Cu(3)-C(4)#3 | 111.07(17) | N(10)-C(13)-H(13B) | 109.5 |
| N(2)-Cu(3)-C(4)#3 | 108.69(15) | H(13A)-C(13)-H(13B) | 109.5 |
| N(7)-Cu(3)-Cu(1)#4 | 123.84(11) | N(10)-C(13)-H(13C) | 109.5 |
| C(7)-Cu(3)-Cu(1)#4 | 123.84(11) | H(13A)-C(13)-H(13C) | 109.5 |
| C(3)-Cu(3)-Cu(1)#4 | 57.98(13) | H(13B)-C(13)-H(13C) | 109.5 |
| N(2)-Cu(3)-Cu(1)#4 | 129.85(10) | N(10)-C(14)-H(14A) | 109.5 |
| C(4)#3-Cu(3)-Cu(1)#4 | 53.09(11) | N(10)-C(14)-H(14B) | 109.5 |
| N(5)-Cu(4)-N(4) | 120.58(18) | H(14A)-C(14)-H(14B) | 109.5 |
| C(5)-Cu(4)-N(4) | 120.58(18) | N(10)-C(14)-H(14C) | 109.5 |
| N(5)-Cu(4)-N(3) | 119.12(18) | H(14A)-C(14)-H(14C) | 109.5 |
| C(5)-Cu(4)-N(3) | 119.12(18) | H(14B)-C(14)-H(14C) | 109.5 |
| N(4)-Cu(4)-N(3) | 120.28(15) | C(16)-N(11)-C(18) | 114.8(10) |
| C(2)-N(2)-Cu(3) | 174.4(3) | C(16)-N(11)-C(15) | 122.3(6) |
| N(2)-C(2)-Cu(2B) | 141.9(15) | C(18)-N(11)-C(15) | 106.3(10) |
| N(2)-C(2)-Cu(2A) | 153.2(5) | C(16)-N(11)-C(17) | 105.5(9) |
| N(2)-C(2)-Cu(2A)#5 | 138.7(4) | C(18)-N(11)-C(17) | 106.5(12) |
| Cu(2A)-C(2)-Cu(2A)#5 | 68.1(3) | C(15)-N(11)-C(17) | 99.3(9) |
| C(3)-N(3)-Cu(4) | 171.4(4) | N(11)-C(15)-H(15A) | 109.5 |
| N(3)-C(3)-Cu(3) | 158.9(4) | N(11)-C(15)-H(15B) | 109.5 |
| N(3)-C(3)-Cu(1)#4 | 128.2(4) | H(15A)-C(15)-H(15B) | 109.5 |
| Cu(3)-C(3)-Cu(1)#4 | 72.46(14) | N(11)-C(15)-H(15C) | 109.5 |
| C(4)-N(4)-Cu(4) | 177.7(4) | H(15A)-C(15)-H(15C) | 109.5 |
| N(4)-C(4)-Cu(3)#6 | 148.0(3) | H(15B)-C(15)-H(15C) | 109.5 |
| N(4)-C(4)-Cu(1)#1 | 137.7(3) | N(11)-C(16)-H(16A) | 109.5 |
| Cu(3)#6-C(4)-Cu(1)#1 | 74.25(14) | N(11)-C(16)-H(16B) | 109.5 |
| C(6)-Cu(2A)-N(1A) | 111.0(3) | H(16A)-C(16)-H(16B) | 109.5 |
| C(6)-Cu(2A)-C(2) | 110.1(3) | N(11)-C(16)-H(16C) | 109.5 |
| N(1A)-Cu(2A)-C(2) | 110.4(3) | H(16A)-C(16)-H(16C) | 109.5 |
| C(6)-Cu(2A)-C(2)#5 | 104.6(3) | H(16B)-C(16)-H(16C) | 109.5 |
| N(1A)-Cu(2A)-C(2)#5 | 108.6(3) | N(11)-C(17)-H(17A) | 109.5 |
| C(2)-Cu(2A)-C(2)#5 | 111.9(3) | N(11)-C(17)-H(17B) | 109.5 |
| C(6)-Cu(2A)-Cu(2A)#5 | 121.7(3) | H(17A)-C(17)-H(17B) | 109.5 |
| N(1A)-Cu(2A)-Cu(2A)#5 | 126.4(4) | N(11)-C(17)-H(17C) | 109.5 |
| C(2)-Cu(2A)-Cu(2A)#5 | 61.1(2) | H(17A)-C(17)-H(17C) | 109.5 |
| C(2)#5-Cu(2A)-Cu(2A)#5 | 50.9(3) | H(17B)-C(17)-H(17C) | 109.5 |
| C(1A)-N(1A)-Cu(2A) | 172.1(4) | N(11)-C(18)-H(18A) | 109.5 |
| N(1A)-C(1A)-Cu(1) | 174.1(3) | N(11)-C(18)-H(18B) | 109.5 |
| C(5)#1-C(5)-Cu(4) | 179.2(7) | H(18A)-C(18)-H(18B) | 109.5 |
| C(6)#7-C(6)-Cu(2A) | 175.12(18) | N(11)-C(18)-H(18C) | 109.5 |
| C(7)#8-C(7)-Cu(3) | 177.58(11) | H(18A)-C(18)-H(18C) | 109.5 |
| C(8)#8-C(8)-Cu(1) | 172.67(11) | H(18B)-C(18)-H(18C) | 109.5 |
| N(6)-Cu(2B)-C(1B) | 118.5(7) | C(21)-N(12)-C(20)#8 | 110.7(4) |
| N(6)-Cu(2B)-C(2) | 117.9(7) | C(21)-N(12)-C(20) | 110.7(4) |
| C(1B)-Cu(2B)-C(2) | 119.4(10) | C(20)#8-N(12)-C(20) | 110.4(5) |
| N(6)-Cu(2B)-Cu(2B)#5 | 110.2(18) | C(21)-N(12)-C(19) | 108.7(5) |
| C(1B)-Cu(2B)-Cu(2B)#5 | 115.1(16) | C(20)#8-N(12)-C(19) | 108.1(3) |
| C(2)-Cu(2B)-Cu(2B)#5 | 61.5(5) | C(20)-N(12)-C(19) | 108.1(4) |
| N(1B)-C(1B)-Cu(2B) | 173.2(11) | N(12)-C(19)-H(19A) | 109.5 |
| C(1B)-N(1B)-Cu(1) | 174.1(3) | N(12)-C(19)-H(19B) | 109.5 |
| N(5)#1-N(5)-Cu(4) | 179.2(7) | H(19A)-C(19)-H(19B) | 109.5 |
| N(6)#7-N(6)-Cu(2B) | 165.6(14) | N(12)-C(19)-H(19C) | 109.5 |
| N(7)#8-N(7)-Cu(3) | 177.58(11) | H(19A)-C(19)-H(19C) | 109.5 |
| N(8)#8-N(8)-Cu(1) | 172.67(11) | H(19B)-C(19)-H(19C) | 109.5 |
| C(10)-N(9)-C(9) | 109.9(5) | N(12)-C(20)-H(20A) | 109.5 |
| C(10)-N(9)-C(11)#7 | 109.7(3) | N(12)-C(20)-H(20B) | 109.5 |
| C(9)-N(9)-C(11)#7 | 109.2(3) | H(20A)-C(20)-H(20B) | 109.5 |
| C(10)-N(9)-C(11) | 109.7(3) | N(12)-C(20)-H(20C) | 109.5 |
| C(9)-N(9)-C(11) | 109.2(3) | H(20A)-C(20)-H(20C) | 109.5 |
| C(11)#7-N(9)-C(11) | 109.2(4) | H(20B)-C(20)-H(20C) | 109.5 |
| N(9)-C(9)-H(9A) | 109.5 | N(12)-C(21)-H(21A) | 109.5 |
| N(9)-C(9)-H(9B) | 109.5 | N(12)-C(21)-H(21B) | 109.5 |
| H(9A)-C(9)-H(9B) | 109.5 | H(21A)-C(21)-H(21B) | 109.5 |
| N(9)-C(9)-H(9C) | 109.5 | N(12)-C(21)-H(21C) | 109.5 |
| H(9A)-C(9)-H(9C) | 109.5 | H(21A)-C(21)-H(21C) | 109.5 |
| H(9B)-C(9)-H(9C) | 109.5 | H(21B)-C(21)-H(21C) | 109.5 |
| N(9)-C(10)-H(10A) | 109.5 | H(1W)-O(1)-H(2W) | 104(3) |

# Table S3. Select bond length of 2 at 296 K.

| Cu(1)-N(1B) | 1.917(2) | N(3A)-C(4A)#4 | 1.522(6) |
| --- | --- | --- | --- |
| Cu(1)-C(1A) | 1.917(2) | N(3A)-C(4A) | 1.522(6) |
| Cu(1)-C(2B) | 1.934(3) | C(3A)-H(3AA) | 0.9600 |
| Cu(1)-N(2A) | 1.934(3) | C(3A)-H(3AB) | 0.9600 |
| Cu(1)-C(1B)#1 | 1.939(2) | C(3A)-H(3AC) | 0.9600 |
| Cu(1)-N(1A)#1 | 1.939(2) | C(4A)-C(4A)#4 | 1.957(16) |
| Cu(2)-N(2B) | 1.850(3) | C(4A)-H(4AA) | 0.9600 |
| Cu(2)-C(2A) | 1.850(3) | C(4A)-H(4AB) | 0.9600 |
| Cu(2)-N(2B)#2 | 1.850(3) | C(4A)-H(4AC) | 0.9600 |
| Cu(2)-C(2A)#2 | 1.850(3) | N(3B)-C(4B)#4 | 1.384(10) |
| N(1A)-C(1A) | 1.150(3) | N(3B)-C(4B) | 1.384(11) |
| N(1A)-Cu(1)#3 | 1.939(2) | N(3B)-C(3B) | 1.793(12) |
| C(2A)-N(2A) | 1.144(5) | N(3B)-C(3B)#4 | 1.793(12) |
| C(1B)-N(1B) | 1.150(3) | C(3B)-H(3BA) | 0.9600 |
| C(1B)-Cu(1)#3 | 1.939(2) | C(3B)-H(3BB) | 0.9600 |
| N(2B)-C(2B) | 1.144(5) | C(3B)-H(3BC) | 0.9600 |
| N(3A)-C(3A)#4 | 1.413(5) | C(4B)-H(4BA) | 0.9600 |
| N(3A)-C(3A) | 1.413(5) | C(4B)-H(4BB) | 0.9600 |
|  |  | C(4B)-H(4BC) | 0.9600 |

# Table S4. Selected bond angles of 2 at 298 K.

| N(1B)-Cu(1)-C(2B) | 122.94(10) | N(3A)-C(4A)-C(4A)#4 | 50.0(4) |
| --- | --- | --- | --- |
| C(1A)-Cu(1)-N(2A) | 122.94(10) | N(3A)-C(4A)-H(4AA) | 109.5 |
| N(1B)-Cu(1)-C(1B)#1 | 119.21(9) | C(4A)#4-C(4A)-H(4AA) | 75.7 |
| C(2B)-Cu(1)-C(1B)#1 | 117.53(9) | N(3A)-C(4A)-H(4AB) | 109.5 |
| C(1A)-Cu(1)-N(1A)#1 | 119.21(9) | C(4A)#4-C(4A)-H(4AB) | 87.9 |
| N(2A)-Cu(1)-N(1A)#1 | 117.53(9) | H(4AA)-C(4A)-H(4AB) | 109.5 |
| N(2B)-Cu(2)-N(2B)#2 | 180 | N(3A)-C(4A)-H(4AC) | 109.5 |
| C(2A)-Cu(2)-C(2A)#2 | 180 | C(4A)#4-C(4A)-H(4AC) | 157.8 |
| C(1A)-N(1A)-Cu(1)#3 | 174.7(3) | H(4AA)-C(4A)-H(4AC) | 109.5 |
| N(1A)-C(1A)-Cu(1) | 175.0(2) | H(4AB)-C(4A)-H(4AC) | 109.5 |
| N(2A)-C(2A)-Cu(2) | 177.7(3) | C(4B)#4-N(3B)-C(4B) | 176.9(14) |
| C(2A)-N(2A)-Cu(1) | 173.0(3) | C(4B)#4-N(3B)-C(3B) | 97.7(7) |
| N(1B)-C(1B)-Cu(1)#3 | 174.7(3) | C(4B)-N(3B)-C(3B) | 83.6(7) |
| C(1B)-N(1B)-Cu(1) | 175.0(2) | C(4B)#4-N(3B)-C(3B)#4 | 83.6(7) |
| C(2B)-N(2B)-Cu(2) | 177.7(3) | C(4B)-N(3B)-C(3B)#4 | 97.7(7) |
| N(2B)-C(2B)-Cu(1) | 173.0(3) | C(3B)-N(3B)-C(3B)#4 | 128.7(14) |
| C(3A)#4-N(3A)-C(3A) | 114.1(6) | N(3B)-C(3B)-H(3BA) | 109.5 |
| C(3A)#4-N(3A)-C(4A)#4 | 120.1(5) | N(3B)-C(3B)-H(3BB) | 109.5 |
| C(3A)-N(3A)-C(4A)#4 | 109.4(4) | H(3BA)-C(3B)-H(3BB) | 109.5 |
| C(3A)#4-N(3A)-C(4A) | 109.4(4) | N(3B)-C(3B)-H(3BC) | 109.5 |
| C(3A)-N(3A)-C(4A) | 120.1(5) | H(3BA)-C(3B)-H(3BC) | 109.5 |
| C(4A)#4-N(3A)-C(4A) | 80.1(7) | H(3BB)-C(3B)-H(3BC) | 109.5 |
| N(3A)-C(3A)-H(3AA) | 109.5 | N(3B)-C(4B)-H(4BA) | 109.5 |
| N(3A)-C(3A)-H(3AB) | 109.5 | N(3B)-C(4B)-H(4BB) | 109.5 |
| H(3AA)-C(3A)-H(3AB) | 109.5 | H(4BA)-C(4B)-H(4BB) | 109.5 |
| N(3A)-C(3A)-H(3AC) | 109.5 | N(3B)-C(4B)-H(4BC) | 109.5 |
| H(3AA)-C(3A)-H(3AC) | 109.5 | H(4BA)-C(4B)-H(4BC) | 109.5 |
| H(3AB)-C(3A)-H(3AC) | 109.5 | H(4BB)-C(4B)-H(4BC) | 109.5 |

# Table S5. Selected bond lengths of 2 at 100 K.

| Cu(1A)-C(1A) | 1.830(5) | C(8B)-Cu(3)#5 | 1.944(4) |
| --- | --- | --- | --- |
| Cu(1A)-C(2A) | 1.877(5) | Cu(2)-Cu(4B)#1 | 3.015(10) |
| Cu(1A)-Cu(5)#1 | 2.913(4) | Cu(2)-Cu(4A)#1 | 3.059(3) |
| Cu(4A)-C(5A) | 1.821(5) | Cu(3)-C(8B)#5 | 1.944(4) |
| Cu(4A)-C(6A) | 1.873(5) | Cu(3)-N(8A)#5 | 1.944(4) |
| Cu(4A)-Cu(6)#2 | 3.000(3) | Cu(3)-Cu(1B)#6 | 2.971(13) |
| Cu(4A)-Cu(2)#1 | 3.059(3) | Cu(5)-C(3B)#4 | 1.948(4) |
| N(1A)-C(1A) | 1.157(5) | Cu(5)-N(3A)#4 | 1.948(4) |
| N(1A)-Cu(6)#3 | 1.942(3) | Cu(5)-Cu(1A)#1 | 2.913(4) |
| N(2A)-C(2A) | 1.155(5) | Cu(5)-Cu(1B)#1 | 3.016(11) |
| N(2A)-Cu(2) | 1.929(4) | Cu(6)-C(1B)#7 | 1.942(3) |
| C(3A)-N(3A) | 1.158(5) | Cu(6)-N(1A)#7 | 1.942(3) |
| C(3A)-Cu(2) | 1.923(4) | Cu(6)-Cu(4A)#2 | 3.000(3) |
| N(3A)-Cu(5)#4 | 1.948(4) | Cu(6)-Cu(4B)#2 | 3.004(10) |
| N(4A)-C(4A) | 1.164(5) | C(9A)-N(9) | 1.461(7) |
| N(4A)-Cu(2) | 1.950(3) | C(9A)-H(9A1) | 0.9800 |
| C(4A)-Cu(3) | 1.911(4) | C(9A)-H(9A2) | 0.9800 |
| C(5A)-N(5A) | 1.162(5) | C(9A)-H(9A3) | 0.9800 |
| N(5A)-Cu(3) | 1.931(3) | C(11A)-N(9) | 1.527(8) |
| C(6A)-N(6A) | 1.166(5) | C(11A)-H(11A) | 0.9800 |
| N(6A)-Cu(5) | 1.926(3) | C(11A)-H(11B) | 0.9800 |
| N(7A)-C(7A) | 1.173(5) | C(11A)-H(11C) | 0.9800 |
| N(7A)-Cu(6) | 1.934(3) | C(9B)-N(9) | 1.637(18) |
| C(7A)-Cu(5) | 1.916(4) | C(9B)-H(9A) | 0.9800 |
| C(8A)-N(8A) | 1.155(5) | C(9B)-H(9AB) | 0.9800 |
| C(8A)-Cu(6) | 1.921(4) | C(9B)-H(9AC) | 0.9800 |
| N(8A)-Cu(3)#5 | 1.944(4) | C(11B)-N(9) | 1.388(18) |
| Cu(1B)-N(2B) | 1.784(9) | C(11B)-H(11D) | 0.9800 |
| Cu(1B)-N(1B) | 1.930(10) | C(11B)-H(11E) | 0.9800 |
| Cu(1B)-Cu(3)#6 | 2.971(13) | C(11B)-H(11F) | 0.9800 |
| Cu(1B)-Cu(5)#1 | 3.016(11) | N(9)-C(12) | 1.478(5) |
| Cu(4B)-N(6B) | 1.770(10) | N(9)-C(10) | 1.484(5) |
| Cu(4B)-N(5B) | 1.933(12) | C(10)-H(10A) | 0.9800 |
| Cu(4B)-Cu(6)#2 | 3.004(10) | C(10)-H(10B) | 0.9800 |
| Cu(4B)-Cu(2)#1 | 3.015(10) | C(10)-H(10C) | 0.9800 |
| C(1B)-N(1B) | 1.157(5) | C(12)-H(12A) | 0.9800 |
| C(1B)-Cu(6)#3 | 1.942(3) | C(12)-H(12B) | 0.9800 |
| C(2B)-N(2B) | 1.155(5) | C(12)-H(12C) | 0.9800 |
| C(2B)-Cu(2) | 1.929(4) | N(10)-C(13) | 1.484(5) |
| N(3B)-C(3B) | 1.158(5) | N(10)-C(15) | 1.485(6) |
| N(3B)-Cu(2) | 1.923(4) | N(10)-C(16) | 1.486(5) |
| C(3B)-Cu(5)#4 | 1.948(4) | N(10)-C(14) | 1.497(5) |
| C(4B)-N(4B) | 1.164(5) | C(13)-H(13A) | 0.9800 |
| C(4B)-Cu(2) | 1.950(3) | C(13)-H(13B) | 0.9800 |
| N(4B)-Cu(3) | 1.911(4) | C(13)-H(13C) | 0.9800 |
| N(5B)-C(5B) | 1.162(5) | C(14)-H(14A) | 0.9800 |
| C(5B)-Cu(3) | 1.931(3) | C(14)-H(14B) | 0.9800 |
| N(6B)-C(6B) | 1.166(5) | C(14)-H(14C) | 0.9800 |
| C(6B)-Cu(5) | 1.926(3) | C(15)-H(15A) | 0.9800 |
| C(7B)-N(7B) | 1.173(5) | C(15)-H(15B) | 0.9800 |
| C(7B)-Cu(6) | 1.934(3) | C(15)-H(15C) | 0.9800 |
| N(7B)-Cu(5) | 1.916(4) | C(16)-H(16A) | 0.9800 |
| N(8B)-C(8B) | 1.155(5) | C(16)-H(16B) | 0.9800 |
| N(8B)-Cu(6) | 1.921(4) | C(16)-H(16C) | 0.9800 |

# Table S6. Selected bond angles of 2 at 100 K.

| C(1A)-Cu(1A)-C(2A) | 174.7(4) | N(8B)-Cu(6)-C(7B) | 119.57(14) |
| --- | --- | --- | --- |
| C(1A)-Cu(1A)-Cu(5)#1 | 102.7(2) | N(8B)-Cu(6)-C(1B)#7 | 123.83(15) |
| C(2A)-Cu(1A)-Cu(5)#1 | 81.40(15) | C(7B)-Cu(6)-C(1B)#7 | 116.24(14) |
| C(5A)-Cu(4A)-C(6A) | 176.9(3) | C(8A)-Cu(6)-N(1A)#7 | 123.83(15) |
| C(5A)-Cu(4A)-Cu(6)#2 | 87.95(16) | N(7A)-Cu(6)-N(1A)#7 | 116.24(14) |
| C(6A)-Cu(4A)-Cu(6)#2 | 90.74(15) | C(8A)-Cu(6)-Cu(4A)#2 | 83.50(12) |
| C(5A)-Cu(4A)-Cu(2)#1 | 101.25(16) | N(7A)-Cu(6)-Cu(4A)#2 | 91.10(13) |
| C(6A)-Cu(4A)-Cu(2)#1 | 79.45(15) | N(1A)#7-Cu(6)-Cu(4A)#2 | 101.54(12) |
| Cu(6)#2-Cu(4A)-Cu(2)#1 | 164.99(17) | N(8B)-Cu(6)-Cu(4B)#2 | 86.0(3) |
| C(1A)-N(1A)-Cu(6)#3 | 171.5(3) | C(7B)-Cu(6)-Cu(4B)#2 | 87.1(4) |
| N(1A)-C(1A)-Cu(1A) | 178.2(4) | C(1B)#7-Cu(6)-Cu(4B)#2 | 102.8(2) |
| C(2A)-N(2A)-Cu(2) | 171.9(3) | N(9)-C(9A)-H(9A1) | 109.5 |
| N(2A)-C(2A)-Cu(1A) | 176.6(4) | N(9)-C(9A)-H(9A2) | 109.5 |
| N(3A)-C(3A)-Cu(2) | 172.3(3) | H(9A1)-C(9A)-H(9A2) | 109.5 |
| C(3A)-N(3A)-Cu(5)#4 | 171.9(3) | N(9)-C(9A)-H(9A3) | 109.5 |
| C(4A)-N(4A)-Cu(2) | 170.8(3) | H(9A1)-C(9A)-H(9A3) | 109.5 |
| N(4A)-C(4A)-Cu(3) | 172.3(3) | H(9A2)-C(9A)-H(9A3) | 109.5 |
| N(5A)-C(5A)-Cu(4A) | 177.5(4) | N(9)-C(11A)-H(11A) | 109.5 |
| C(5A)-N(5A)-Cu(3) | 173.5(3) | N(9)-C(11A)-H(11B) | 109.5 |
| N(6A)-C(6A)-Cu(4A) | 177.8(4) | H(11A)-C(11A)-H(11B) | 109.5 |
| C(6A)-N(6A)-Cu(5) | 171.7(3) | N(9)-C(11A)-H(11C) | 109.5 |
| C(7A)-N(7A)-Cu(6) | 173.2(3) | H(11A)-C(11A)-H(11C) | 109.5 |
| N(7A)-C(7A)-Cu(5) | 172.9(3) | H(11B)-C(11A)-H(11C) | 109.5 |
| N(8A)-C(8A)-Cu(6) | 172.7(3) | N(9)-C(9B)-H(9A) | 109.5 |
| C(8A)-N(8A)-Cu(3)#5 | 172.1(3) | N(9)-C(9B)-H(9AB) | 109.5 |
| N(2B)-Cu(1B)-N(1B) | 171.2(11) | H(9A)-C(9B)-H(9AB) | 109.5 |
| N(2B)-Cu(1B)-Cu(3)#6 | 95.0(5) | N(9)-C(9B)-H(9AC) | 109.5 |
| N(1B)-Cu(1B)-Cu(3)#6 | 89.2(4) | H(9A)-C(9B)-H(9AC) | 109.5 |
| N(2B)-Cu(1B)-Cu(5)#1 | 79.8(4) | H(9AB)-C(9B)-H(9AC) | 109.5 |
| N(1B)-Cu(1B)-Cu(5)#1 | 96.7(5) | N(9)-C(11B)-H(11D) | 109.5 |
| Cu(3)#6-Cu(1B)-Cu(5)#1 | 172.3(6) | N(9)-C(11B)-H(11E) | 109.5 |
| N(6B)-Cu(4B)-N(5B) | 171.4(11) | H(11D)-C(11B)-H(11E) | 109.5 |
| N(6B)-Cu(4B)-Cu(6)#2 | 92.7(4) | N(9)-C(11B)-H(11F) | 109.5 |
| N(5B)-Cu(4B)-Cu(6)#2 | 85.9(4) | H(11D)-C(11B)-H(11F) | 109.5 |
| N(6B)-Cu(4B)-Cu(2)#1 | 82.2(4) | H(11E)-C(11B)-H(11F) | 109.5 |
| N(5B)-Cu(4B)-Cu(2)#1 | 100.0(4) | C(11B)-N(9)-C(12) | 123.5(9) |
| Cu(6)#2-Cu(4B)-Cu(2)#1 | 172.7(6) | C(9A)-N(9)-C(12) | 112.6(4) |
| N(1B)-C(1B)-Cu(6)#3 | 171.5(3) | C(11B)-N(9)-C(10) | 117.8(8) |
| C(1B)-N(1B)-Cu(1B) | 171.5(6) | C(9A)-N(9)-C(10) | 115.3(4) |
| N(2B)-C(2B)-Cu(2) | 171.9(3) | C(12)-N(9)-C(10) | 110.4(3) |
| C(2B)-N(2B)-Cu(1B) | 176.0(7) | C(9A)-N(9)-C(11A) | 107.5(5) |
| C(3B)-N(3B)-Cu(2) | 172.3(3) | C(12)-N(9)-C(11A) | 105.7(4) |
| N(3B)-C(3B)-Cu(5)#4 | 171.9(3) | C(10)-N(9)-C(11A) | 104.6(4) |
| N(4B)-C(4B)-Cu(2) | 170.8(3) | C(11B)-N(9)-C(9B) | 105.3(12) |
| C(4B)-N(4B)-Cu(3) | 172.3(3) | C(12)-N(9)-C(9B) | 96.7(7) |
| C(5B)-N(5B)-Cu(4B) | 174.5(6) | C(10)-N(9)-C(9B) | 96.1(8) |
| N(5B)-C(5B)-Cu(3) | 173.5(3) | N(9)-C(10)-H(10A) | 109.5 |
| C(6B)-N(6B)-Cu(4B) | 172.2(7) | N(9)-C(10)-H(10B) | 109.5 |
| N(6B)-C(6B)-Cu(5) | 171.7(3) | H(10A)-C(10)-H(10B) | 109.5 |
| N(7B)-C(7B)-Cu(6) | 173.2(3) | N(9)-C(10)-H(10C) | 109.5 |
| C(7B)-N(7B)-Cu(5) | 172.9(3) | H(10A)-C(10)-H(10C) | 109.5 |
| C(8B)-N(8B)-Cu(6) | 172.7(3) | H(10B)-C(10)-H(10C) | 109.5 |
| N(8B)-C(8B)-Cu(3)#5 | 172.1(3) | N(9)-C(12)-H(12A) | 109.5 |
| C(3A)-Cu(2)-N(2A) | 125.09(15) | N(9)-C(12)-H(12B) | 109.5 |
| N(3B)-Cu(2)-C(2B) | 125.09(15) | H(12A)-C(12)-H(12B) | 109.5 |
| N(3B)-Cu(2)-C(4B) | 116.23(14) | N(9)-C(12)-H(12C) | 109.5 |
| C(2B)-Cu(2)-C(4B) | 118.30(15) | H(12A)-C(12)-H(12C) | 109.5 |
| C(3A)-Cu(2)-N(4A) | 116.23(14) | H(12B)-C(12)-H(12C) | 109.5 |
| N(2A)-Cu(2)-N(4A) | 118.30(15) | C(13)-N(10)-C(15) | 109.2(4) |
| N(3B)-Cu(2)-Cu(4B)#1 | 85.2(3) | C(13)-N(10)-C(16) | 110.5(3) |
| C(2B)-Cu(2)-Cu(4B)#1 | 106.0(2) | C(15)-N(10)-C(16) | 108.7(3) |
| C(4B)-Cu(2)-Cu(4B)#1 | 84.0(4) | C(13)-N(10)-C(14) | 109.8(3) |
| C(3A)-Cu(2)-Cu(4A)#1 | 87.37(12) | C(15)-N(10)-C(14) | 110.1(4) |
| N(2A)-Cu(2)-Cu(4A)#1 | 107.46(12) | C(16)-N(10)-C(14) | 108.5(3) |
| N(4A)-Cu(2)-Cu(4A)#1 | 80.09(14) | N(10)-C(13)-H(13A) | 109.5 |
| N(4B)-Cu(3)-C(5B) | 122.41(14) | N(10)-C(13)-H(13B) | 109.5 |
| C(4A)-Cu(3)-N(5A) | 122.41(14) | H(13A)-C(13)-H(13B) | 109.5 |
| N(4B)-Cu(3)-C(8B)#5 | 119.29(14) | N(10)-C(13)-H(13C) | 109.5 |
| C(5B)-Cu(3)-C(8B)#5 | 117.95(14) | H(13A)-C(13)-H(13C) | 109.5 |
| C(4A)-Cu(3)-N(8A)#5 | 119.29(14) | H(13B)-C(13)-H(13C) | 109.5 |
| N(5A)-Cu(3)-N(8A)#5 | 117.95(14) | N(10)-C(14)-H(14A) | 109.5 |
| N(4B)-Cu(3)-Cu(1B)#6 | 87.9(3) | N(10)-C(14)-H(14B) | 109.5 |
| C(5B)-Cu(3)-Cu(1B)#6 | 102.0(2) | H(14A)-C(14)-H(14B) | 109.5 |
| C(8B)#5-Cu(3)-Cu(1B)#6 | 85.7(2) | N(10)-C(14)-H(14C) | 109.5 |
| C(7A)-Cu(5)-N(6A) | 126.22(14) | H(14A)-C(14)-H(14C) | 109.5 |
| N(7B)-Cu(5)-C(6B) | 126.22(14) | H(14B)-C(14)-H(14C) | 109.5 |
| N(7B)-Cu(5)-C(3B)#4 | 116.56(14) | N(10)-C(15)-H(15A) | 109.5 |
| C(6B)-Cu(5)-C(3B)#4 | 116.84(14) | N(10)-C(15)-H(15B) | 109.5 |
| C(7A)-Cu(5)-N(3A)#4 | 116.56(14) | H(15A)-C(15)-H(15B) | 109.5 |
| N(6A)-Cu(5)-N(3A)#4 | 116.84(14) | N(10)-C(15)-H(15C) | 109.5 |
| C(7A)-Cu(5)-Cu(1A)#1 | 78.50(14) | H(15A)-C(15)-H(15C) | 109.5 |
| N(6A)-Cu(5)-Cu(1A)#1 | 109.32(14) | H(15B)-C(15)-H(15C) | 109.5 |
| N(3A)#4-Cu(5)-Cu(1A)#1 | 87.88(12) | N(10)-C(16)-H(16A) | 109.5 |
| N(7B)-Cu(5)-Cu(1B)#1 | 82.6(3) | N(10)-C(16)-H(16B) | 109.5 |
| C(6B)-Cu(5)-Cu(1B)#1 | 106.4(2) | H(16A)-C(16)-H(16B) | 109.5 |
| C(3B)#4-Cu(5)-Cu(1B)#1 | 86.5(2) | N(10)-C(16)-H(16C) | 109.5 |
| C(8A)-Cu(6)-N(7A) | 119.57(14) | H(16A)-C(16)-H(16C) | 109.5 |
|  |  | H(16B)-C(16)-H(16C) | 109.5 |

# Figure S5. Vibrational infrared spectra of solid samples of 1 and 2 at 298 K.

# Figure S6. Luminescence spectrum of (left) 1 and (right) 2 at 78 K and 298 K.

Figure S7. Lifetime measurements of 1 at (left) 298 K (𝜆em = 522 nm) and (right) 78 K. An excitation wavelength of 350 nm was used for both lifetime measurements.

Figure S8. Lifetime measurements of 2 at (left) 298 K (𝜆em = 420 nm) and (right) 78 K (𝜆em = 440 nm). An excitation wavelength of 350 nm was used for both lifetime measurements.

Table S7. DFT ground state parameters of 1 compared to experimental values.

|  | Distances (Å)/Angles(o) |  |  |
| --- | --- | --- | --- |
|  | M06/CEP-31G(d) | B3LYP/SDD | Experimental |
| Cu⋯Cu (Rhomboid) | 2.673 | 2.806 | 2.489 |
| CuC3v⋯NMe4+ | 5.349 | 5.674 | 5.718 |
| NC-CuC3v-CN | 120.0 | 120.0 | 120.0 |
| (𝜇2-CN)-Cu-(𝜇2-CN) | 110.7 | 107.2 | 108.4 |

Table S8. DFT ground state parameters of 2 compared to experimental values.

|  | Distances (Å)/Angles(o) |  |  |
| --- | --- | --- | --- |
|  | M06/CEP-31G(d) | B3LYP/SDD | Experimental |
| CuC3v⋯CuC3v | 5.127 | 5.116 | 4.980 |
| CuC3v⋯CuC∞v | 5.223 | 5.166 | 4.926 |
| CuC∞v⋯NMe4+ | 4.935 | 5.510 | 5.141 |
| Cu-Cu-Cu | 166.1 | 172.0 | 175.4 |
| NC-CuC3v-CN | 107.3 | 107.6 | 118.5 |

Figure S9. M06/CEP-31G(d) ground state structure of 1(left) and 2 (right).

Table S9. M06/CEP-31G(d) TD-DFT calculation excited state transitions for 1 at 300 nm. Percent contributions noted.

| Transition |  |  | Contribution | Percent Contribution |
| --- | --- | --- | --- | --- |
| HOMO-5 | ➝ | LUMO+4 | 0.29692 | 27% |
| HOMO-5 | ➝ | LUMO | 0.2794 | 24% |
| HOMO | ➝ | LUMO | 0.25509 | 20% |
| HOMO-8 | ➝ | LUMO+4 | 0.1319 | 5% |
| HOMO-5 | ➝ | LUMO+6 | 0.12917 | 5% |
| HOMO-5 | ➝ | LUMO+2 | 0.12013 | 4% |
| HOMO | ➝ | LUMO+8 | –0.10686 | 4% |
| HOMO | ➝ | LUMO+5 | 0.10579 | 3% |
| HOMO | ➝ | LUMO+1 | 0.10518 | 3% |
| HOMO-2 | ➝ | LUMO | –0.10325 | 3% |

Table S10. M06/CEP-31G(d) TD-DFT calculation excited state transitions for 2 at 330 nm. Percent contributions noted.

| Transition |  |  | Contribution | Percent Contribution |
| --- | --- | --- | --- | --- |
| HOMO-8 | ➝ | LUMO | 0.32687 | 24% |
| HOMO-9 | ➝ | LUMO | –0.2935 | 19% |
| HOMO-8 | ➝ | LUMO+1 | –0.2126 | 10% |
| HOMO-4 | ➝ | LUMO+1 | –0.1919 | 8% |
| HOMO-6 | ➝ | LUMO+1 | –0.17759 | 7% |
| HOMO-6 | ➝ | LUMO+3 | –0.14608 | 5% |
| HOMO-7 | ➝ | LUMO+1 | 0.14025 | 4% |
| HOMO-6 | ➝ | LUMO | 0.13889 | 4% |
| HOMO-3 | ➝ | LUMO+1 | –0.13586 | 4% |
| HOMO-9 | ➝ | LUMO+1 | –0.13421 | 4% |
| HOMO-2 | ➝ | LUMO+1 | –0.12752 | 4% |
| HOMO-7 | ➝ | LUMO | 0.12265 | 3% |
| HOMO-6 | ➝ | LUMO+2 | 0.11918 | 3% |

Figure S10. Uncorrected optical memory results of (left) 1 and (right) 2.