Supplementary Materials: Dual-Responsive Nanotubes Assembled by Amphiphilic Dendrimers: Controlled Release and Crosslinking

Minghui Zhang 1,2, Hui Yang 1,*, Jiazhong Wu 3, Siyu Yang 3, Danfeng Yu 4, Xu Wu 4, Aiqing Ma 5, Keji Sun 5 and Jinben Wang 1

Minghui Zhang 1,2, Hui Yang 1,*, Jiazhong Wu 3, Siyu Yang 3, Danfeng Yu 4, Xu Wu 4, Aiqing Ma 5, Keji Sun 5 and Jinben Wang 1

1	CAS Key Lab of Colloid, Interface and Chemical Thermodynamics, Institute of Chemistry, Chinese Academy of Sciences, Beijing 100190, China; zhangminghui@iccas.ac.cn (M.Z.); jbwang@iccas.ac.cn (J.W.)

2	University of Chinese Academy of Sciences, Beijing 100049, China

3	State Key Laboratory of Enhanced Oil Recovery, Research Institute of Petroleum Exploration and Development of PetroChina, Beijing 100083, China; wujiazhong@petrochina.com.cn (J.W.); yangsiy@petrochina.com.cn (S.Y.)

4	Department of Chemistry and Chemical Engineering, Guangzhou University, Guangzhou 510006, China; ccyudanfeng@gzhu.edu.cn (D.Y.); xuwu@gzhu.edu.cn (X.W.)

5	Petroleum Engineering Technology Research Institute, Shengli Oilfield Branch, China Petrochemical Corporation LTD, Dongying 257000, China; maq7979@163.com (A.M.); skj502@sina.com (K.S.)

*	Correspondence: yanghui@iccas.ac.cn; Tel: +8610-62523395; Fax: +8610-62523395

GnC12 was synthesized using 0.5 G, 1.5 G, and 2.5 G Polyamindoamine (PAMAM) as the core material. The tertiary amine was introduced by reaction with N,N-Dimethyl-1,2-ethanediamine. Then, the tertiary amine groups reacted with 1-bromododecane to form the quaternary ammonium compound. All the products were recrystallized by acetone or ethanol repeatedly and characterized by 1H NMR. Taking G1C12 for example, a scheme of the reaction is shown in Scheme S1.

Scheme S1. The synthesis pathway of the amphiphilic dendrimer G1C12.

G1C12: 1H NMR (400 MHz, CDCl3) δ 9.63–8.10 (m, 4H), 3.90 (t, J = 84.9 Hz, 16H), 3.47 (d, J = 46.1 Hz, 32H), 3.19 (s, 4H), 3.09–2.79 (m, 8H), 2.78–2.32 (m, 8H), 1.75 (s, 8H), 1.25 (s, 72H), 0.88 (t, J = 6.7 Hz, 12H).

G2C12: 1H NMR (400 MHz, CDCl3) δ 9.45–8.39 (m, 8H), 8.05 (s, 4H), 3.74 (s, 32H), 3.51 (s, 24H), 3.32 (d, J = 16.6 Hz, 48H), 2.46–2.75 (t, 40H), 1.74–2.01 (s, 36H), 1.25–1.35 (m, 144H), 0.88 (t, J = 6.9 Hz, 24H).

G3C12: 1H NMR (400 MHz, CDCl3) δ 8.72 (d, J = 60.5 Hz, 16H), 8.09 (s, 8H), 7.93 (s, 4H), 3.59 (d, J = 111.3 Hz, 120H), 3.31 (d, J = 38.3 Hz, 96H), 2.75 (s, 56H), 2.62–2.21 (m, 80H), 1.74 (s, 36H), 1.28 (d, J = 41.4 Hz, 288H), 0.86 (t, J = 6.6 Hz, 48H).

Figure S1. Characterization data of G1C12 using 1H NMR.

Figure S2. Characterization data of G2C12 using 1H NMR.

Figure S3. Characterization data of G3C12 using 1H NMR.

Figure S4. TGA curves of pristine HNTs, HNTs@(G1C12/PSS)5.5, HNTs@(G2C12/PSS)5.5, and HNTs@(G3C12/PSS)5.5 under N2.

Figure S5. The 5 µm × 5 µm AFM images: (a) (G1C12/PSS)5.5; (b) (G2C12/PSS)5.5; (c) (G3C12/PSS)5.5.

Figure S6. Shifts of frequency and dissipation for multilayers in response to different salt concentrations as a function of time for bare silica substrate.

Figure S7. The 5 µm × 5 µm AFM images of adosorbed (G1C12/PSS)5.5 films in response to different pH buffer solutions: (a) pH = 5; (b) pH = 3; (c) pH = 1.