Supporting Information

Thermogelling Behaviors of Aqueous Poly(N-isopropylacrylamide-co-2-hydroxyethyl methacrylate) Microgel-Silica Nanoparticle Composite Dispersions

Byung Soo Hwang,1,† Jong Sik Kim2,† , Ju Min Kim1,2,* and Tae Soup Shim1,2,*

1	Department of Chemical Engineering and 2Department of Energy Systems Research, Ajou University, Suwon 16499, Republic of Korea

*	Correspondence: jumin@ajou.ac.kr; tsshim@ajou.ac.kr

† These authors contributed equally to this work.

Figure 1. (a) UV-vis spectrum of p(NiPAm-co-HEMA) microgel dispersion with molar ratio between NiPAm and HEMA of 7:3 at various pH values. The increase of transmittance at acidic of pH 4 and alkalic of pH 10 is attributed to the sedimentation of microgels. (b, c) photograph images of p(NiPAm-co-HEMA) microgel dispersion at (b) pH 4, and (c) pH 10. Photos were taken after slightly shaking the sedimented microgels solution for the visualization.

Figure 2. Microscopic images of p(NiPAm-co-HEMA) microgel and silica nanoparticle composite. The composite was 1:5 in weight ratio. (a) Small aggregates at room temperature. (b) local aggregation as the temperature increases. (c) Global aggregation and gelation of the composite with 1:5 weight ratio.

Figure 3. Evolution of dynamic modulus of 1:5 weight ratio composite. Turnover of G’(storage modulus) and G”(loss modulus) was observed 51.3℃. .