# Adsorption tests for thermodynamic and kinetic analysis

## Thermodynamic analysis of gold adsorption in CA Langmuir Isotherm

Table S1. Experimental data of gold adsorption in AC for the determination of the Langmuir Isotherm

| Particle Size | Activate Carbon Mass | Ci | Ce | 1/Ce | Log Ce | Ln Ce | qe | 1/qe | Log qe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (micron) | (g) | mg/L | mg/L |  |  |  |  |  |  |
| 106 | 0.010 | 10 | 8.698 | 0.115 | 0.939 | 2.163 | 65.100 | 0.015 | 1.814 |  |
|  | 0.050 |  | 5.903 | 0.169 | 0.771 | 1.775 | 40.970 | 0.024 | 1.612 |  |
|  | 0.125 |  | 2.345 | 0.426 | 0.370 | 0.852 | 30.620 | 0.033 | 1.486 |  |
|  | 0.250 |  | 0.172 | 5.814 | -0.764 | -1.760 | 19.656 | 0.051 | 1.293 |  |
| 75 | 0.010 | 10 | 8.363 | 0.120 | 0.922 | 2.124 | 81.850 | 0.012 | 1.913 |  |
|  | 0.050 |  | 5.315 | 0.188 | 0.726 | 1.671 | 46.850 | 0.021 | 1.671 |  |
|  | 0.125 |  | 1.483 | 0.674 | 0.171 | 0.394 | 34.068 | 0.029 | 1.532 |  |
|  | 0.250 |  | 0.155 | 6.452 | -0.810 | -1.864 | 19.690 | 0.051 | 1.294 |  |
| 53 | 0.010 | 10 | 9.258 | 0.108 | 0.967 | 2.225 | 37.100 | 0.027 | 1.569 |  |
|  | 0.050 |  | 5.766 | 0.173 | 0.761 | 1.752 | 42.340 | 0.024 | 1.627 |  |
|  | 0.125 |  | 1.837 | 0.544 | 0.264 | 0.608 | 32.652 | 0.031 | 1.514 |  |
|  | 0.250 |  | 0.244 | 4.098 | -0.613 | -1.411 | 19.512 | 0.051 | 1.290 |  |
| 45 | 0.010 | 10 | 8.822 | 0.113 | 0.946 | 2.177 | 58.900 | 0.017 | 1.770 |  |
|  | 0.050 |  | 5.544 | 0.180 | 0.744 | 1.713 | 44.560 | 0.022 | 1.649 |  |
|  | 0.125 |  | 1.369 | 0.730 | 0.136 | 0.314 | 34.524 | 0.029 | 1.538 |  |
|  | 0.250 |  | 0.204 | 4.902 | -0.690 | -1.590 | 19.592 | 0.051 | 1.292 |  |
| 38 | 0.010 | 10 | 8.890 | 0.112 | 0.949 | 2.185 | 55.500 | 0.018 | 1.744 |  |
|  | 0.050 |  | 5.505 | 0.182 | 0.741 | 1.706 | 44.950 | 0.022 | 1.653 |  |
|  | 0.125 |  | 1.294 | 0.773 | 0.112 | 0.258 | 34.824 | 0.029 | 1.542 |  |
|  | 0.250 |  | 0.211 | 4.739 | -0.676 | -1.556 | 19.578 | 0.051 | 1.292 |  |

Table S2. Parameters obtained from the gold adsorption in AC for the determination of the Langmuir Isotherm (1/Ce vs 1/qe)

| Particle Size (micron) | Parameters |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | b | m | qmax (mg/g) | KL | RL | R^2 |
| 106 | 0.0228 | 0.0049 | 43.8596 | 4.6531 | 0.0210 | 0.8175 |
| 75 | 0.0191 | 0.0050 | 52.3560 | 3.8200 | 0.0255 | 0.8706 |
| 53 | 0.0253 | 0.0064 | 39.5257 | 3.9531 | 0.0247 | 0.9737 |
| 45 | 0.0205 | 0.0063 | 48.7805 | 3.2540 | 0.0298 | 0.9499 |
| 38 | 0.0205 | 0.0065 | 48.7805 | 3.1538 | 0.0307 | 0.9679 |

Figure S1. Gold adsorption graphs in AC Langmuir Isotherm (1/Ce vs 1/qe)

## Thermodynamic analysis of gold adsorption in AC Temkin Isotherm

Table S3. Experimental data of gold adsorption in AC for the determination of the Temkin Isotherm

| Particle Size | AC Mass | Ci | Ce | Ln Ce | qe |
| --- | --- | --- | --- | --- | --- |
| (microns) | (g) | mg/L | mg/L |  |  |
| 106 | 0.010 | 10 | 8.698 | 2.163 | 65.100 |  |
|  | 0.050 |  | 5.903 | 1.775 | 40.970 |  |
|  | 0.125 |  | 2.345 | 0.852 | 30.620 |  |
|  | 0.250 |  | 0.172 | -1.760 | 19.656 |  |
| 75 | 0.010 | 10 | 8.363 | 2.124 | 81.850 |  |
|  | 0.050 |  | 5.315 | 1.671 | 46.850 |  |
|  | 0.125 |  | 1.483 | 0.394 | 34.068 |  |
|  | 0.250 |  | 0.155 | -1.864 | 19.690 |  |
| 53 | 0.010 | 10 | 9.258 | 2.225 | 37.100 |  |
|  | 0.050 |  | 5.766 | 1.752 | 42.340 |  |
|  | 0.125 |  | 1.837 | 0.608 | 32.652 |  |
|  | 0.250 |  | 0.244 | -1.411 | 19.512 |  |
| 45 | 0.010 | 10 | 8.822 | 2.177 | 58.900 |  |
|  | 0.050 |  | 5.544 | 1.713 | 44.560 |  |
|  | 0.125 |  | 1.369 | 0.314 | 34.524 |  |
|  | 0.250 |  | 0.204 | -1.590 | 19.592 |  |
| 38 | 0.010 | 10 | 8.890 | 2.185 | 55.500 |  |
|  | 0.050 |  | 5.505 | 1.706 | 44.950 |  |
|  | 0.125 |  | 1.294 | 0.258 | 34.824 |  |
|  | 0.250 |  | 0.211 | -1.556 | 19.578 |  |

Table S4. Parameters obtained from the gold adsorption in AC for the determination of the Temkin Isotherm (Ln Ce contra qe)

| Particle Size (microns) | Parameters |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | b | m | BT(J/mol) | KT (L/mg) | R^2 |
| 106 | 32.077 | 9.2522 | 9.2522 | 32.039 | 0.709 |
| 75 | 38.168 | 12.816 | 12.816 | 19.651 | 0.742 |
| 53 | 28.396 | 5.6752 | 5.6752 | 148.937 | 0.885 |
| 45 | 33.211 | 9.4598 | 9.4598 | 33.473 | 0.934 |
| 38 | 32.905 | 8.9616 | 8.9616 | 39.322 | 0.971 |

Figure S2. Gold adsorption graphs in AC Temkin Isotherm (Ln Ce vs qe)

## Kinetic analysis of gold adsorption in AC using the pseudo first order model

Table S5. Experimental data of the adsorption of gold in AC size 106 microns for the determination of the kinetic speed constant using the pseudo first order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 106-1 |  |  | 106-2 |  |  | 106-3 |  |  | 106-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.645 | 1.775 | 1.555 | 8.832 | 1.168 | 1.075 | 7.939 | 0.824 | 0.805 | 6.920 | 0.616 | 0.300 |
| 3 |  | 9.637 | 1.815 | 1.546 | 8.708 | 1.292 | 1.031 | 7.785 | 0.886 | 0.777 | 5.475 | 0.905 | 0.059 |
| 5 |  | 9.672 | 1.640 | 1.583 | 8.575 | 1.425 | 0.983 | 6.861 | 1.256 | 0.591 | 4.302 | 1.140 | -0.191 |
| 10 |  | 9.483 | 2.585 | 1.367 | 8.485 | 1.515 | 0.949 | 5.646 | 1.742 | 0.278 | 2.535 | 1.493 | -0.750 |
| 15 |  | 9.316 | 3.420 | 1.128 | 7.324 | 2.676 | 0.351 | 5.21 | 1.916 | 0.136 | 1.991 | 1.602 | -1.011 |
| 20 |  | 9.195 | 4.025 | 0.910 | 7.09 | 2.910 | 0.171 | 4.328 | 2.269 | -0.232 | 1.450 | 1.710 | -1.364 |
| 30 |  | 9.162 | 4.190 | 0.842 | 6.509 | 3.491 | -0.501 | 3.422 | 2.631 | -0.842 | 0.766 | 1.847 | -2.130 |
| 40 |  | 9.047 | 4.765 | 0.557 | 6.418 | 3.582 | -0.664 | 3.209 | 2.716 | -1.062 | 0.558 | 1.888 | -2.561 |
| 50 |  | 9.029 | 4.855 | 0.504 | 6.239 | 3.761 | -1.091 | 2.93 | 2.828 | -1.452 | 0.373 | 1.925 | -3.214 |
| 60 |  | 8.758 | 6.210 | -1.204 | 6.17 | 3.830 | -1.321 | 2.864 | 2.854 | -1.572 | 0.288 | 1.942 | -3.764 |
| 90 |  | 8.747 | 6.265 | -1.406 | 5.968 | 4.032 | -2.733 | 2.467 | 3.013 | -3.020 | 0.199 | 1.960 | -5.221 |
| 120 |  | 8.698 | 6.510 | - | 5.903 | 4.097 | - | 2.345 | 3.062 | - | 0.172 | 1.966 | - |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 6.510 |  |  | 4.097 |  |  | 3.062 |  |  | 1.966 |  |  |

Table S6. Parameters obtained from the adsorption of gold in AC size 106 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

| Test ID | Parameters |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | K1 | R^2 |
| 106-1 | 1.7152 | -0.0354 | 5.5578 | -0.00030 | 0.9017 |
| 106-2 | 1.1155 | -0.0433 | 3.0511 | -0.00036 | 0.9846 |
| 106-3 | 0.7399 | -0.0424 | 2.0957 | -0.00035 | 0.9841 |
| 106-4 | 0.0136 | -0.0617 | 1.0137 | -0.00051 | 0.9849 |

Figure S3. Gold adsorption graphs in AC size 106 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

Table S7. Experimental data of the adsorption of gold in AC size 75 microns for the determination of the kinetic speed constant using the pseudo first order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 75-1 |  |  | 75-2 |  |  | 75-3 |  |  | 75-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.234 | 3.830 | 1.471 | 7.181 | 2.819 | 0.624 | 5.972 | 1.611 | 0.585 | 2.585 | 1.483 | -0.722 |
| 3 |  | 8.783 | 6.085 | 0.742 | 7.027 | 2.973 | 0.538 | 4.678 | 2.129 | 0.245 | 2.739 | 1.452 | -0.660 |
| 5 |  | 8.582 | 7.090 | 0.091 | 6.574 | 3.426 | 0.230 | 4.523 | 2.191 | 0.196 | 3.014 | 1.397 | -0.559 |
| 10 |  | 8.531 | 7.345 | -0.174 | 6.187 | 3.813 | -0.137 | 3.103 | 2.759 | -0.434 | 1.182 | 1.764 | -1.583 |
| 15 |  | 8.529 | 7.355 | -0.186 | 6.074 | 3.926 | -0.276 | 3.369 | 2.652 | -0.282 | 0.758 | 1.848 | -2.115 |
| 20 |  | 8.501 | 7.495 | -0.371 | 5.96 | 4.040 | -0.439 | 3.005 | 2.798 | -0.496 | 0.426 | 1.915 | -2.915 |
| 30 |  | 8.464 | 7.680 | -0.683 | 5.637 | 4.363 | -1.133 | 2.292 | 3.083 | -1.128 | 0.335 | 1.933 | -3.324 |
| 40 |  | 8.461 | 7.695 | -0.713 | 5.515 | 4.485 | -1.609 | 1.995 | 3.202 | -1.586 | 0.236 | 1.953 | -4.123 |
| 50 |  | 8.414 | 7.930 | -1.366 | 5.512 | 4.488 | -1.625 | 1.623 | 3.351 | -2.882 | 0.221 | 1.956 | -4.328 |
| 60 |  | 8.413 | 7.935 | -1.386 | 5.464 | 4.536 | -1.904 | 1.621 | 3.352 | -2.897 | 0.222 | 1.956 | -4.313 |
| 90 |  | 8.39 | 8.050 | -2.002 | 5.379 | 4.621 | -2.749 | 1.524 | 3.390 | -4.110 | 0.158 | 1.968 | -7.419 |
| 120 |  | 8.363 | 8.185 | - | 5.315 | 4.685 | - | 1.483 | 3.407 | - | 0.155 | 1.969 | - |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 8.185 |  |  | 4.685 |  |  | 3.407 |  |  | 1.969 |  |  |

Table S8. Parameters obtained from the adsorption of gold in CA size 75 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

| Test ID | Parameters |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | K1 | R^2 |
| 75-1 | 0.5278 | 0.0300 | 1.6952 | 0.00025 | 0.9074 |
| 75-2 | 0.2819 | -0.0687 | 1.3256 | -0.00057 | 0.9547 |
| 75-3 | 0.3588 | -0.0479 | 1.4316 | -0.00040 | 0.9239 |
| 75-4 | 0.2776 | -0.1226 | 1.3200 | -0.00102 | 0.9967 |

Figure S4. Gold adsorption graphs in AC size 75 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

Table S9. Experimental data of the adsorption of gold in AC size 53 microns for the determination of the kinetic speed constant using the pseudo first order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 53-1 |  |  | 53-2 |  |  | 53-3 |  |  | 53-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.98 | 0.100 | 1.284 | 6.777 | 3.223 | 0.011 | 3.155 | 2.738 | -0.640 | 1.203 | 1.759 | -1.651 |
| 3 |  | 9.61 | 1.950 | 0.565 | 6.298 | 3.702 | -0.631 | 3.134 | 2.746 | -0.656 | 0.798 | 1.840 | -2.200 |
| 5 |  | 9.407 | 2.965 | -0.294 | 6.282 | 3.718 | -0.662 | 3.046 | 2.782 | -0.726 | 0.563 | 1.887 | -2.752 |
| 10 |  | 9.574 | 2.130 | 0.457 | 6.093 | 3.907 | -1.118 | 2.635 | 2.946 | -1.142 | 0.460 | 1.908 | -3.142 |
| 15 |  | 9.474 | 2.630 | 0.077 | 5.973 | 4.027 | -1.575 | 2.533 | 2.987 | -1.279 | 0.370 | 1.926 | -3.681 |
| 20 |  | 9.43 | 2.850 | -0.151 | 5.896 | 4.104 | -2.040 | 2.221 | 3.112 | -1.873 | 0.354 | 1.929 | -3.817 |
| 30 |  | 9.432 | 2.840 | -0.139 | 5.884 | 4.116 | -2.137 | 2.186 | 3.126 | -1.969 | 0.298 | 1.940 | -4.528 |
| 40 |  | 9.35 | 3.250 | -0.777 | 5.875 | 4.125 | -2.216 | 2.022 | 3.191 | -2.604 | 0.290 | 1.942 | -4.689 |
| 50 |  | 9.321 | 3.395 | -1.155 | 5.872 | 4.128 | -2.244 | 1.889 | 3.244 | -3.873 | 0.288 | 1.942 | -4.733 |
| 60 |  | 9.314 | 3.430 | -1.273 | 5.849 | 4.151 | -2.489 | 1.855 | 3.258 | -4.934 | 0.283 | 1.943 | -4.854 |
| 90 |  | 9.282 | 3.590 | -2.120 | 5.841 | 4.159 | -2.590 | 1.845 | 3.262 | -5.745 | 0.268 | 1.946 | -5.339 |
| 120 |  | 9.258 | 3.710 | - | 5.766 | 4.234 | - | 1.837 | 3.265 | - | 0.244 | 1.951 | - |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 3.710 |  |  | 4.234 |  |  | 3.265 |  |  | 1.951 |  |  |

Table S10. Parameters obtained from the adsorption of gold in CA size 53 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

| Test ID | Parameters |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | K1 | R^2 |
| 53-1 | 0.6175 | -0.0318 | 1.8543 | -0.00027 | 0.8695 |
| 53-2 | -0.8377 | -0.0262 | 0.4327 | -0.00022 | 0.7043 |
| 53-3 | -0.4717 | -0.0625 | 0.6239 | -0.00052 | 0.9674 |
| 53-4 | -2.6544 | -0.0376 | 0.0703 | -0.00031 | 0.7790 |

Figure S5. Gold adsorption graphs in AC size 53 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

Table S11. Experimental data of the adsorption of gold in AC size 45 microns for the determination of the kinetic speed constant using the pseudo first order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 44-1 |  |  | 45-2 |  |  | 45-3 |  |  | 45-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.381 | 3.095 | 1.028 | 6.318 | 3.682 | -0.256 | 3.034 | 2.786 | -0.406 | 2.063 | 1.587 | -0.989 |
| 3 |  | 8.899 | 5.505 | -0.955 | 5.796 | 4.204 | -1.378 | 2.8 | 2.880 | -0.558 | 0.813 | 1.837 | -2.105 |
| 5 |  | 8.857 | 5.715 | -1.743 | 5.741 | 4.259 | -1.625 | 2.277 | 3.089 | -1.013 | 0.523 | 1.895 | -2.752 |
| 10 |  | 8.843 | 5.785 | -2.254 | 5.817 | 4.183 | -1.298 | 1.957 | 3.217 | -1.447 | 0.318 | 1.936 | -3.781 |
| 15 |  | 8.8 | 6.000 | - | 5.681 | 4.319 | -1.988 | 1.762 | 3.295 | -1.850 | 0.260 | 1.948 | -4.492 |
| 20 |  | 8.795 | 6.025 | - | 5.65 | 4.350 | -2.244 | 1.637 | 3.345 | -2.233 | 0.248 | 1.950 | -4.733 |
| 30 |  | 8.749 | 6.255 | - | 5.575 | 4.425 | -3.474 | 1.526 | 3.390 | -2.768 | 0.217 | 1.957 | -5.952 |
| 40 |  | 8.9 | 5.500 | -0.942 | 5.771 | 4.229 | -1.483 | 1.478 | 3.409 | -3.133 | 0.207 | 1.959 | -7.419 |
| 50 |  | 8.895 | 5.525 | -1.008 | 5.611 | 4.389 | -2.703 | 1.518 | 3.393 | -2.820 | 0.196 | 1.961 | - |
| 60 |  | 8.817 | 5.915 | - | 5.594 | 4.406 | -2.996 | 1.373 | 3.451 | -6.438 | 0.192 | 1.962 | - |
| 90 |  | 8.857 | 5.715 | -1.743 | 5.613 | 4.387 | -2.674 | 1.372 | 3.451 | -6.725 | 0.212 | 1.958 | -6.438 |
| 120 |  | 8.822 | 5.890 | - | 5.544 | 4.456 | - | 1.369 | 3.452 | - | 0.204 | 1.959 | - |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 5.890 |  |  | 4.456 |  |  | 3.452 |  |  | 1.959 |  |  |

Table S12. Parameters obtained from the adsorption of gold in CA size 45 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

| Test ID | Parameters |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | K1 | R^2 |
| 44-1 | 0.5532 | -0.323 | 1.7388 | -0.0027 | 0.7484 |
| 45-2 | -1.3866 | -0.0212 | 0.2499 | -0.0002 | 0.4183 |
| 45-3 | -0.5542 | -0.0719 | 0.5745 | -0.0006 | 0.898 |
| 45-4 | -1.7486 | -0.1471 | 0.1740 | -0.0012 | 0.9478 |

Figure S6. Gold adsorption graphs in AC size 45 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

Table S13. Experimental data of the adsorption of gold in AC size 38 microns for the determination of the kinetic speed constant using the pseudo first order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 38-1 |  |  | 38-2 |  |  | 38-3 |  |  | 38-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) | Ce(Au) | qt | Ln(qe-qt) |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.086 | 4.570 | -0.020 | 5.939 | 4.061 | -0.835 | 2.149 | 3.140 | -1.073 | 1.580 | 1.684 | -1.295 |
| 3 |  | 8.872 | 5.640 | - | 5.66 | 4.340 | -1.864 | 1.8 | 3.280 | -1.598 | 0.749 | 1.850 | -2.229 |
| 5 |  | 8.862 | 5.690 | - | 5.619 | 4.381 | -2.172 | 1.732 | 3.307 | -1.742 | 0.494 | 1.901 | -2.872 |
| 10 |  | 8.933 | 5.335 | -1.537 | 5.596 | 4.404 | -2.397 | 1.714 | 3.314 | -1.784 | 0.373 | 1.925 | -3.430 |
| 15 |  | 9.003 | 4.985 | -0.571 | 5.47 | 4.530 | - | 1.46 | 3.416 | -2.712 | 0.290 | 1.942 | -4.148 |
| 20 |  | 8.995 | 5.025 | -0.644 | 5.437 | 4.563 | - | 1.427 | 3.429 | -2.934 | 0.267 | 1.947 | -4.492 |
| 30 |  | 8.862 | 5.690 | - | 5.634 | 4.366 | -2.048 | 1.493 | 3.403 | -2.531 | 0.258 | 1.948 | -4.667 |
| 40 |  | 8.86 | 5.700 | - | 5.429 | 4.571 | - | 1.472 | 3.411 | -2.642 | 0.241 | 1.952 | -5.116 |
| 50 |  | 8.85 | 5.750 | - | 5.469 | 4.531 | - | 1.355 | 3.458 | -3.713 | 0.245 | 1.951 | -4.991 |
| 60 |  | 8.912 | 5.440 | -2.207 | 5.502 | 4.498 | - | 1.369 | 3.452 | -3.507 | 0.228 | 1.954 | -5.684 |
| 90 |  | 8.911 | 5.445 | -2.254 | 5.446 | 4.554 | - | 1.584 | 3.366 | -2.154 | 0.226 | 1.955 | -5.809 |
| 120 |  | 8.89 | 5.550 | - | 5.505 | 4.495 | - | 1.294 | 3.482 | - | 0.211 | 1.958 | - |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 5.550 |  |  | 4.495 |  |  | 3.482 |  |  | 1.958 |  |  |

Table S14. Parameters obtained from the adsorption of gold in CA size 38 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

| Test ID | Parameters |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | K1 | R^2 |
| 38-1 | -0.0658 | -0.0201 | 0.9363 | -0.00017 | 0.3851 |
| 38-2 | -1.1021 | -0.1505 | 0.3322 | -0.00125 | 0.709 |
| 38-3 | -1.93 | -0.0159 | 0.1451 | -0.00013 | 0.3002 |
| 38-4 | -2.7675 | -0.0441 | 0.0628 | -0.00037 | 0.7318 |

Figure S7. Gold adsorption graphs in AC size 38 microns for the determination of the pseudo first order model (Time vs Ln (qe-qt))

## Kinetic analysis of gold adsorption in AC using the pseudo second order model

Table S15. Experimental data of the adsorption of gold in AC size 106 microns for the determination of the kinetic speed constant using the pseudo second order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 106-1 |  |  | 106-2 |  |  | 106-3 |  |  | 106-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.645 | 1.775 | 0.563 | 8.832 | 1.168 | 0.856 | 7.939 | 0.824 | 1.213 | 6.920 | 0.616 | 1.623 |
| 3 |  | 9.637 | 1.815 | 1.653 | 8.708 | 1.292 | 2.322 | 7.785 | 0.886 | 3.386 | 5.475 | 0.905 | 3.315 |
| 5 |  | 9.672 | 1.640 | 3.049 | 8.575 | 1.425 | 3.509 | 6.861 | 1.256 | 3.982 | 4.302 | 1.140 | 4.388 |
| 10 |  | 9.483 | 2.585 | 3.868 | 8.485 | 1.515 | 6.601 | 5.646 | 1.742 | 5.742 | 2.535 | 1.493 | 6.698 |
| 15 |  | 9.316 | 3.420 | 4.386 | 7.324 | 2.676 | 5.605 | 5.21 | 1.916 | 7.829 | 1.991 | 1.602 | 9.364 |
| 20 |  | 9.195 | 4.025 | 4.969 | 7.09 | 2.910 | 6.873 | 4.328 | 2.269 | 8.815 | 1.450 | 1.710 | 11.696 |
| 30 |  | 9.162 | 4.190 | 7.160 | 6.509 | 3.491 | 8.594 | 3.422 | 2.631 | 11.402 | 0.766 | 1.847 | 16.244 |
| 40 |  | 9.047 | 4.765 | 8.395 | 6.418 | 3.582 | 11.167 | 3.209 | 2.716 | 14.725 | 0.558 | 1.888 | 21.182 |
| 50 |  | 9.029 | 4.855 | 10.299 | 6.239 | 3.761 | 13.294 | 2.93 | 2.828 | 17.680 | 0.373 | 1.925 | 25.969 |
| 60 |  | 8.758 | 6.210 | 9.662 | 6.17 | 3.830 | 15.666 | 2.864 | 2.854 | 21.020 | 0.288 | 1.942 | 30.890 |
| 90 |  | 8.747 | 6.265 | 14.366 | 5.968 | 4.032 | 22.321 | 2.467 | 3.013 | 29.869 | 0.199 | 1.960 | 45.914 |
| 120 |  | 8.698 | 6.510 | 18.433 | 5.903 | 4.097 | 29.290 | 2.345 | 3.062 | 39.190 | 0.172 | 1.966 | 61.050 |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 6.510 |  |  | 4.097 |  |  | 3.062 |  |  | 1.966 |  |  |

Table S16. Parameters obtained from the adsorption of gold in CA size 106 microns for the determination of the pseudo second order model (Time vs t/qt)

| Test ID | Parameters |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | qe^2 (mg/g) | K2 | R^2 |
| 106-1 | 2.0474 | 0.1402 | 7.1327 | 50.8749 | 0.0096 | 0.9760 |
| 106-2 | 2.1641 | 0.2255 | 4.4346 | 19.6656 | 0.0235 | 0.9904 |
| 106-3 | 2.3488 | 0.3078 | 3.2489 | 10.5551 | 0.0403 | 0.9978 |
| 106-4 | 1.6362 | 0.4926 | 2.0300 | 4.1211 | 0.1483 | 0.9998 |

Figure S8. Graphs of gold adsorption in CA size 106 microns for the determination of the pseudo second order model (Time vs t/qt)

Table S17. Experimental data of the adsorption of gold in AC size 75 microns for the determination of the kinetic speed constant using the pseudo second order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 75-1 |  |  | 75-2 |  |  | 75-3 |  |  | 75-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.234 | 3.830 | 0.261 | 7.181 | 2.819 | 0.355 | 5.972 | 1.611 | 0.621 | 2.585 | 1.483 | 0.674 |
| 3 |  | 8.783 | 6.085 | 0.493 | 7.027 | 2.973 | 1.009 | 4.678 | 2.129 | 1.409 | 2.739 | 1.452 | 2.066 |
| 5 |  | 8.582 | 7.090 | 0.705 | 6.574 | 3.426 | 1.459 | 4.523 | 2.191 | 2.282 | 3.014 | 1.397 | 3.579 |
| 10 |  | 8.531 | 7.345 | 1.361 | 6.187 | 3.813 | 2.623 | 3.103 | 2.759 | 3.625 | 1.182 | 1.764 | 5.670 |
| 15 |  | 8.529 | 7.355 | 2.039 | 6.074 | 3.926 | 3.821 | 3.369 | 2.652 | 5.655 | 0.758 | 1.848 | 8.115 |
| 20 |  | 8.501 | 7.495 | 2.668 | 5.96 | 4.040 | 4.950 | 3.005 | 2.798 | 7.148 | 0.426 | 1.915 | 10.445 |
| 30 |  | 8.464 | 7.680 | 3.906 | 5.637 | 4.363 | 6.876 | 2.292 | 3.083 | 9.730 | 0.335 | 1.933 | 15.520 |
| 40 |  | 8.461 | 7.695 | 5.198 | 5.515 | 4.485 | 8.919 | 1.995 | 3.202 | 12.492 | 0.236 | 1.953 | 20.483 |
| 50 |  | 8.414 | 7.930 | 6.305 | 5.512 | 4.488 | 11.141 | 1.623 | 3.351 | 14.922 | 0.221 | 1.956 | 25.565 |
| 60 |  | 8.413 | 7.935 | 7.561 | 5.464 | 4.536 | 13.228 | 1.621 | 3.352 | 17.902 | 0.222 | 1.956 | 30.681 |
| 90 |  | 8.39 | 8.050 | 11.180 | 5.379 | 4.621 | 19.476 | 1.524 | 3.390 | 26.546 | 0.158 | 1.968 | 45.722 |
| 120 |  | 8.363 | 8.185 | 14.661 | 5.315 | 4.685 | 25.614 | 1.483 | 3.407 | 35.224 | 0.155 | 1.969 | 60.945 |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 8.185 |  |  | 4.685 |  |  | 3.407 |  |  | 1.969 |  |  |

Table S18. Parameters obtained from the adsorption of gold in CA size 75 microns for the determination of the pseudo second order model (Time vs t/qt)

| Test ID | Parameters |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | qe^2 (mg/g) | K2 | R^2 |
| 75-1 | 0.1928 | 0.1217 | 8.2169 | 67.5179 | 0.0768 | 0.9997 |
| 75-2 | 0.4896 | 0.2108 | 4.7438 | 22.5040 | 0.0908 | 0.9996 |
| 75-3 | 0.8691 | 0.2863 | 3.4928 | 12.1999 | 0.0943 | 0.9991 |
| 75-4 | 0.5303 | 0.5025 | 1.9900 | 3.9603 | 0.4762 | 0.9999 |

Figure S9. Graphs of gold adsorption in CA size 75 microns for the determination of the pseudo second order model (Time vs t/qt)

Table S19. Experimental data of the adsorption of gold in AC size 53 microns for the determination of the kinetic speed constant using the pseudo second order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 53-1 |  |  | 53-2 |  |  | 53-3 |  |  | 53-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.98 | 0.100 | 10.000 | 6.777 | 3.223 | 0.310 | 3.155 | 2.738 | 0.365 | 1.203 | 1.759 | 0.568 |
| 3 |  | 9.61 | 1.950 | 1.538 | 6.298 | 3.702 | 0.810 | 3.134 | 2.746 | 1.092 | 0.798 | 1.840 | 1.630 |
| 5 |  | 9.407 | 2.965 | 1.686 | 6.282 | 3.718 | 1.345 | 3.046 | 2.782 | 1.798 | 0.563 | 1.887 | 2.649 |
| 10 |  | 9.574 | 2.130 | 4.695 | 6.093 | 3.907 | 2.560 | 2.635 | 2.946 | 3.394 | 0.460 | 1.908 | 5.241 |
| 15 |  | 9.474 | 2.630 | 5.703 | 5.973 | 4.027 | 3.725 | 2.533 | 2.987 | 5.022 | 0.370 | 1.926 | 7.788 |
| 20 |  | 9.43 | 2.850 | 7.018 | 5.896 | 4.104 | 4.873 | 2.221 | 3.112 | 6.428 | 0.354 | 1.929 | 10.367 |
| 30 |  | 9.432 | 2.840 | 10.563 | 5.884 | 4.116 | 7.289 | 2.186 | 3.126 | 9.598 | 0.298 | 1.940 | 15.461 |
| 40 |  | 9.35 | 3.250 | 12.308 | 5.875 | 4.125 | 9.697 | 2.022 | 3.191 | 12.534 | 0.290 | 1.942 | 20.597 |
| 50 |  | 9.321 | 3.395 | 14.728 | 5.872 | 4.128 | 12.112 | 1.889 | 3.244 | 15.411 | 0.288 | 1.942 | 25.741 |
| 60 |  | 9.314 | 3.430 | 17.493 | 5.849 | 4.151 | 14.454 | 1.855 | 3.258 | 18.416 | 0.283 | 1.943 | 30.874 |
| 90 |  | 9.282 | 3.590 | 25.070 | 5.841 | 4.159 | 21.640 | 1.845 | 3.262 | 27.590 | 0.268 | 1.946 | 46.239 |
| 120 |  | 9.258 | 3.710 | 32.345 | 5.766 | 4.234 | 28.342 | 1.837 | 3.265 | 36.751 | 0.244 | 1.951 | 61.501 |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 3.710 |  |  | 4.234 |  |  | 3.265 |  |  | 1.951 |  |  |

Table S20. Parameters obtained from the adsorption of gold in CA size 53 microns for the determination of the pseudo second order model (Time vs t/qt)

| Test ID | Parameters |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | qe^2 (mg/g) | K2 | R^2 |
| 53-1 | 1.5994 | 0.2608 | 3.8344 | 14.7023 | 0.0425 | 0.9956 |
| 53-2 | 0.1746 | 0.2366 | 4.2265 | 17.8637 | 0.3206 | 0.9999 |
| 53-3 | 0.2939 | 0.3038 | 3.2916 | 10.8349 | 0.3140 | 0.9999 |
| 53-4 | 0.1045 | 0.5122 | 1.9524 | 3.8117 | 2.5105 | 1.0000 |

Figure S10. Graphs of gold adsorption in CA size 53 microns for the determination of the pseudo second order model (Time vs t/qt)

Table S21. Experimental data of the adsorption of gold in AC size 45 microns for the determination of the kinetic speed constant using the pseudo second order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 44-1 |  |  | 45-2 |  |  | 45-3 |  |  | 45-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.381 | 3.095 | 0.323 | 6.318 | 3.682 | 0.272 | 3.034 | 2.786 | 0.359 | 2.063 | 1.587 | 0.630 |
| 3 |  | 8.899 | 5.505 | 0.545 | 5.796 | 4.204 | 0.714 | 2.8 | 2.880 | 1.042 | 0.813 | 1.837 | 1.633 |
| 5 |  | 8.857 | 5.715 | 0.875 | 5.741 | 4.259 | 1.174 | 2.277 | 3.089 | 1.619 | 0.523 | 1.895 | 2.638 |
| 10 |  | 8.843 | 5.785 | 1.729 | 5.817 | 4.183 | 2.391 | 1.957 | 3.217 | 3.108 | 0.318 | 1.936 | 5.164 |
| 15 |  | 8.8 | 6.000 | 2.500 | 5.681 | 4.319 | 3.473 | 1.762 | 3.295 | 4.552 | 0.260 | 1.948 | 7.700 |
| 20 |  | 8.795 | 6.025 | 3.320 | 5.65 | 4.350 | 4.598 | 1.637 | 3.345 | 5.979 | 0.248 | 1.950 | 10.254 |
| 30 |  | 8.749 | 6.255 | 4.796 | 5.575 | 4.425 | 6.780 | 1.526 | 3.390 | 8.851 | 0.217 | 1.957 | 15.333 |
| 40 |  | 8.9 | 5.500 | 7.273 | 5.771 | 4.229 | 9.459 | 1.478 | 3.409 | 11.734 | 0.207 | 1.959 | 20.423 |
| 50 |  | 8.895 | 5.525 | 9.050 | 5.611 | 4.389 | 11.392 | 1.518 | 3.393 | 14.737 | 0.196 | 1.961 | 25.500 |
| 60 |  | 8.817 | 5.915 | 10.144 | 5.594 | 4.406 | 13.618 | 1.373 | 3.451 | 17.387 | 0.192 | 1.962 | 30.587 |
| 90 |  | 8.857 | 5.715 | 15.748 | 5.613 | 4.387 | 20.515 | 1.372 | 3.451 | 26.078 | 0.212 | 1.958 | 45.975 |
| 120 |  | 8.822 | 5.890 | 20.374 | 5.544 | 4.456 | 26.930 | 1.369 | 3.452 | 34.758 | 0.204 | 1.959 | 61.249 |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 5.890 |  |  | 4.456 |  |  | 3.452 |  |  | 1.959 |  |  |

Table S22. Parameters obtained from the adsorption of gold in CA size 45 microns for the determination of the pseudo second order model (Time vs t/qt)

| Test ID | Parameters |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | qe^2 (mg/g) | K2 | R^2 |
| 44-1 | 0.0164 | 0.1719 | 5.8173 | 33.8414 | 1.8018 | 0.9984 |
| 45-2 | 0.1135 | 0.2251 | 4.4425 | 19.7355 | 0.4464 | 0.9997 |
| 45-3 | 0.1906 | 0.2881 | 3.4710 | 12.0480 | 0.4355 | 1.0000 |
| 45-4 | 0.0701 | 0.5096 | 1.9623 | 3.8507 | 3.7046 | 1.0000 |

Figure S11. Graphs of gold adsorption in CA size 106 microns for the determination of the pseudo second order model (Time vs t/qt)

Table S23. Experimental data of the adsorption of gold in AC size 38 microns for the determination of the kinetic speed constant using the pseudo second order model

|  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  | Test ID |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 38-1 |  |  | 38-2 |  |  | 38-3 |  |  | 38-4 |  |  |
|  |  | Mass |  |  | Mass |  |  | Mass |  |  | Mass |  |  |
|  |  | gr |  |  | gr |  |  | gr |  |  | gr |  |  |
|  |  | 0.01 |  |  | 0.05 |  |  | 0.125 |  |  | 0.25 |  |  |
| Time | Ci | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt | Ce(Au) | qt | t/qt |
| min | mg/L | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  | mg/L | mg/gr |  |
| 1 | 10 | 9.086 | 4.570 | 0.219 | 5.939 | 4.061 | 0.246 | 2.149 | 3.140 | 0.318 | 1.580 | 1.684 | 0.594 |
| 3 |  | 8.872 | 5.640 | 0.532 | 5.66 | 4.340 | 0.691 | 1.8 | 3.280 | 0.915 | 0.749 | 1.850 | 1.621 |
| 5 |  | 8.862 | 5.690 | 0.879 | 5.619 | 4.381 | 1.141 | 1.732 | 3.307 | 1.512 | 0.494 | 1.901 | 2.630 |
| 10 |  | 8.933 | 5.335 | 1.874 | 5.596 | 4.404 | 2.271 | 1.714 | 3.314 | 3.017 | 0.373 | 1.925 | 5.194 |
| 15 |  | 9.003 | 4.985 | 3.009 | 5.47 | 4.530 | 3.311 | 1.46 | 3.416 | 4.391 | 0.290 | 1.942 | 7.724 |
| 20 |  | 8.995 | 5.025 | 3.980 | 5.437 | 4.563 | 4.383 | 1.427 | 3.429 | 5.832 | 0.267 | 1.947 | 10.274 |
| 30 |  | 8.862 | 5.690 | 5.272 | 5.634 | 4.366 | 6.871 | 1.493 | 3.403 | 8.816 | 0.258 | 1.948 | 15.397 |
| 40 |  | 8.86 | 5.700 | 7.018 | 5.429 | 4.571 | 8.751 | 1.472 | 3.411 | 11.726 | 0.241 | 1.952 | 20.494 |
| 50 |  | 8.85 | 5.750 | 8.696 | 5.469 | 4.531 | 11.035 | 1.355 | 3.458 | 14.459 | 0.245 | 1.951 | 25.628 |
| 60 |  | 8.912 | 5.440 | 11.029 | 5.502 | 4.498 | 13.339 | 1.369 | 3.452 | 17.379 | 0.228 | 1.954 | 30.700 |
| 90 |  | 8.911 | 5.445 | 16.529 | 5.446 | 4.554 | 19.763 | 1.584 | 3.366 | 26.735 | 0.226 | 1.955 | 46.041 |
| 120 |  | 8.89 | 5.550 | 21.622 | 5.505 | 4.495 | 26.696 | 1.294 | 3.482 | 34.459 | 0.211 | 1.958 | 61.293 |
|  |  | qe |  |  | qe |  |  | qe |  |  | qe |  |  |
|  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  | mg/gr |  |  |
|  |  | 5.550 |  |  | 4.495 |  |  | 3.482 |  |  | 1.958 |  |  |

Table S24. Parameters obtained from the adsorption of gold in CA size 38 microns for the determination of the pseudo second order model (Time vs t/qt)

| Test ID | Parameters |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | b | m | qe (mg/g) | qe^2 (mg/g) | K2 | R^2 |
| 38-1 | 0.0491 | 0.1803 | 5.5463 | 30.7616 | 0.6621 | 0.9990 |
| 38-2 | 0.0226 | 0.2212 | 4.5208 | 20.4376 | 2.1650 | 0.9998 |
| 38-3 | 0.0792 | 0.2897 | 3.4518 | 11.9152 | 1.0597 | 0.9996 |
| 38-4 | 0.0847 | 0.5103 | 1.9596 | 3.8402 | 3.0745 | 1.0000 |

Figure S12. Graphs of gold adsorption in CA size 106 microns for the determination of the pseudo second order model (Time vs t/qt)