Table S1. Chemical components for BG 11 media.

| Manufacturer | Component | Concentration(mg/L) |
| --- | --- | --- |
|  |  | in BG 11 |
| Sigma (USA) | K2HPO4 | 40 |
|  | MgSO4·7H2O | 75 |
|  | CaCl2·2H2O | 36 |
|  | Ferric Ammonium Citrate | 6 |
|  | Na2EDTA·2H2O | 1 |
|  | ZnSO4·7H2O | 0.22 |
| Baker (USA) | Na2CO3 | 20 |
|  | H3BO3 | 2.86 |
|  | MnCl2·4H2O | 1.81 |
| Fisher (USA) | NaNO3 | 1500 |
|  | Citric acid·H2O | 6 |
| J.T. Baker (USA) | Na2MoO4·2H2O | 0.39 |
| Mallinckroft (USA) | Co(NO3)2·6H2O | 0.0494 |
| MCIB (USA) | CuSO4·5H2O | 0.079 |

Table S2. Size information of the utilized CFs for removal of M. aeruginosa.

| Sorbents | Inner diameter of used needles (mm) | aAverage diameter of CFs (mm) | bVolume of sorbent (mm3) | c Length of sorbents (mm) | d Surface area (mm2) |
| --- | --- | --- | --- | --- | --- |
| CF1 | 0.66 | 0.29 | 1 | 15.47 | 14.07 |
| CF2 | 0.47 | 0.19 | 1 | 34.67 | 20.93 |
| CF3 | 0.31 | 0.10 | 1 | 132.88 | 40.88 |
| CF4 | 0.29 | 0.04 | 1 | 794.42 | 99.92 |

a Average diameters of each CFs were calculated from recorded diameters at 10 parts of CFs through microscopic observation. b Assumed unit volume. c Derived by applied values of assumed unit volume and diameters of CFs to equation for volume of cylinder (V=Lπr2). d Derived by applied values of diameters and lengths of CFs to equation for surface area of cylinder (S=2πrL).

Figure S1. The FT-IR spectrum of (A) raw chitosan powder and (B) manufactured chitosan fiber.

| (A) | (B) |
| --- | --- |

Figure S2. The color change of applied chitosan fiber (A) before and (B) after treatment of M. aeruginosa cells.