Supplementary Materials:

RuCu Nanorod Arrays Synergistically Promote Efficient Water-Splitting

Figure S1. XRD spectrum of NF

Figure S2.XRD spectra of CuCl-2h, CuCl-8h, and CuCl-12h

Figure S3.XRD spectra of RuCuCl/NF-1,RuCuCl/NF-2,and RuCuCl/NF-3

Figure S4. (a-b) SEM images of CuCl-2h. (c-d) SEM images of CuCl-8h. (e-f) CuCl-12h.

Figure S5. (a-b)SEM CuCl samples were washed by immersion in deionized water for 5 min three times after completion of the reaction and stored in vacuum drying.

Figure S6. (a-d)SEM CuCl samples were washed after completion of the reaction by immersion in deionized water with dissolved oxygen exhausted by nitrogen for 5 min three times, vacuum dried and stored for backup;

Figure S7. (a-d)SEM CuCl samples were cleaned after completion of the reaction by immersion in deionized water drained of dissolved oxygen by nitrogen for 5 min three times, after which they were placed in deionized drained of oxygen and sealed for storage;

Figure S8. (a-d)SEM CuCl samples were removed from the NF after completion of the reaction and washed by immersion in deionized water with dissolved oxygen exhausted by nitrogen for 5 min three times, after which it was placed in deionized with oxygen exhausted and stored open.

Figure S9. SEM images of Ru/NF and eds mapping profiles of Ni, Ru, and O elements.

Figure S10. (a)SEM image of RuCuCl/NF-2.  (b) TEM image of RuCuCl/NF-2

Figure S11. XRD spectra of RuCuCl/NF-2-N2

Figure S12. (a-b)SEM  RuCuCl/NF-2-N2

Figure S13. Evaluation and comparison of OER performance of NF, CuCl/NF, Ru/NF, and RuCuCl/NF-2 electrodes in neutral environment: (a) Polarization curves. (b)Tafel plots. (c)Overpotential at current density of 10 mA/cm2, and tafel slope comparison. (d) Nyquist plots.

Table S1. Comparison of the HER performance of RuCuCl/NF-2 catalysts under neutral conditions with recently reported electrolyzed water catalysts.

| Catalyst | Electrolyte | Tafel plots(mV/dec) | η10(mV) | Reference |
| --- | --- | --- | --- | --- |
| RuCuCl/NF-2 | 1.0 M PBS | 68.3 | 61.6 | This work |
| NiCo2Px | 1.0 M PBS | 63.3 | 63 | 48 |
| Cu0.08Co0.92P NAs/CP | 1.0 M PBS | 83.5 | 81 | 49 |
| Mn-Co-P/Ti | 1.0 M PBS | 82 | 86 | 50 |
| Karst NF | 1.0 M PBS | 99 | 110 | 51 |
| Hollow Ni(S0.5Se0.5)2 | 1.0 M PBS | 81 | 124 | 52 |
| SiO2/PPy NTs– CFs | 1.0 M PBS | 100.2 | 192 | 53 |
| MoP700 | 1.0 M PBS | 79 | 196 | 54 |

Table S2. comparison of the HER performance of RuCuCl/NF-2 with recently reported Ru-based catalysts.

| Catalyst | Electrolyte | Tafel plots(mV/dec) | η10(mV) | Reference |
| --- | --- | --- | --- | --- |
| RuCuCl/NF-2 | 1.0M KOH | 21.9 | 25 | This work |
| P-Ru-CoNi-LDH | 1.0M KOH | 69 | 29 | 55 |
| Ru0.10@2H-MoS2 | 1.0M KOH | 64.9 | 51 | 56 |
| Ru/Co4N-CoF2 | 1.0M KOH | 144.1 | 53 | 57 |
| Ru/BP 2000 | 1.0M KOH |  | 54.2 | 58 |
| RuSx | 1.0M KOH |  | 58 | 59 |
| Sr2RuO4 | 1.0M KOH | 51 | 61 | 60 |
| RuPx@NPC | 1.0M KOH | 46 | 74 | 61 |
| Ru@C3N4/C | 1.0M KOH | Near to Pt | 79 | 62 |
| RuO2/Co3O4 | 1.0M KOH | 91 | 89 | 63 |
| S-RuP@NPSC-900 | 1.0M KOH | 90.23 | 92 | 64 |
| Ru-NPs/SAs@N-TC | 1.0M KOH | 58 | 97 | 65 |

Table S3. Comparison of RuCuCl/NF-2 with recently reported Ru-doped catalysts for overall water splitting.

| Catalyst | The voltage at 10 mA cm-2(V) | Reference |
| --- | --- | --- |
| RuCuCl/NF-2 | 1.489 | This work |
| RuSAs-MoO3- x/NF | 1.487 | 66 |
| SF-Ru | 1.51 | 67 |
| Ru@MoO(S)3 | 1.526 | 68 |
| Ru–NiSe2/NF | 1.537 | 69 |
| Ru/NiFe(OH)x/NiFe-MOF | 1.54 | 70 |
| RuP/CoNiP4O12 | 1.56 | 71 |
| Ru@NiCo-MOF-4 | 1.57 | 72 |
| Ru-CoP/NCs | 1.58 | 73 |
| Ru-H2O/CC-350 | 1.67 | 74 |