Synthesis, Structure and Properties of Coordination Polymers Based on 1,4-Bis((2-methyl-1H-imidazol-1-yl)methyl)benzene and Different Carboxylate Ligands

Kang Liu, Yaowen Zhang, Liming Deng, Shaoshao Jiao and Lei Wang *

Table S1. Selected bond distances (Å) and angles (°) for 1

| Zn1-O3 | 1.9498(13) | Zn1-O31 | 1.9498(13) |
| --- | --- | --- | --- |
| Zn1-N1 | 2.0173(15) | Zn1-N11 | 2.0173(15) |
| O3-Zn1-O31 | 99.53(9) | O31-Zn1-N11 | 121.52(6) |
| O3-Zn1-N11 | 101.02(6) | O3-Zn1-N1 | 121.52(6) |
| O31-Zn1-N1 | 101.02(6) | N11-Zn1-N1 | 112.89(9) |

Symmetry transformations used to generate equivalent atoms: 11-X,+Y,1/2-Z.

Table S2. Selected bond distances (Å) and angles (°) for 2

| Cu1-N2 | 1.930(2) | Cu1-N1 | 1.897(2) |
| --- | --- | --- | --- |
| Cu1-O3 | 2.0214(18) | Cu1-O21 | 2.651(22) |
| Cu1-O1 | 1.9940(18) |  |  |
| N1-Cu1-N2 | 176.12(8) | N1-Cu1-O1 | 80.80(8) |
| N1-Cu1-O3 | 80.35(9) | N2-Cu1-O1 | 102.30(8) |
| N2-Cu1-O3 | 96.67(8) | O1-Cu1-O3 | 160.88(8) |
| O21-Cu1-N2 | 88.33(57) | O21-Cu1-N1 | 89.38(9) |
| O21-Cu1-O1 | 89.17(8) | O21-Cu1-O3 | 93.77(6) |

Symmetry transformations used to generate equivalent atoms: 11-X,1-Y,2-Z.

Table S3. Selected bond distances (Å) and angles (°) for 3

| Cu1-N2 | 2.027(2) | Cu1-N3 | 1.968(2) |
| --- | --- | --- | --- |
| Cu1-O2 | 1.9651(19) | Cu1-O31 | 2.632(2) |
| Cu1-O3 | 2.213(2) | Cu1-O4 | 2.0060(19) |
| O3-Cu13 | 2.632(2) |  |  |
| N2-Cu1-O3 | 90.24(9) | O2-Cu1-O31 | 121.80(8) |
| N2-Cu1-O31 | 88.47(8) | O2-Cu1-O3 | 90.06(8) |
| N3-Cu1-N2 | 171.39(10) | O2-Cu1-O4 | 174.30(8) |
| N3-Cu1-O3 | 95.60(9) | O3-Cu1-O31 | 147.50(10) |
| N3-Cu1-O31 | 89.98(8) | O4-Cu1-N2 | 93.29(9) |
| N3-Cu1-O4 | 92.75(9) | O4-Cu1-O3 | 92.74(8) |
| O2-Cu1-N2 | 81.73(9) | O4-Cu1-O31 | 54.95(7) |
| O2-Cu1-N3 | 91.91(9) |  |  |

Symmetry transformations used to generate equivalent atoms: 11+X,+Y,+Z; 2-X,-Y,-Z; 3-1+X,+Y,+Z.

Table S4. Parameters of hydrogen bonds for compound 1

| D-H···A | d(D-H)/Å | d(H-A)/Å | d(D-A)/Å | ∠DHA/(o) |
| --- | --- | --- | --- | --- |
| O1-H1A···O2 | 0.84(1) | 2.04(4) | 2.84(2) | 160.9(35) |

Table S5. Parameters of hydrogen bonds for compound 2

| D-H···A | d(D-H)/Å | d(H-A)/Å | d(D-A)/Å | ∠DHA/(o) |
| --- | --- | --- | --- | --- |
| C2-H2···O2 | 0.93 | 2.40(2) | 3.23(9) | 148.3(20) |
| C15-H15···O1 | 0.93 | 2.64(2) | 3.53(3) | 160.7(15) |
| C12-H12A···O4 | 0.97 | 2.48(2) | 3.34(3) | 147.9(14) |

Table S6. Parameters of hydrogen bonds for compound 3

| D-H···A | d(D-H)/Å | d(H-A)/Å | d(D-A)/Å | ∠DHA/(o) |
| --- | --- | --- | --- | --- |
| O5-H5A···O4 | 0.84(1) | 1.97(1) | 2.78(3) | 165.9(10) |
| O5-H5B···O6 | 0.84(3) | 1.91(3) | 2.74(3) | 168.2(28) |
| O6-H6D···O1 | 0.84(1) | 1.92(1) | 2.74(3) | 165.1(13) |
| O6-H6E···O5 | 0.84(2) | 1.90(2) | 2.73(3) | 174.3(25) |

Figure S1. The PXRD data of 1.

Figure S2. The PXRD data of 2.

Figure S3. The PXRD data of 3.