Electronic supplementary information (ESI)

Ultrasound- and Thermo-Responsive Ionic Liquid Polymer

Kohei Itsuki, Yuuki Kawata, Komol Kanta Sharker and Shin-ichi Yusa*

Department of Applied Chemistry, Graduate School of Engineering, University of Hyogo, 2167 Shosha, Himeji, Hyogo 671-2280, Japan;

flowing.yumeniji.quiz@gmail.com (I.K.); yuki.chibikitty.1020@gmail.com (K.Y.); sharkerkomol@diu.edu.bd (K.K.S.); yusa@eng.u-hyogo.ac.jp (S.Y.)

* Correspondence: yusa@eng.u-hyogo.ac.jp; Tel.: +81-79-267-4954

Figure S1. Synthesis route of PAMPSP4448 and PAMPSP4444.

Figure S2. 1H NMR spectrum for PAMPSP4444 in CDCl3.

Figure S3. Percent transmittance (%T) at 800 nm for the aqueous PAMPSP4448 solutions at Cp = 5.0 g/L as a function of the sonication time at 50 C.

Figure S4. Percent transmittance (%T) at 800 nm for the aqueous PAMPSP4448 solutions as a function of temperature at Cp = 0.5 (a) and 1.0 g/L (b). The temperature was increased from 0 to 50 C (heating; —) and decreased from 50 to 0 C (cooling, ---) at 1°C/min with stirring. The solutions were sonicated for 10 min at 50 C and then cooled.

Figure S5. Percent transmittance (%T) at 800 nm for (a) PAMPSP4444 in water and (b) in 0.1 M aqueous NaCl as a function of temperature at Cp = 5.0 g/L. The temperature was increased from 0 to 50 C (—) and decreased from 50 to 0 C (---) at 1°C/min with stirring.

Figure S6. Hydrodynamic radius (Rh) distributions for the transparent aqueous PAMPSP4448 solutions at 25 °C. The solution was sonicated at 50 °C. After sonication, the solution was cooled to 5 °C and then heated to 25 °C. Rh distributions were measured for the transparent aqueous PAMPSP4448 solutions at 25 °C after (a) one, (b) two, and (c) three sonication cycles.