Supplementary Material

| Figure SF1: Triplicate 1 of the quality evaluation. | Figure SF2: Triplicate 2 of the quality evaluation. | Figure SF3: Triplicate 3 of the quality evaluation. |
| --- | --- | --- |

Table S1: Images of the photo-resin formulations after lamination, UV-exposure, and hard bake.

|  | ED0 |  |  | ED10 |  |  | ED20 |  |  | ED30 |  |  | ED40 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | T1 | T2 | T3 | T1 | T2 | T3 | T1 | T2 | T3 | T1 | T2 | T3 | T1 | T2 | T3 |
| C0 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C30 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C50 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C100 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

ED = Epoxidation degree (% mol∙(molpolymer)-1)

C = Amount of photocatalyst (% mol∙(molpolymer)-1)

T = triplicate experiment 1, 2 and 3

Table S2: Images of the photo-resin formulations after development.

|  | ED0 |  |  | ED10 |  |  | ED20 |  |  | ED30 |  |  | ED40 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | T1 | T2 | T3 | T1 | T2 | T3 | T1 | T2 | T3 | T1 | T2 | T3 | T1 | T2 | T3 |
| C0 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C30 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C50 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| C100 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

ED = Epoxidation degree (% mol∙(molpolymer)-1)

C = Amount of photocatalyst (% mol∙(molpolymer)-1)

T = triplicate experiment 1, 2 and 3

Table S3: Quality control for the evaluation of the photo-resin formulations.

| Samples | ED0 (t1) | ED0 (t2) | ED0(t3) | ED10(t1) | ED10(t2) | ED10(t3) | ED20(t1) | ED20(t2) | ED20(t3) | ED30(t1) | ED30(t2) | ED30(t3) | ED40(t1) | ED40(t2) | ED40(t3) | C average |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | - |
| C0 t-average | 0.0 |  |  | 0.0 |  |  | 0.0 |  |  | 0.0 |  |  | 0.0 |  |  | 0.0 |
| C3 | 1.0 | 1.0 | 1.0 | 0.0 | 0.5 | 0.5 | 0.0 | 0.5 | 0.5 | 0.5 | 0.5 | 1.0 | 0.5 | 0.5 | 0.5 | - |
| C3 t-average | 1.0 |  |  | 0.3 |  |  | 0.3 |  |  | 0.7 |  |  | 0.5 |  |  | 0.6 |
| C5 | 0.0 | 0.0 | 0.0 | 0.5 | 1.0 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 1.0 | 0.5 | 0.5 | 1.0 | 1.0 | - |
| C5 t-average | 0.0 |  |  | 0.7 |  |  | 0.5 |  |  | 0.7 |  |  | 0.8 |  |  | 0.5 |
| C10 | 0.5 | 0.0 | 0.0 | 0.5 | 0.5 | 0.5 | 0.5 | 1.0 | 0.5 | 0.5 | 1.0 | 1.0 | 0.5 | 1.0 | 1.0 | - |
| C10 t-average | 0.2 |  |  | 0.5 |  |  | 0.7 |  |  | 0.8 |  |  | 0.8 |  |  | 0.6 |
| C30 | 0.0 | 0.0 | 0.0 | 0.5 | 1.0 | 1.0 | 1.0 | 0.5 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | - |
| C30 t-average | 0.0 |  |  | 0.8 |  |  | 0.8 |  |  | 1.0 |  |  | 1.0 |  |  | 0.7 |
| C50 | 0.0 | 0.0 | 0.0 | 1.0 | 0.5 | 0.5 | 1.0 | 0.5 | 1.0 | 0.5 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | - |
| C50 t-average | 0.0 |  |  | 0.7 |  |  | 0.8 |  |  | 0.8 |  |  | 1.0 |  |  | 0.7 |
| C100 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.5 | 0.5 | 0.5 | 0.5 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | - |
| C100 t-average | 0.0 |  |  | 0.0 |  |  | 0.5 |  |  | 0.8 |  |  | 1.0 |  |  | 0.5 |
| ED average |  | ED0 | 0.2 |  | ED10 | 0.4 |  | ED20 | 0.5 |  | ED30 | 0.7 |  | ED40 | 0.7 | - |

*t-average: the average values for the triplicate measurements

* Average: the average of the referred feature

Table S4: Patterned structures generated thorough UV Lithography after hard bake.

| Triplicate | P1ED0C3 | P1ED40C30 | P2ED0C3 | P2ED40C30 | P3ED0C3 | P3ED40C30 |
| --- | --- | --- | --- | --- | --- | --- |
| T1 |  |  |  |  |  |  |
| T2 |  |  |  |  |  |  |
| T3 |  |  |  |  |  |  |

Table S5: Patterned structures generated thorough Deep-UV Lithography after hard bake.

| Triplicate | P1ED0C3 | P1ED40C30 | P2ED0C3 | P2ED40C30 | P3ED0C3 | P3ED40C30 |
| --- | --- | --- | --- | --- | --- | --- |
| T1 |  |  |  |  |  |  |
| T2 |  |  |  |  |  |  |
| T3 |  |  |  |  |  |  |

Table S6: Patterned structures generated thorough UV Lithography after development.

| Triplicate | P1ED0C3 | P1ED40C30 | P2ED0C3 | P2ED40C30 | P3ED0C3 | P3ED40C30 |
| --- | --- | --- | --- | --- | --- | --- |
| T1 |  |  |  |  |  |  |
| T2 |  |  |  |  |  |  |
| T3 |  |  |  |  |  |  |

Table S7: Patterned structures generated thorough Deep-UV Lithography after development.

| Triplicate | P1ED0C3 | P1ED40C30 | P2ED0C3 | P2ED40C30 | P3ED0C3 | P3ED40C30 |
| --- | --- | --- | --- | --- | --- | --- |
| T1 |  |  |  |  |  |  |
| T2 |  |  |  |  |  |  |
| T3 |  |  |  |  |  |  |

Figure SF4: SEM Images of P1ED40C30 formulation. Patterned structures generated thorough UV Lithography after development.

Figure SF5: SEM Images of P2ED40C30 formulation. Patterned structures generated thorough UV Lithography after development.

Figure SF6: SEM Images of P3ED40C30 formulation. Patterned structures generated thorough UV Lithography after development.