Multi-material 3D printed shape memory polymer with tunable melting and transition temperature activated by heat and light

Ela Sachyani Keneth1, Rama Lieberman1, Matthew Rednor1, Giulia Scalet2, Ferdinando Auricchio2 and Shlomo Magdassi1*.

1. Casali Center of Applied Chemistry, Institute of Chemistry and the Center for Nanoscience and Nanotechnology, The Hebrew University of Jerusalem, 91904 Jerusalem, Israel

2.  Department of Civil Engineering and Architecture, University of Pavia, Pavia, Italy

* Corresponding author.

Email addresses: magdassi@mail.huji.ac.il (S. Magdassi)

Figure S1: Young's modulus analysis for pure PCLMA polymer below transition temperature.

Figure S2: Young's modulus analysis for 10 wt% NCVL: PCLMA polymer composition below transition temperature.

Supporting information

Figure S3: Young's modulus analysis for 20 wt% NCVL: PCLMA polymer composition below transition temperature.

Figure S4: Young's modulus analysis for 30 wt% NCVL: PCLMA polymer composition below transition temperature.

Figure S5: Young's modulus analysis for 40 wt% NCVL: PCLMA polymer composition below transition temperature.

Figure S6: Young's modulus analysis for 50 wt% NCVL: PCLMA polymer composition below transition temperature.

Figure S7: Young's modulus analysis for pure PCLMA polymer above transition temperature.

Figure S8: Young's modulus analysis for 10 wt% NCVL: PCLMA polymer composition above transition temperature.

Figure S9: Young's modulus analysis for 20 wt% NCVL:PCLMA polymer composition above transition temperature.

Figure S10: Young's modulus analysis for 30 wt% NCVL:PCLMA polymer composition above transition temperature.

Figure S11: Young's modulus analysis for 40 wt% NCVL:PCLMA polymer composition above transition temperature

Figure S12: Young's modulus analysis for 50 wt% NCVL:PCLMA polymer composition above transition temperature

Figure S13: Experimental setup for the cube's light activation.

Table 1: Constitutive model parameters adopted for modeling the pure ink (i.e., pure PCLMA) in the finite element analysis.

| Parameter | Symbol | Value | Unit |
| --- | --- | --- | --- |
| Young’s modulus of the glassy phase | Eg | 185 | MPa |
| Young’s modulus of the rubbery phase | Er | 0.25 | MPa |
| Poisson’s ratio of the glassy phase | νg | 0.29 | - |
| Poisson’s ratio of the rubbery phase | νr | 0.49 | - |
| Transformation temperature | θt | 56.5 | °C |
| Half-width of the temperature range | Δθ | 3 | °C |
| Transformation coefficient | w | 3.8 | 1/°C |
| Plastic hardening coefficient | h | 10 | MPa |
| Stress limit for plastic yielding of the glassy phase | Rpg | 15 | MPa |
| Imperfect shape-fixing coefficient | c | 1 | - |
| Incomplete shape-recovery coefficient | cp | 0 | - |

Table 2: Constitutive model parameters adopted for modelling the mixed ink (i.e., ink composed of 40 wt% NVCL) in the finite element analysis.

| Parameter | Symbol | Value | Unit |
| --- | --- | --- | --- |
| Young’s modulus of the glassy phase | Eg | 245 | MPa |
| Young’s modulus of the rubbery phase | Er | 17 | MPa |
| Poisson’s ratio of the glassy phase | νg | 0.29 | - |
| Poisson’s ratio of the rubbery phase | νr | 0.49 | - |
| Transformation temperature | θt | 51 | °C |
| Half-width of the temperature range | Δθ | 3 | °C |
| Transformation coefficient | w | 3.8 | 1/°C |
| Plastic hardening coefficient | h | 10 | MPa |
| Stress limit for plastic yielding of the glassy phase | Rpg | 10 | MPa |
| Imperfect shape-fixing coefficient | c | 1 | - |
| Incomplete shape-recovery coefficient | cp | 0 | - |

Movie S1: A 3D printed two-lid-box with two transition temperatures activated by direct heating.

Movie S2: A 3D printed carbon nanotubes (CNTs) coated two-lid-box with two transition temperatures activated by light.