Supplementary Materials

Construction of NIR Light Controlled Micelles with Photothermal Conversion Property: Poly (poly(ethylene glycol) methyl ether methacrylate) (PPEGMA) as Hydrophilic Block and Ketocyanine Dye as NIR Photothermal Conversion Agent

Lan Yao, Haihui Li, Kai Tu, Lifen Zhang*, Zhenping Cheng*, Xiulin Zhu

Suzhou Key Laboratory of Macromolecular Design and Precision Synthesis, State and Local Joint Engineering Laboratory for Novel Functional Polymeric Materials, College of Chemistry, Chemical Engineering and Materials Science, Soochow University, Suzhou 215123 (China); 20174209022@stu.suda.edu.cn (L.Y.); harvey1119@163.com (H.L.); sudatukai@163.com (K.T.); xlzhu@suda.edu.cn (X.Z.)

*	Correspondence: zhanglifen@suda.edu.cn (L.Z.); chengzhenping@suda.edu.cn (Z.C.)

Figure S1 1H NMR spectra of (a) PT-1 in CDCl3; (b) PT-2 in DMSO-d6; (c) NIR 800 in DMSO-d6.

Figure S1 1H NMR spectra of (a) PT-1 in CDCl3; (b) PT-2 in DMSO-d6; (c) NIR 800 in DMSO-d6.

Figure S3 GPC traces of PBnMA-b-P(BAPMA-co-PEGMA) before and after chain extension using PBnMA as the macroinitiator. Polymerization conditions: R = [BnMA]0/[CPDN]0/[AIBN]0, T = 80 oC, Vtoluene = 1.0 mL, t = 20 h. Chain extension conditions: R = [BAPMA]0:[PEGMA]0:[Macro-CTA]0:[AIBN]0, T = 80 oC, Vtoluene = 1.0 mL, t = 24 h. (a) Macro-CTA is P1; (b) Macro-CTA is P2; (c) Macro-CTA is P3.

Figure S2 1H NMR spectrum of BAPMA in CDCl3.

Figure S4 1H NMR spectra of P7-NH2 before (a) and after (b) with NIR 800 in DMSO-d6.