Supplementary Information

Influence of Lyophilization and Cryoprotection on the Stability and Morphology of Drug-Loaded Poly(Ethylene Glycol-b-ε-caprolactone) Micelles

Table S1. Concentration and volume of stock solutions combined to prepare copolymer solutions in ultrapure water for the determination of the CAC of PEG-b-PCL block copolymer micelles.

| Conc. of copolymer in PBS (mg/L)a | Volume of pyrene stock solution (µL)b | Conc. of copolymer stock solution (mg/L)c | Volume of copolymer stock solution (µL) | Volume of ultrapure water added (µL) |
| --- | --- | --- | --- | --- |
| 500 | 20 | 2000 | 500 | 2000 |
| 100 | 20 | 2000 | 100 | 2000 |
| 50.0 | 20 | 1000 | 100 | 2000 |
| 10.0 | 20 | 1000 | 20 | 2000 |
| 5.00 | 20 | 1000 | 10 | 2000 |
| 2.50 | 20 | 100 | 50 | 2000 |
| 1.00 | 20 | 100 | 20 | 2000 |
| 0.75 | 20 | 100 | 15 | 2000 |
| 0.50 | 20 | 100 | 10 | 2000 |
| 0.25 | 20 | 10 | 50 | 2000 |

a Copolymer solutions were prepared in high purity water via the solvent evaporation approach with a constant pyrene concentration of 6 × 10-7 M. b A 6 × 10-5 M pyrene stock solution in acetone was used to prepare all solutions. c All stock solutions were prepared in acetone.

Figure S1. Pyrene (6 x 10-7 M) fluorescent emission spectra (λex = 334 nm) for (a) PEG2PCL0.4, (b) PEG2PCL1.1, (c) PEG2PCL1.8 and (d) PEG2PCL4.0 copolymers at various copolymer concentrations.

Figure S2. Pyrene (6 x 10-7 M) fluorescent emission spectra (λex = 334 nm) for (a) PEG5PCL0.6, (b) PEG5PCL1.3, (c) PEG5PCL2.4, (d) PEG5PCL4.2 and (e) PEG5PCL9.5 copolymers at various copolymer concentrations.

Figure S3. Pyrene (6 x 10-7 M) fluorescent emission spectra (λex = 334 nm) for (a) PEG10PCL3.2, (b) PEG10PCL7.9, (c) PEG10PCL10.7 and (d) PEG10PCL14.9 copolymers at various copolymer concentrations.

Figure S4. Illustration of preparation, lyophilization and characterisation of PEGX-b-PCLY micelles.

Table S2. Polydispersity index (PDI) of micelles before and after lyophilization/reconstitution in the absence and presence of β-CD (-/+CD) as cryoprotectant, as determined by dynamic light scattering DLS; values are expressed as mean ± standard deviation (n=3).

| Copolymer | Blank |  | Gossypol (GP) | Phloretin (PH) | Before freeze-drying (-CD) (PDI ± SD) | Before freeze-drying (+CD) (PDI ± SD) | After freeze-drying (-CD) (PDI ± SD) | After freeze-drying (+CD) (PDI ± SD) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PEG2PCL0.4 | √ |  | - | - | 0.149 ± 0.010 | 0.156 ± 0.009 | 0.196 ± 0.010 | 0.185 ± 0.013 |
| PEG2PCL1.1 | √ |  | - | - | 0.189 ± 0.011 | 0.245 ± 0.014 | 0.145 ± 0.048 | 0.149 ± 0.008 |
| PEG2PCL1.1 | - |  | √ | - | 0.140 ± 0.004 | 0.179 ± 0.052 | 0.162 ± 0.025 | 0.145 ± 0.005 |
| PEG2PCL1.1 |  | - | - | √ | 0.135 ± 0.023 | 0.158 ± 0.003 | 0.157 ± 0.009 | 0.126 ± 0.002 |
| PEG2PCL1.8 |  | √ | - | - | 0.225 ± 0.006 | 0.252 ± 0.007 | 0.141 ± 0.001 | 0.228 ± 0.002 |
| PEG2PCL1.8 |  | - | √ | - | 0.160 ± 0.025 | 0.187 ± 0.034 | 0.136 ± 0.008 | 0.132 ± 0.005 |
| PEG2PCL1.8 |  | - | - | √ | 0.147 ± 0.011 | 0.178 ± 0.030 | 0.158 ± 0.008 | 0.184 ± 0.005 |
| PEG2PCL4.0 |  | √ | - | - | 0.245 ± 0.030 | 0.195 ± 0.003 | 0.210 ± 0.011 | 0.186 ± 0.039 |
| PEG5PCL0.6 |  | √ | - | - | 0.262 ± 0.007 | 0.242 ± 0.003 | 0.210 ± 0.016 | 0.177 ± 0.050 |
| PEG5PCL1.3 |  | √ | - | - | 0.241 ± 0.008 | 0.245 ± 0.038 | 0.185 ± 0.016 | 0.188 ± 0.006 |
| PEG5PCL1.3 |  | - | √ | - | 0.126 ± 0.010 | 0.185 ± 0.016 | 0.148 ± 0.006 | 0.147 ± 0.007 |
| PEG5PCL1.3 |  | - | - | √ | 0.205 ± 0.003 | 0.257 ± 0.050 | 0.205 ± 0.003 | 0.246 ± 0.056 |
| PEG5PCL2.4 |  | √ | - | - | 0.192 ± 0.008 | 0.145 ± 0.030 | 0.176 ± 0.035 | 0.163 ± 0.011 |
| PEG5PCL2.4 |  | - | √ | - | 0.220 ± 0.060 | 0.201 ± 0.004 | 0.236 ± 00.17 | 0.158 ± 0.008 |
| PEG5PCL2.4 |  | - | - | √ | 0.197 ± 0.002 | 0.139 ± 0.005 | 0.131 ± 0.002 | 0.159 ± 0.014 |
| PEG5PCL4.2 |  | √ | - | - | 0.123 ± 0.006 | 0.132 ± 0.046 | 0.176 ± 0.006 | 0.138 ± 0.005 |
| PEG5PCL4.2 |  | - | √ | - | 0.192 ± 0.004 | 0.175 ± 0.003 | 0.156 ± 0.019 | 0.158 ± 0.016 |
| PEG5PCL4.2 |  | - | - | √ | 0.168 ± 0.028 | 0.085 ± 0.009 | 0.140 ± 0.040 | 0.137 ± 0.034 |
| PEG5PCL9.5 |  | √ | - | - | 0.138 ± 0.004 | 0.145 ± 0.011 | 0.128 ± 0.011 | 0.116 ± 0.021 |
| PEG5PCL9.5 |  | - | √ | - | 0.193 ± 0.002 | 0.197 ± 0.005 | 0.153 ± 0.011 | 0.156 ± 0.016 |
| PEG5PCL9.5 |  | - | - | √ | 0.144 ± 0.013 | 0.127 ± 0.011 | 0.118 ± 0.019 | 0.168 ± 0.030 |
| PEG10PCL3.2 |  | √ | - | - | 0.173 ± 0.004 | 0.186 ± 0.006 | 0.133 ± 0.002 | 0.186 ± 0.015 |
| PEG10PCL7.9 |  | √ | - | - | 0.170 ± 0.009 | 0.176 ± 0.003 | 0.195 ± 0.020 | 0.172 ± 0.009 |
| PEG10PCL7.9 |  | - | √ | - | 0.183 ± 0.013 | 0.172 ± 0.007 | 0.243 ± 0.011 | 0.232 ± 0.009 |
| PEG10PCL7.9 |  | - | - | √ | 0.149 ± 0.014 | 0.164 ± 0.006 | 0.182 ± 0.006 | 0.216 ± 0.024 |
| PEG10PCL10.7 |  | √ | - | - | 0.146 ± 0.017 | 0.149 ± 0.007 | 0.119 ±0.006 | 0.125 ± 0.002 |
| PEG10PCL10.7 |  | - | √ | - | 0.138 ± 0.006 | 0.153 ± 0.008 | 0.186 ± 0.006 | 0.187 ± 0.013 |
| PEG10PCL10.7 |  | - | - | √ | 0.116 ± 0.007 | 0.225 ± 0.042 | 0.230 ± 0.005 | 0.191 ± 0.017 |
| PEG10PCL14.9 |  | √ | - | - | 0.160 ± 0.008 | 0.160 ± 0.011 | 0.128 ±0.013 | 0.187 ± 0.025 |

Figure S5. Number, volume and intensity particle size distributions for (a) PEG2PCL0.4, (b) PEG2PCL1.1, (c) PEG2PCL1.8 and (d) PEG2PCL4.0 micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S6. Number, volume and intensity particle size distributions for (a) PEG5PCL0.6, (b) PEG5PCL1.3, (c) PEG5PCL2.4, (d) PEG5PCL4.2 and (e) PEG5PCL9.5 micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S7. Number, volume and intensity particle size distributions for (a) PEG10PCL3.2, (b) PEG10PCL7.9, (c) PEG10PCL10.7 and (d) PEG10PCL14.9 micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S8. SAXS profiles for (a) PEG2PCL0.4, (b) PEG2PCL1.1, (c) PEG2PCL1.8 and (d) PEG2PCL4.0 micelles/aggregates as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S9. SAXS profiles for (a) PEG5PCL0.6, (b) PEG5PCL1.3, (c) PEG5PCL2.4, (d) PEG5PCL4.2 and (e) PEG5PCL9.5 micelles/aggregates as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD). Background multiplication factor (BMF) for PEG5PCL1.3 LR+CD, PEG5PCL2.4 LR+CD, PEG5PCL4.2 LR+CD and PEG5PCL9.5 LR+CD was 0.72, 0.55, 0.55 and 0.53, respectively.

Figure S10. SAXS profiles for (a) PEG10PCL3.2, (b) PEG10PCL7.9, (c) PEG10PCL10.7 and (d) PEG10PCL14.9 micelles/aggregates as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD) (BMF for PEG10PCL3.2 LR+CD, PEG10PCL7.9 LR+CD and PEG10PCL10.7 LR+CD was 0.45, 0.55 and 0.53, respectively).

Figure S11. Number, volume and intensity particle size distributions for PEG5PCL1.3 (a) blank micelles and (b) gossypol (GP) and (c) phloretin (PH) loaded micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S12. Number, volume and intensity particle size distributions for PEG5PCL2.4 (a) blank micelles and (b) gossypol (GP) and (c) phloretin (PH) loaded micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S13. Number, volume and intensity particle size distributions for PEG5PCL4.2 (a) blank micelles and (b) gossypol (GP) and (c) phloretin (PH) loaded micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S14. Number, volume and intensity particle size distributions for PEG5PCL9.5 (a) blank micelles and (b) gossypol (GP) and (c) phloretin (PH) loaded micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S15. SAXS profiles for (a) gossypol and (b) phloretin loaded PEG5PCL1.3 micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S16. SAXS profiles for (a) gossypol and (b) phloretin loaded PEG5PCL2.4 micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S17. SAXS profiles for (a) gossypol and (b) phloretin loaded PEG5PCL4.2 micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD) (BMF for PEG5PCL4.2 GP LR+CD and PEG5PCL4.2 PH LR+CD was 0.65 and 0.91, respectively).

Figure S18. SAXS profiles for (a) gossypol and (b) phloretin loaded PEG5PCL9.5 micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD)  (BMF for PEG5PCL9.5 PH LR+CD was 0.91).

Figure S19. Number, volume and intensity particle size distributions for PEG2PCL1.8 (a) blank micelles and (b) gossypol (GP) and (c) phloretin (PH) loaded micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S20. Number, volume and intensity particle size distributions for PEG10PCL10.7 (a) blank micelles and (b) gossypol (GP) and (c) phloretin (PH) loaded micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S21. Hydrodynamic diameter (Dh) versus weight fraction of PCL (fPCL) as determined from number particle size distributions (PSDs) for (a) gossypol (GP) and (b) phloretin (PH) loaded PEG2PCL1.8 micelles as prepared (AP) and after lyophilization/reconstitution (LR) and in the absence and presence of β-CD (-/+CD). All values are reported as the mean + std. dev. (n = 3).

Figure S22. Dh versus fPCL as determined from number PSDs for (a) gossypol (GP) and (b) phloretin (PH) loaded PEG10PCL10.7 micelles as prepared (AP) and after lyophilization/reconstitution (LR) and in the absence and presence of β-CD (-/+CD). All values are reported as the mean + std. dev. (n = 3).

Figure S23. SAXS profiles for (a) gossypol and (b) phloretin loaded PEG2PCL1.8 micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).

Figure S24. SAXS profiles for (a) gossypol and (b) phloretin loaded PEG10PCL10.7 micelles as prepared (AP) and after lyophilization/reconstitution (LR) in the absence and presence of β-CD (-/+CD).