SUPPLEMENTARY

Dielectric elastomer actuators have recently been used to drive tunable optic and acoustic devices. For example, a circular DEA was used to adjust the membrane tension in an acoustic absorber while it can be equally useful to unfold the microwrinkles on a tunable window device [1]. On the other hand, an annular DEA was used to relax the membrane tension that stretched a deformable lens of oil capsule [2-4]. This work uses similar DEA drive. The drive of these tunable devices requires only small displacement. Hence, analysis of electrostatically induced deformation can assume small strain, and thus simple elastic models can be used instead of nonlinear models which were previously used for the analysis of large deformation [5-7].

# Dielectric Elastomer Actuator Design

Figure 1. Isometric cross-sectional view of the various designs of the DEAs. Schematic of (a) circular DEA for radial actuation under isotonic condition; (b) circular DEA for tension change under isometric condition, (c) annular DEA for controlling the hole size in a passive membrane.

A dielectric elastomer actuator is a soft capacitor that undergoes an areal expansion when being compressed by Maxwell stress [8, 9]. The Maxwell stress (electrostatic pressure) can modulate the membrane tension, which greatly helps to enhance the voltage-induced areal expansion. However, the level of actuation varies substantially with the boundary and loading conditions, even when ideally compliant electrodes were used to drive the dielectric elastomer actuators. This supplementary article sequentially presented the analyses of three designs of dielectric elastomer actuators shown in Figure 1, which include (1) a circular DEA for radial actuation under isotonic condition; (2) a circular DEA for tension change under isometric condition, (3) an annular DEA for controlling the hole size in a passive membrane.[7] The formulation for the annular DEA is applied to evaluate theoretical prediction for the micro-perforated dielectric elastomer actuators (MPDEA).

## Circular DEA for Radial Actuation under Isotonic Condition

Figure 2. DEA with circular disc electrodes at (left) inactivated state; (right) activated state.

Let us consider a circular DEA sandwiched by small compliant electrode disks as shown in Figure 2. While being surrounded by a large passive pre-stretched membrane, the electroded membrane can maintain a constant pre-stress even during DEA activation. Under this biaxial isotonic condition, the voltage-induced net biaxial strains (∆S1 and ∆S2)  is simply the Poisson’s ratio effect of Maxwell stress and is given as:

|  | ∆S1=S1-S10=νPeE, | (S.1) |
| --- | --- | --- |
|  | ∆S2=S2-S20=νPeE. |  |

where E and ν are the Young modulus and Poisson's ratio of dielectric elastomer membrane, respectively. The biaxial pre-strains (S10 and S20) due to initially applied biaxial pre-stress T10 and T20 is given by [10]

|  | S10=T10E-νT20E, | (S.2) |
| --- | --- | --- |
|  | S20=T20E-νT10E, |  |

and the total biaxial strains under voltage activation are given by constitutive equations

|  | S1=T1E-νT2E-νT3E, | (S.3) |
| --- | --- | --- |
|  | S2=T2E-νT1E-νT3E. |  |

where T3 is the normal traction due to the electrostatic pressure (Pe) expressed as [6, 8, 11, 12],

|  | T3=-Pe=-ϵrϵoVt22, | (S.4) |
| --- | --- | --- |

and T1=T10 and T2=T20  for the isotonic condition. Here V and t are the applied voltage and thickness of the membrane.

## Circular DEA for Tension Change under Isometric Condition

Figure 3. DEA with annular electrodes at (left) inactivated state; (right) activated state.

Next, we consider a circular DEA sandwiched fully by compliant electrodes as shown in Figure 3. There is no passive membrane and the whole DEA is surrounded by a fixed boundary. Under this isometric condition, activation of the DEA cannot produce any areal expansion, but it can reduce the membrane tension. Based on the constitutive equation for a biaxially pre-stretched membrane given in [7]Equation (S.3) and isometric boundary condition S1=S10 and S2=S20, the membrane’s biaxial tensions under voltage activation of the DEA are derived to be

|  | T1=T10-νPe1-ν, | (S.5) |
| --- | --- | --- |
|  | T2=T20-νPe1-ν. |  |

using the isometric identity, S1+νS2=S10+νS20 or, νS1+S2=νS10+S20.

Under equibiaxial pre-tension, i.e. T1=T2 and T10=T20, the membrane stress change  ΔT=T1-T10=T2-T20 is solely due to the electrostatic pressure following,

|  | ΔT=-νPe1-ν. | (S6) |
| --- | --- | --- |

## Annular DEA for Controlling the Hole Size in a Passive Membrane

Next, we consider a DEA of annular shape which is used to control the size of a hole through the central passive membrane (see Figure 4). The external annular DEA and the inner passive annulus are made of the same piece of pre-stretched dielectric elastomer membrane. The difference lies in the electrode coverage of the former. The diameter of through-hole at the centre of the passive annular membrane is moderated by DEA. Voltage activation of the DEA can control membrane tension. In turn, this distant membrane tension change tunes the hole diameter of the passive inner annulus.

Figure 4. Schematic of a DEA with an annular electrode surrounding a hole at: (left) inactivated state; (right) activated state.

Let’s consider an annular DEA of radius b with the through-hole of a radius, and an initial radial pre-stress σ1∞ (see Figure 4). In the case that DEA is much larger than the passive annulus, the voltage induced stress change (Δσ1∞)  can be approximated as that induced under the isometric condition (refer to Equation (S6)) as

|  | Δσ1∞=-νPe1-ν. | (S.7) |
| --- | --- | --- |

Stress distribution in the DEA and passive annulus follows the general solution for stress surrounding a hole under radial loading, which is given as:

| σrr=σ1∞+σ2∞21-a2r2+σ1∞-σ2∞21-4a2r2+3a4r4cos2θ, |  | (S.8) |
| --- | --- | --- |
|  | σrθ=-σ1∞-σ2∞21+2a2r2-3a4r4sin2θ, |  |
|  | σθθ=σ1∞+σ2∞21+a2r2-σ1∞-σ2∞21+3a4r4cos2θ, |  |

where σ1∞ and σ2∞ are the applied bi-axial pre-stress far away from the hole. For the case of radial pre-stretching i.e. σ1∞=σ2∞, according to the plane stress analysis [13, 14], the stress distribution reduces to:

|  | σrr=σ1∞1-a2r2, | (S.9) |
| --- | --- | --- |
|  | σrθ=0, |  |
|  | σθθ=σ1∞1+a2r2. |  |

Similarly, the change in stress distribution (∆σrr,∆σrθ and ∆σθθ) are obtained by substituting Equation (S.7) in Equation (S.9) as,

|  | ∆σrr=∆σ1∞1-a2r2=-νPe1-ν1-a2r2, | (S.10) |
| --- | --- | --- |
|  | ∆σrθ=0 |  |
|  | ∆σθθ=∆σ1∞1+a2r2=-νPe1-ν1+a2r2. |  |

Since there is no electrode near the holes, the stress along thickness direction near the perforation holes does not change. The radial strain can be calculated from the equivalent radial stress using these constitutive equations as,

|  | ∆εrr=1E∆σrr-ν∆σθθ-ν∆σzz, | (S.11) |
| --- | --- | --- |
|  | =1E-νPe1-ν1-a2r2+ννPe1-ν1+a2r2. |  |

Integration of this radial strain to the radius yields the radial displacement as,

|  | ∆ur=∆εrrdr=-ν1-νPeEr+a2r-νr-a2r+cθ,z, | (S.12) |
| --- | --- | --- |

The unknown constant cθ,z can be solved by using the isometric boundary condition that applies the outer edge of the DEA does not move, i.e.∆ur=0 at r=b as,

|  | cθ,z=ν1-νPeEb+a2b-νb-a2b. | (S.13) |
| --- | --- | --- |

In turn, the radial displacement takes the following form,

| ∆ur=-ν1-νPeEr+a2r-νr-a2r-b+a2b+νb-a2b | (S.14) |
| --- | --- |

As such, the reduction of the hole radius (i.e. ∆ur at r=a) by voltage activation is given by

|  | ∆urr=a=∆a(V)=ν1-νPeEb+a2b-2a-νb-a2b | (S.15) |
| --- | --- | --- |

This equation is used to predict the hole size change of a tunable micro-perforated membrane absorber or MSDEBA.

# Microwrinkle Formation and Electrical Unfolding

Figure 5. (a) Stretch states of a dielectric elastomer actuator during the wrinkle formation and unfolding; (b) Schematic of an isometric view of a wrinkled surface.

Hard coating such as metal or conductive oxide in submicron thickness is axially stiffer and non-stretchable as compared to an elastomer substrate. But, under axial compression, it buckles into wrinkles. This microwrinkled thin film becomes stretchable as it is unfoldable. Hence, this microwrinkled thin films of metal or conductive oxides can make compliant electrodes for dielectric elastomer actuators.

## Microwrinkle Formation.

Here, we show the fabrication of wrinkled compliant electrodes for a DEA or a soft capacitor. The fabrication is done in three steps (see Figure 5). First, a pristine elastomer membrane is radially pre-stretched. This enlarges the diameter of the elastomeric substrate from an initial value DS0 to be pre-stretched diameter DSI. Meanwhile, this reduces the membrane thickness from an initial value of t0 to tI, which follows the relationship of volume incompressibility t0DS02=tIDSI2.

Second, the thin films of metal or conductive oxides are deposited on both sides of the first pre-stretched elastomer substrate. The diameter of these as-deposited film is DI.

Third, the thin films are subjected to a biaxial compression by relaxing the elastomer pre-stretch. This reduces the thin film diameter to DII in proportion to the elastomer diameter DSII following the relationship DII/DI=DSII/DSI.

The pre-compression strain in the thin films is

|  | e0=DIIDI-1. | (S.16) |
| --- | --- | --- |

Critical microwrinkling happens if the pre-compression strain is equal to the critical buckling strain given by (see Figure 5(b)) [15],

|  | ec=1433EsEf2, | (S.17) |
| --- | --- | --- |

which depends on the modulus mismatch between the film and the substrate. Here, Es and Ef are Young’s modulus of the substrate and thin-film respectively.

Then, the critical pitch length Lc of the microwrinkle is [15-19]:

|  | Lc=2πtf3Ef3Es | (S.18) |
| --- | --- | --- |

where tf is the thickness of thin-film.

Post-buckling  happens to the thin film when pre-compressive strain is greater than the critical strain ec [15, 20, 21]. According to the Accordion bellow mechanics, the amplitude of the post buckled wrinkle is

|  | A=Lc1+νπe-ec, | (S.19) |
| --- | --- | --- |

while the pitch length decreases with an increase in the compressive strain as

|  | L=Lc1-e(1-ec). | (S.20) |
| --- | --- | --- |

Equation (S.18), (S.19), and (S.20) suggests that a harder coating can form wrinkles of higher amplitude even under a smaller compressive strain.

Figure 6. Schematic of a DEA at (a) in-active and (b) active states

## Voltage-induced Unfolding of Microwrinkles.

Voltage-induced activation strain can unfold the microwrinkled thin-film electrodes of a DEA (see Figure 6). A high voltage (V) activation of the DEA induces a radial expansion with diameter increment ΔD(V) = D(V) – DII, relative to the diameter prior electrical activation DII (see Figure 5). Based on the strain model given in Equation (S.1), the elastomer membrane is subjected to the following radial expansive strain:

|  | ΔD(V)DII=12νεrε0EsVtII2, | (S.21) |
| --- | --- | --- |

where ν is the Poisson’s ratio which has a value of 0.5 for the incompressible elastomer. In turn, the reduced compressive strain in the microwrinkled thin films relative to their as-deposited diameter (DI) is given as:

|  | eV=DVDI-1=e0+ΔDVDIIDIIDI=e0+ΔDVDII1+e0 ≈e0+1+e0εrε04YsVtII2. | (S.22) |
| --- | --- | --- |

This helps to unfold the microwrinkled electrodes. Such reversible microwrinkling and unfolding are useful to tune an optical diffuser.

# Acoustic Absorption Coefficient of a Microperforated Membrane Absorber

Figure 7. (a) Schematic showing the perforation size change by voltage activation of the MPDEA; (b) An equivalent electro-acoustic circuit representing the MPDEA backed by an air cavity. (retrieved from [22])

This described Micro-perforated membrane absorber consists of an MPDEA and a back cavity. The air-filled back cavity has a depth L from a rigid backplate. Consider a sound wave of a frequency f that travels at the sound speed c0 in the air. Upon normally impinging on the rigid wall (normal incidence), the sound reflects and produces an equivalent source pressure 2p. The sound absorption coefficient αV of this MPDEA has a similar expression as derived for the perforated membrane absorber,[23] except here it is also dependent on the voltage applied to MPDEA as given by:

|  |  | αV=4RezV1+RezV2+ImzV2, | (S.23) |
| --- | --- | --- | --- |

Where z is the total acoustic impedance of the resonant absorber as presented in the electro-acoustic model in Figure 7(b). The model has a mass-impedance element in series with a cavity reactance zH=-jcotωHc0, where ω=2πf, f is the frequency (Hz). The mass-impedance is voltage tunable. It consists of a parallel connection of a membrane impedance zM=1ρ0c0RM+jMM, and a perforation impedance zP=1ρ0c0RP+jMP. Here, R and M denotes the acoustic resistance and reactance respectively. Based on the electro-acoustic model, the total acoustic impedance is

|  | z=zMzPzM+zP+zH, | (S.24) |
| --- | --- | --- |

The pre-tensioned micro-perforated membrane vibrates like a string when it is subjected to s sound pressure wave ∆p in the air of density ρo and the viscosity μ. Applying a voltage to the MPDEA reduces the membrane tension. This modulated membrane tension T(V) also tunes the membrane’s resonant frequency [24]. Consider a pre-tensioned circular membrane with an outer radius Ro with material properties as: membrane surface density (ρm) and internal damping (η). Its membrane acoustic impedance zM is given by [23]:

|  | zMU=ωρpjρ0c02KmemUL0J1KmemUL0J0KmemUL0-1-1 | (S.25) |
| --- | --- | --- |

where Kmem'=ω2ρmTV+2jωη is voltage-dependent (as indicated with a prime symbol), J1 is the Bessel function of the first kind and first order, and J0 is the same of zeroth order. This shows the dependence of membrane impedance on the electrically controllable tension.

The acoustic impedance of the array of N perforations in the MPDEA with the circular membrane of outer radius Ro is a sum of contribution by individual holes of a’, given by

|  | zPV=n=1NRo2a'2zholeR,V | (S.26) |
| --- | --- | --- |

where a'=a-∆a(V) is the activated hole size.

The acoustic impedance zholeR,V of individual holes at the radial coordinate R in the circular flexible membrane is given by [25]

| zholeR,V=j2ρ0c0ωρmKaira'J1Kaira'J0Kaira'J0KmemRJ0KmemR0-1+1zMaa'δ'-1, | (S.27) |
| --- | --- |

where Kair=-jρ0ωμ, δ'=Na'2/Ro2 is the perforation ratio of the membrane with N number of holes.

Maa’s estimated acoustic impedance zMaa' of a hole in the rigid panel is given by[25, 26]

| zMaa'=36.75×10-3ta'2δ'1+x'232+24x'a't+j0.294×10-3ωtδ'1+19+x'2/2+1.70a't, | (S.28) |
| --- | --- |

where x'=a'2f/5 is the perforation constant. These equations show the dependence of perforation impedance on both hole size and tension which are electrically controllable.

Two kinds of acoustic absorbers were fabricated, namely, 1-layered MPDEA and 2-layered MPDEA. Each layer is a 3 time radially pre-stretched VHB4910 tape, with a pre-stretched membrane thickness of 125.0 µm. The Young’s modulus of these radially pre-stretched membranes averages at 1.14 MPa. The parameters affecting the acoustic behaviour of the fabricated MPDEAs are shown in below.

Table 1. Design parameters for the MPDEAs.

| Sample | Pre-stretch ratio λ | Initial hole’s diameter 2a μm() | Thickness t (μm) | Perforation ratio δ (%) |
| --- | --- | --- | --- | --- |
| One-layer MPDEA | 3 | 447.50 | 125.0 | 0.427 |
| Two-layer MPDEA | 3 | 541.04 | 2×125.0 | 0.626 |

The parameters used for theoretical modelling of the two-layer MPDEA are TV=0kV=57.69N/m and TV=5kV=49.29N/m (Measured), μ=1.846×10-5kg/(m∙s), R0=0.01025m c0=346m/s ρ0=1.184kg/m3, ρm=0.1904kg/m2 (surface density), η=0.02, and H=0.04m.

REFERENCES

[1]	Z. Lu, Y. Cui, M. Debiasi, and Z. Zhao, "A Tunable Dielectric Elastomer Acoustic Absorber," Acta Acustica united with Acustica, vol. 101, no. 4, pp. 863-866, 2015.

[2]	M. Shrestha, T.-G. La, and G. K. Lau, "Inkjet Printed Stretchable Electrodes For Tunable Focus Lens," in 2nd International Conference on Progress in Additive Manufacturing (Pro-AM 2016) Singapore, 2016.

[3]	L. Maffli, S. Rosset, M. Ghilardi, F. Carpi, and H. Shea, "Ultrafast All-Polymer Electrically Tunable Silicone Lenses," Advanced Functional Materials, vol. 25, no. 11, pp. 1656-1665, 2015.

[4]	Federico Carpi , Gabriele Frediani, Simona Turco , and Danilo De Rossi, "Bioinspired Tunable Lens with Muscle-Like Electroactive Elastomers," Adv. Funct. Mater. , vol. 21, pp. 4152–4158, 2011.

[5]	R. Pelrine, R. Kornbluh, Q. Pei, and J. Joseph, "High-speed electrically actuated elastomers with strain greater than 100%," Science, vol. 287, no. 5454, pp. 836-839, 2000.

[6]	G. Kofod, P. Sommer-Larsen, R. Kornbluh, and R. Pelrine, "Actuation Response of Polyacrylate Dielectric Elastomers," Journal of Intelligent Materials Systems and Structures, vol. 14, no. 12, pp. 787-793, 2003.

[7]	M. Shrestha, "Smart window for tuning transparency and noise absorption," 2019.

[8]	Ronald E. Pelrine, Roy D. Kornbluh , and Jose P. Joseph, "Electrostriction of polymer dielectrics with compliant electrodes as a means of actuation," Sensors and Actuators A: Physical, vol. 64, pp. 77-85, 1998.

[9]	M. Kollosche, J. Zhu, Z. Suo, and G. Kofod, "Complex interplay of nonlinear processes in dielectric elastomers," Physical Review E, vol. 85, no. 5, 2012.

[10]	F. Carpi, P. Chiarelli, A. Mazzoldi, and D. De Rossi, "Electromechanical characterisation of dielectric elastomer planar actuators: comparative evaluation of different electrode materials and different counterloads," Sensors and Actuators A: Physical, vol. 107, no. 1, pp. 85-95, 2003.

[11]	M. Wissler and E. Mazza, "Electromechanical coupling in dielectric elastomer actuators," Sensors and Actuators A: Physical, vol. 138, no. 2, pp. 384-393, 2007.

[12]	Z. Suo, "Theory of dielectric elastomers," Acta Mechanica Solida Sinica, vol. 23, no. 6, pp. 549-578, 2010.

[13]	A. D. Wilson, "Inplane displacement of a stressed membrane with a hole measured by holographic interferometry," Applied optics, vol. 10.4, pp. 908-912, 1971.

[14]	S. Timoshenko and J. N. Goodie, "Theory of Elasticity," 3rd ed.: McGraw-Hill Education, 1987, pp. 90-97.

[15]	P. Kim, M. Abkarian, and H. A. Stone, "Hierarchical folding of elastic membranes under biaxial compressive stress," Nat Mater, vol. 10, no. 12, pp. 952-7, Dec 2011.

[16]	J. Genzer and J. Groenewold, "Soft matter with hard skin: From skin wrinkles to templating and material characterization," Soft Matter, vol. 2, no. 4, p. 310, 2006.

[17]	A. L. Volynskii, S. Bazhenov, O. V. Lebedeva, and N. F. Bakeev, "Mechanical buckling instability of thin coatings deposited on soft polymer substrates," Journal of Materials Science, vol. 35, pp. 547– 554, 2000.

[18]	M. D. Casper, A. Ö. Gözen, M. D. Dickey, J. Genzer, and J.-P. Maria, "Surface wrinkling by chemical modification of poly(dimethylsiloxane)-based networks during sputtering," Soft Matter, vol. 9, no. 32, p. 7797, 2013.

[19]	Dan Wu, Huimin Xie, and Yajun Yin, "Fracture behavior of thin aluminum films on soft substrate," presented at the International Conference on Fracture, China, 2013.

[20]	H. Jiang, D. Y. Khang, J. Song, Y. Sun, Y. Huang, and J. A. Rogers, "Finite deformation mechanics in buckled thin films on compliant supports," Proc Natl Acad Sci U S A, vol. 104, no. 40, pp. 15607-12, Oct 2007.

[21]	S. H. Low and G. K. Lau, "Bi-axially crumpled silver thin-film electrodes for dielectric elastomer actuators," Smart Materials and Structures, vol. 23, no. 12, p. 125021, 2014.

[22]	Z. Lu, M. Shrestha, and G.-K. Lau, "Electrically tunable and broader-band sound absorption by using micro-perforated dielectric elastomer actuator," Applied Physics Letters, vol. 110, no. 18, p. 182901, 2017.

[23]	C. Li, B. Cazzolato, and A. Zander, "Acoustic impedance of micro perforated membranes: Velocity continuity condition at the perforation boundary," J Acoust Soc Am, vol. 139, no. 1, pp. 93-103, Jan 2016.

[24]	Z. Lu, H. Godaba, Y. Cui, C. C. Foo, M. Debiasi, and J. Zhu, "An electronically tunable duct silencer using dielectric elastomer actuators," J Acoust Soc Am, vol. 138, no. 3, pp. EL236-41, Sep 2015.

[25]	Y. Li and B. M. Assouar, "Acoustic metasurface-based perfect absorber with deep subwavelength thickness," Applied Physics Letters, vol. 108, no. 6, p. 063502, 2016.

[26]	D.-Y. Maa, "Potential of microperforated panel absorber," Journal of the Acoustical Society of America, vol. 104, no. 5, 1998.