Supplementary material

Figure S1. Full field strain measurement using digital image correlation (DIC) on VN-A foam submitted to quasi-static compression (strain rate = 0.01 s-1)

Figure S2. Sensibility analysis of the quality of the fit (measure with R2) between experimental point and the fitted stress vs. strain vs. strain rate surface in impact compression. The varied parameters are the degree of the polynomial fit function (x=strain rate, y=strain and z= stress)

Figure S3. Stress vs. strain data dependant of the falling height of the impactor in compression (a), b) and c)) and in combined compression and shear (d), e) and f) for VN-A, VN-B and VN-C

Table S4. Coefficient of the equation of the fitted surface for the dynamic compression and compression and shear experiments. The equation for engineering strain (ε), strain rate (τ, in s-1) and engineering stress (σ, in MPa) is : σ = P01+ P02*τ + P03* ε + P04* ε * τ + P05* ε 2+P06* τ * ε 2 +P07* ε 3 +P08* τ * ε 3 +P09* ε 4 +P10* τ * ε 4 +P11* ε 5

|  | P01 | P02 | P03 | P04 | P05 | P06 | P07 | P08 | P09 | P10 | P11 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Compression |  |  |  |  |  |  |  |  |  |  |  |
| VN-A | 0.015024 | -0.00016 | 7.179431 | 0.005303 | -50.6775 | -0.00474 | 154.9543 | -0.00683 | -212.629 | 0.009198 | 109.9579 |
| VN-B | -0.00778 | -8.5E-05 | 17.21608 | -0.00916 | -115.953 | 0.100709 | 326.1629 | -0.24255 | -410.552 | 0.173589 | 193.9375 |
| VN-C | 0.020099 | -0.0002 | 23.80014 | -0.01559 | -163.719 | 0.236052 | 475.953 | -0.6654 | -616.255 | 0.549516 | 300.7181 |
| Compression and shear |  |  |  |  |  |  |  |  |  |  |  |
| VN-A_comp. | 0.010035 | -0.00011 | 6.520374 | 0.002314 | -45.8227 | 0.025353 | 131.3971 | -0.08157 | -168.306 | 0.063221 | 82.45689 |
| VN-A_shear | 0.006431 | -6.1E-05 | 2.413618 | -0.00104 | -16.7353 | 0.022327 | 48.17804 | -0.05594 | -61.3093 | 0.04315 | 29.39983 |
| VN-B_comp. | -0.00087 | -3.5E-05 | 8.395636 | -0.00377 | -49.0205 | 0.048529 | 122.1456 | -0.10801 | -139.781 | 0.062038 | 63.01459 |
| VN-B_shear | 0.008019 | -5.2E-05 | 2.821841 | 8.46E-05 | -17.6541 | 0.009947 | 49.44416 | -0.02467 | -63.359 | 0.015053 | 31.24846 |
| VN-C_comp. | -0.05293 | 0.000265 | 17.50793 | -0.04863 | -75.113 | 0.639532 | -96.6524 | -2.03703 | 978.5668 | 1.879094 | -1241.44 |
| VN-C_shear | -0.01047 | 5.2E-05 | 7.936058 | -0.02321 | -63.965 | 0.3558 | 196.4778 | -1.39452 | -191.083 | 1.650063 | -17.8061 |

Figure S5. Strain rate dependent behavior of Vinyl Nitrile foams in combined compression and shear: surface plots and experimental data (markers) showing engineering stress vs strain and dynamic strain rate for (a1) and (a2) VN-A in compression and shear, respectively; (b1) and (b2) VN-B in compression and shear, respectively; (c1) and (c2)  VN-C in compression and shear, respectively