Supplementary Material

Facile Solution Synthesis, Processing and Characterization of n- and p-Type Binary and Ternary Bi–Sb Tellurides

Bejan Hamawandi 1, Sedat Ballikaya 2, Hazal Batili 1, Viking Roosmark 1, Martina Orlovská 3, Aminu Yusuf 4, Mats Johnsson 5, Rafal Szukiewicz 6,7, Maciej Kuchowicz 6,7 and Muhammet S. Toprak 1,*

1	Department of Applied Physics, KTH Royal Institute of Technology, SE10691 Stockholm, Sweden; bejan@kth.se (B.H.); batili@kth.se (H.B.)

2	Department of Physics, Istanbul University, Fatih, 34320 Istanbul, Turkey; ballikaya@istanbul.edu.tr

3	Department of Inorganic Materials, Slovak University of Technology in Bratislava, 812 37 Bratislava, Slovak Republic; martina.orlovska@stuba.sk

4	Department of Elec. and Elec. Engineering, Istanbul University-Cerrahpasa, Avcilar, 34135 Istanbul, Turkey; sedatballikaya@yahoo.com

5	Department of Materials and Environmental Chemistry, Stockholm University, SE-106 91 Stockholm, Sweden; mats.johnsson@mmk.su.se

6	ŁUKASIEWICZ Research Network—PORT Polish Center for Technology Development, Stablowicka 147, 54–066 Wroclaw, Poland; Rafal.Szukiewicz@port.org.pl (R.S.); Maciej.Kuchowicz@port.org.pl (M.K.)

7	Institute of Experimental Physics, University of Wroclaw, Maxa Borna 9, 50–204 Wroclaw, Poland

*	Correspondence: toprak@kth.se

Table 1. Literature review on microwave (MW) assisted synthesis of Bi2Te3; Details of the synthetic route (solvent, reactor), reaction temperature-time; morphology of resultant structures; the quantity typically obtained according to described procedure in the articles, and the reported transport data.

| Composition | Synthetic route, Solvent, Reactor | Rxn T and time | Morphology; Quantity* | ZT | Ref |
| --- | --- | --- | --- | --- | --- |
| ﻿Bi2Te3 | MW, polyol (EG); reflux system | T: No data t: 0.5–6 h | Nanorod; 1 mmol; 0.8 g | No data | [1] |
| Bi2Te3 | MW, mixed solvents of water and ethylene glycol (EG) | T: 150 oC t: 30 min | Hollow spheres 0.2 mmol; 0.16 g | No data | [2] |
| Bi2Te3 | MW, mixed solvents of water, and ethylene glycol (EG) | ﻿T: 150 oC t: 30 min | ﻿Hollow spheres, nanosaws, sheets; 0.03 mmol; 0.025 g | No data | [3] |
| Bi2Te3 | MW, polyol (EG) | ﻿T: 170–195 ◦C t: 30–60 min | ﻿Nanosheets and nanotubes 0.13 mmol; 0.11 g (based on Te) | No data | [4] |
| Bi2Te3 | MW; reduction in water; reflux system | T: No data t: 10 min | Nanocrystals; 1 mmol; 0.8 g | Single point at 300 K n-type ﻿ ZT: 1.18 | [5] |
| Bi2-xSbxTe3 (x: 0 – 2) | MW, polyol (EG) | ﻿T: 220 ◦C t: 2 min | ﻿Hexagonal platelets; 8 g | n-type - Bi2Te3 ZT: 1.04 at 440 K p-type - Sb2Te3, ZT: 1.37 at 523 K | This work |

*Quantity is estimated from the experimental details given in the respective articles, assuming 100% yield.

| (a) | (b) |
| --- | --- |

Figure 1. (a) Screenshot of the reactor for experimental design using multivessel rotor; (b) Multivessel high pressure rotor used for the MW assisted synthesis of Bi2-xSbxTe3 nanoparticles. The system can take up to 15 reactors which can be filled up to about 100 mL each, making it possible to synthesize high and reproducible quality nanostructures with a high yield, at a pilot scale, without needing any complicated or reflux systems.

| (a) | (b) |
| --- | --- |

Figure 2. (a) Typical temperature (T) – time (t) – power (P) profile of the MW-assisted synthesis process for Bi2-xSbxTe3 samples. (b) As-synthesized sample transferred to a centrifuge vial and phase separation is easily achieved, yielding typically 2–3 g sample per reactor vessel. A total of 4 positions/vials (out of 15) during the MW assisted reaction is sufficient to prepare 8–10 g of these materials within a reaction time of 2 min.

|  | (1) |
| --- | --- |
|  | (2) |
| TOP(Te) Te + TOPO |  |
| (2-x) Bi + x Sb + 3 Te(TOP) → Bi2-xSbxTe3 + 3 TOPO | (3) |

Figure 3. Reaction mechanism showing the molecular structure of organic components used for the polyol synthesis of Bi2-xSbxTe3 nanoparticles. While Bi2-xSbxTe3 nanoparticles are formed ethyleneglycol (EG) is converted to diacetyl (rxn (1)), while trioctylphosphine (TOP) is converted to trioctylphosphine oxide (TOPO) (rxn (2)).

| (a) | (b) |
| --- | --- |

Figure 4. (a) Unit cell of Bi2Te3 [6], and (b) Estimated change of the lattice parameter of a (or b) by substitution of Sb (x) in Bi2-xSbxTe3 system.

| (a) | (b) | (c) |
| --- | --- | --- |

Figure 5. (a) TEM micrograph of a typical as-made Bi2Te3 nanoparticle with a lateral cross-sectional size of about 500 nm; (b) High resolution micrograph showing lattice fringes (distance between the planes is measured as 0.22 nm, corresponding to (110) plane of rhombohedral Bi2Te3 structure) and (c) Fourier-transform of the selected square region in (b) showing crystalline nature of Bi2Te3 nanoplatelet.

.

Figure 6. High resolution XPS Spectra of as-made Bi2-xSbxTe3 samples, for the regions Bi 4f, Sb 3d and Te 3d.

Table 2. Transport properties for nanostructured bulk Bi2-xSbxTe3: mass density (𝜌) in percentage of the theoretical density, total thermal conductivity (tot), Lorentz number (Lo), electronic thermal conductivity (el), lattice thermal conductivity (lat).

| Sample | 𝜌 % | T (K) | total (W m−1 K − 1) | Lo (x10−8 V2/K2) | el (W m−1 K−1) | lat (W m−1 K−1) |
| --- | --- | --- | --- | --- | --- | --- |
| Bi2Te3 | 78 | 300 | 0.94788 | 1.81 | 0.5775 | 0.37038 |
|  |  | 440 | 0.87553 | 1.71 | 0.60205 | 0.27348 |
| Bi1.8Sb0.2Te3 | 83 | 300 | 1.33091 | 1.97 | 1.1668 | 0.1632 |
|  |  | 523 | 1.05234 | 1.79 | 0.97789 | 0.07211 |
| Bi0.5Sb1.5Te3 | 78 | 300 | 0.85478 | 1.89 | 0.22724 | 0.62754 |
|  |  | 523 | 0.46612 | 1.71 | 0.24597 | 0.22015 |
| Sb2Te3 | 81 | 300 | 1.11645 | 1.89 | 1.3072 | -0.19075 |
|  |  | 523 | 0.84984 | 1.72 | 0.8478 | 0.00204 |

Fig S7. Hybrid thermoelectric film (1.5 × 5 cm2) with Ag paste contact. The films are made by blending the as-made thermoelectric nanoparticles with the polymer PVDF.

| (a) | (b) | (c) |
| --- | --- | --- |

Figure 8. Microstructure of the as-made Bi2Te3 nanoparticles-PVDF hybrid thermoelectric film at different magnifications. PVDF is visible as a dark shade in the rightmost micrograph, showing perfusing nanoparticles.

Figure 9. Device characteristic of the large area film made with Bi2Te3 nanoplatelets and PVDF. The resultant transport qualities for the film are S = - 46.12 µV/K, σ = 0.6013 S/m leading to a power factor of PF = 1.284 × 10−3 µW/mK2.

Reference

- Zhou, B; Zhao, Y.; Pu, L.; Zhu, J. Microwave-assisted synthesis of nanocrystalline Bi2Te3. Mater. Chem. Phys. 2006, vol. 96, pp. 192–196.

- Jiang, Y.; Zhu, Y.J.; Chen, L.D. Microwave-assisted preparation of Bi2Te3 hollow nanospheres. Chem. Lett. 2007, vol. 36, no. 3, pp. 382–383

- Jiang,Y.; Zhu, Y.J. Bi2Te3 nanostructures prepared by microwave heating. J. Cryst. Growth  2007, vol. 306, no. 2, pp. 351–355.

- Yao, Q.; Zhu, Y.; Chen, L.; Sun, Z.; Chen, X. Microwave-assisted synthesis and characterization of Bi2Te3 nanosheets and nanotubes. J. Alloys Compd. 2009, vol. 481, no. 1–2, pp. 91–95.

- Pradhan, S.; Das, R.; Bhar, R.; Bandyopadhyay, R.; Pramanik, P. A simple fast microwave-assisted synthesis of thermoelectric bismuth telluride nanoparticles from homogeneous reaction-mixture. J. Nanoparticle Res. 2017, vol. 19, no. 2, pp. 69-1 – 69-9.

- Available on line: https://materialsproject.org/materials/mp-34202/ (Accessed on 24 Jan 2020)