Supporting Information

Controlling the Structures, Flexibility, Conductivity Stability of Three-Dimensional Conductive Networks of Silver Nanoparticles/Carbon-Based Nanomaterials with Nanodispersion and their Application in Wearable Electronic Sensors

Chih-Wei Chiu 1,*, Jia-Wun Li 1, Chen-Yang Huang 1, Shun-Siang Yang 1, Yu-Chian Soong 1,

Chih-Lung Lin 1, Jimmy Chi-Min Lee 1, William Anderson Lee Sanchez 1, Chih-Chia Cheng 2,

and Maw-Cherng Suen 3

1 Department of Materials Science and Engineering, National Taiwan University of Science and Technology, Taipei 10607, Taiwan

2 Graduate Institute of Applied Science and Technology, National Taiwan University of Science and Technology, Taipei 10607, Taiwan

3 Department of Fashion Business Administration, LEE-MING Institute of Technology, New Taipei City 24305, Taiwan

* Correspondence: cwchiu@mail.ntust.edu.tw; Tel.: +886-2-2737-6521; Fax: +886-2-2737-6544

Received: date; Accepted: date; Published: date

Figure S1. GPC curves for PIB-SA, POE-2000, and PIB-POE-PIB triblock copolymer.

Figure S2. FT-IR spectra of PIB-SA, PIB-POE-PIB intermediate, and PIB-POE-PIB triblock copolymer.

Figure S3. (a) PIB-POE-PIB triblock copolymer in different solvents: (1) DI Water, (2) DMF, (3) acetone, (4) ethanol, (5) THF, and (6) toluene. (b) Carbon black dispersed in (1) DI water, (2) DMF without PIB-POE-PIB, and (3) DMF with PIB-POE-PIB.

Figure S4. (a) UV-vis absorption spectra (b) TEM images of colloidal AgNP particles in DI water containing AgNO3 and PIB-POE-PIB at weight ratios: (1) 1:1, (2) 5:1, and (3) 1:5.

Figure S5. TGA plots of AgNPs/PIB-POE-PIB/carbon-based nanomaterials hybrids with different weight ratios. (a) AgNPs/PIB-POE-PIB/CB (b) AgNPs/PIB-POE-PIB/CNT, and (c) AgNPs/PIB-POE-PIB/GO.

Figure S6. Preparation of highly electrically conductive films. Photos of AgNP/PIB-POE-PIB/carbon-based nanomaterials hybrid films with a weight ratio of 20:20:1 heated at 80 oC, 180 oC, 300 oC and 360 oC for 30 min. (a) AgNP/PIB-POE-PIB/CB, (b) AgNP/PIB-POE-PIB/CNT, and (c) AgNP/PIB-POE-PIB/GO.

Figure S7. (a) A circuit connected using (1) a non-conductive PI film and (2) an AgNP/PIB-POE-PIB/CB thin film. The latter is shown to be conductive. (b) After the thin film was subjected to flexural fatigue tests 5000 times, its sheet resistance was constant and approximately 10-1~10-2 Ω/sq. (c) The result showed that the sheet resistance of thin film is maintained by at least 10-1 Ω/sq after a durability test. (d)The cross-sectional and (e) the surface view of nanohybrid film after flexural fatigue tests 5000 times.

Figure S8. (a) Optical images of heart rate monitor device featuring AgNP/PIB-POE-PIB/CNT hybrid electrodes. (b) When the body was at rest and during exercise, complete and satisfactory signals for QRS-complexes and P- and T-waves were acquired from the ECGs obtained.

Figure S9. (a) Optical images of heart rate monitor device featuring AgNP/PIB-POE-PIB/CB hybrid electrodes. (b) Complete and satisfactory signals for QRS-complexes and P- and T-waves are acquired from the ECGs when the subject was at rest and during exercise.

Table S1. GPC results of PIB-SA, POE-2000 and PIB-POE-PIB triblock copolymer.

| Sample | Mn (Da) | Mw (Da) | Mz (Da) | Mz+1 (Da) | PDI |
| --- | --- | --- | --- | --- | --- |
| PIB-SA | 1785 | 2363 | 3055 | 3773 | 1.32 |
| POE-2000 | 2814 | 2882 | 2947 | 3011 | 1.02 |
| PIB-POE-PIB | 4696 | 6057 | 7431 | 8915 | 1.28 |

Table S2. The solubility of PIB-POE-PIB triblock copolymer in various solvents.

| Sample | Solubilitiesa |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | DI Water | DMF | Acetone | Ethanol | THF | Toluene |
| PIB-SA | - | - | +- | +- | + | + |
| POE-2000 | + | + | + | + | + | + |
| PIB-POE-PIB | +- | + | + | + | + | + |

a Concentration maintain with 0.25 g/10 ml. (+) soluble; (−) insoluble(+/−) ; Soluble but forming sediments after 2 h settlement.