Electronic Supporting Information (ESI)

Development of porous titania structure with improved photocatalytic activity: Response surface modeling and multi-objective optimization

Elvira Mahu, Maria Ignat *, Corneliu Cojocaru *,  Petrisor Samoila, Cristina Coromelci, Iuliean Asaftei, Valeria Harabagiu

submitted to:

NANOMATERIALS

Analysis of Variance (ANOVA) to test the significance of fitted models

Table  S1. ANOVA test for the fitted model.

| Source | DF (a) | SS (b) | MS (c) | F-value (d) | P-value (e) | R2 (f) | Radj 2 (g) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Model | 5 | 751.72 | 150.34 | 6.58 | 0.0296 | 0.868 | 0.736 |
| Residual | 5 | 114.28 | 22.86 |  |  |  |  |
| Total | 10 | 866.00 |  |  |  |  |  |

Table  S2. ANOVA test for the fitted model .

| Source | DF | SS | MS | F-value | P-value | R2 | Radj 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Model | 3 | 3.08410-3 | 1.02810-3 | 24.29 | 0.0004 | 0.912 | 0.875 |
| Residual | 7 | 2.96210-4 | 4.23210-5 |  |  |  |  |
| Total | 10 | 3.38110-3 |  |  |  |  |  |

Table  S3. ANOVA test for the fitted model .

| Source | DF (a) | SS (b) | MS (c) | F-value (d) | P-value (e) | R2 (f) | Radj 2 (g) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Model | 5 | 81.75 | 16.35 | 21.82 | 0.0021 | 0.956 | 0.912 |
| Residual | 5 | 3.75 | 0.75 |  |  |  |  |
| Total | 10 | 85.49 |  |  |  |  |  |

Table  S4. ANOVA test for the fitted model .

| Source | DF (a) | SS (b) | MS (c) | F-value (d) | P-value (e) | R2 (f) | Radj 2 (g) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Model | 5 | 72.66 | 14.53 | 11.84 | 0.0084 | 0.922 | 0.844 |
| Residual | 5 | 6.14 | 1.23 |  |  |  |  |
| Total | 10 | 78.80 |  |  |  |  |  |

(a) degree of freedom; (b) sum of squares; (c) mean square; (d) ratio between mean squares;

(e) probability of randomness; (f) coefficient of determination; (g) adjusted coefficient of determination;

As probability values (P-value) are less than 0.05 and the values of determination coefficient (R2) tend to unity (R21), the developed models are statistically significant and can be used to navigate the design space.

Fig.S1. Nitrogen adsorption-desorption isotherms, and corresponding BJH pore size distributions (calculated from adsorption and desorption branches, respectively).

20 µm

10 µm

20 µm

10 µm

M4 - SEM

M4 - SEM

M5 - SEM

M5 - SEM

Fig.S2. SEM images for the synthesized TiO2 nanoparticles - M4 and M5 samples.

Fig.S3. UVDR-derived Tauc indirect plots for the synthesized TiO2 nanoparticles - M4 and M5 samples, and determined band gap energies.

Fig.S4. FTIR spectra of synthesized TiO2 nanoparticles - M4 and M5 samples.

Fig.S5 Plots of ln(C/Co) as a function of time for the reduction of CR dye and 2,4D pesticide catalyzed by M5 TiO2 sample.