Supporting information for

Construction of Reinforced Self-Cleaning and Efficient Photothermal PDMS@GDY@Cu Sponges toward Anticorrosion and Antibacterial Applications

Yi Hu 1, Junmei Pu 1, Yingzi Hu 1, You Zi 1, Hongyan Chen 2, Mengke Wang 1,* and Weichun Huang 1

- School of Chemistry and Chemical Engineering, Nantong University, Nantong 226019, China;

2107320023@stmail.ntu.edu.cn (Y.H.); 2208320003@stmail.ntu.edu.cn (J.P.); 
2013320447@stmail.ntu.edu.cn (Y.H.); ziyou@ntu.edu.cn (Y.Z.); huangweichun@ntu.edu.cn (W.H.)

2	Engineering Training Center, Nantong University, Nantong 226019, China; chenhy@ntu.edu.cn

*	Correspondence: mengkewang@ntu.edu.cn

Table S1 Each component in the studied samples.

|  | Cu (wt%) | GDY (wt%) | PDMS (wt%) |
| --- | --- | --- | --- |
| Cu | 100 0 | 0 | 0 |
| PDMS@Cu | 78.4 2.1 | 0 | 21.7 2.1 |
| GDY@Cu-1 | 93.8 0.5 | 6.2 0.5 | 0 |
| GDY@Cu-2 | 87.2 0.2 | 12.8 0.2 | 0 |
| PDMS@GDY@Cu-1 | 75.4 0.3 | 5.0 0.5 | 19.6 0.8 |
| PDMS@GDY@Cu-2 | 71.9 0.1 | 10.6 0.2 | 17.6 0.1 |

Figure S1. Wavelength of the xenon short arc lamp solar simulator.

Figure S2. SEM image of the pristine Cu sponge.

Figure S3. SEM image of the GDY@Cu-1.

Figure S4. (a) SEM image of the GDY@Cu-2 and EDS mapping images of (b) C, (c) Cu, and (d) O elements.

Figure S5. Wettability of the PDMS@Cu-1 sponge.

Figure S6. Photographs of the samples before and after 7-day EIS characterization.

Figure S7. Antibacterial activity against (a) E. coil and (b) S. mutans at different temperatures.

Figure S8. TEM image of the GDY obtained by the sonication of PDMS@GDY@Cu-1 after two-week antibacterial experiment.