Supplementary Material: Low-Temperature Fabrication of High-Performance and Stable GZO/Ag/GZO Multilayer Structures for Transparent Electrode Applications

Akhmed K. Akhmedov 1, Aslan Kh. Abduev 1, Soslan Sh. Makhmudov 1, Vladimir M. Kanevsky 2, Arsen E. Muslimov 2 and Abil Sh. Asvarov 1, 2, *

1	Institute of Physics, Dagestan Federal Research Center, Russian Academy of Sciences, Makhachkala, Russia; cht-if-ran@mail.ru

2	Shubnikov Institute of Crystallography, Federal Research Center Crystallography and Photonics, Russian Academy of Sciences, Moscow, Russia; office@crys.ras.ru

*	Correspondence: abil-as@list.ru

| (a) |  |
| --- | --- |
| (b) |  |
| FIGURE S1. Cross-sectional SEM images of the GAG-3 (a) and GAG-4 (b) trilayer structures. |  |

Fig. S1 shows cross-sectional SEM images of GAG-3 and GAG-4 samples. The SEM image of GAG-3 was collected from the sample, prepared by simple cleaving of the Si substrate with trilayer structure on it (Fig. S1 (a)), while for GAG-4 the FIB technique was preliminarily employed for SEM sample preparation (Fig. S1 (b)).

Fig. S1 shows that the introducing of the Ag interlayer into the GAG structure results in breaking the GZO layer into two equal parts by both thickness and structure. The SEM images of Fig. S1(b) confirmed that, at a thickness ≥ 10 nm, a connected Ag interlayer without separated island shapes was well formed.

| (a) | Root Mean Square (RMS) Sq=0,897148 nm | (d) | RMS Sq= 1,08599 nm |
| --- | --- | --- | --- |
| (b) | RMS Sq= 1,22575 nm | (e) | RMS Sq= 1,19469 nm nm |
| (c) | RMS Sq= 1,14176 nm nm | (f) | RMS Sq= 1,11599 nm |
| FIGURE S2. AFM images (2×2 μm2) prepared in semi-contact mode for GAG-0 (a), GAG-1 (b), GAG-3 (c), GAG-4 (d), GAG-5 (e), and GAG-6 (f). |  |  |  |
| FIGURE S3. GAG-3 XRD plot in comparison with XRD spectra of pure bulk Ag and pure bulk ZnO materials. |  |  |  |  |  |