Supplementary Materials: The Exploration and Analysis of the Magnetic Relaxation Behavior in Three Isostructural Cyano-Bridged 3d−4f Linear Heterotrinuclear Compounds

Xia Xiong 1, Yangyu Liu 1, Shan Li 1, Anqi Xue 1, Juan Wang 1, Chi Zhang 1, Wenhua Zhu 1,*, and Haoling Sun 2,*

Table S1. Selected bond lengths (Å) and angles () for 1.

| 1 |  |  |  |
| --- | --- | --- | --- |
| Y(1)−N(1)#1 | 2.353(11) | Fe(1)−C(3) | 1.963(10) |
| Y(1)−N(1) | 2.353(11) | Fe(1)−C(3)#3 | 1.963(10) |
| Y(1)−O(1) | 2.208(11) | Fe(1)−C(3)#6 | 1.963(10) |
| Fe(1)−C(1) | 1.915(13) | Fe(1)−C(3)#7 | 1.963(10) |
| Fe(1)−C(2) | 1.922(13) |  |  |
| N(1)−Y(1)−N(1)#1 | 180 | O1#3−Y1−O1#7 | 89.92(45) |
| O1−Y(1)−O1#6 | 89.92(45) | O(1)−Y(1)−N(1) | 88.0(8) |
| O1#6−Y1−O1#7 | 89.92(45) | O(1)−Y(1)−N(1)#1 | 92.0(8) |
| O1−Y1−O1#3 | 89.92(45) |  |  |
| C(1)−Fe(1)−C(2) | 180 | C(3)#7−Fe(1)−C(3) | 178.3(5) |
| C(1)−Fe(1)−C(3) | 89.1(2) | C(3)#3−Fe(1)−C(3)#6 | 178.3(5) |
| C(1)−Fe(1)−C(3)#3 | 89.1(2) | C(3)#3−Fe(1)−C(3) | 89.987(8) |
| C(1)−Fe(1)−C(3)#6 | 89.1(2) | C(3)#6−Fe(1)−C(3) | 89.987(8) |
| C(1)−Fe(1)−C(3)#7 | 89.1(2) | C(3)#7−Fe(1)−C(3)#3 | 89.987(8) |
| C(2)−Fe(1)−C(3) | 90.9(2) | C(3)#7−Fe(1)−C(3)#6 | 89.987(8) |
| C(2)−Fe(1)−C(3)#3 | 90.9(2) |  |  |
| C(2)−Fe(1)−C(3)#6 | 90.9(2) |  |  |
| C(2)−Fe(1)−C(3)#7 | 90.9(2) |  |  |

Symmetry codes: #1 −x, −y, −z; #3 −y, x, z; #6 y, −x, z; #7 −x, −y, z.

Table S2. Hydrogen bonding geometry for 1: lengths (Å) and angles ().

| D−H···A | d(D−H) | d(H···A) | d(D···A) | <(DHA) |
| --- | --- | --- | --- | --- |
| N(2)−H(2)···N(2)#13 | 0.85 | 1.72 | 2.57(2) | 180 |
| O(2)−H(2A)···N(3) | 0.85 | 1.85 | 2.70(3) | 179.6 |
| O(2)−H(2A)···N(3)#2 | 0.85 | 2.10 | 2.91(3) | 159.0 |
| O(2)−H(2B)···N(3)#9 | 0.85 | 2.12 | 2.92(3) | 158.3 |
| O(2)−H(2B)···N(3)#10 | 0.85 | 1.84 | 2.68(32) | 179.3 |

Symmetry codes: #2 −x, y, z; #9 −y+1/2, x+1/2, −z+1/2; #10 −y+1/2, −x+1/2, −z+1/2; #13 −x, −y, −z+1.

Table S3. Selected bond lengths (Å) and angles () for 2.

| 2 |  |  |  |
| --- | --- | --- | --- |
| Dy(1)−N(1)#1 | 2.372(13) | Fe(1)−C(3) | 1.946(10) |
| Dy(1)−N(1) | 2.372(13) | Fe(1)−C(3)#3 | 1.946(10) |
| Dy(1)−O(1) | 2.244(11) | Fe(1)−C(3)#4 | 1.946(10) |
| Fe(1)−C(1) | 1.904(15) | Fe(1)−C(3)#5 | 1.946(10) |
| Fe(1)−C(2) | 1.906(14) |  |  |
| N(1)−Dy(1)−N(1)#1 | 180 | O1#4−Dy1−O1#5 | 89.98(44) |
| O1−Dy(1)−O1#3 | 89.98(44) | O(1)−Dy(1)−N(1) | 89.20(70) |
| O1#3−Dy1−O1#5 | 89.98(44) | O(1)−Dy(1)−N(1)#1 | 90.80(70) |
| O1−Dy1−O1#4 | 89.98(44) |  |  |
| C(1)−Fe(1)−C(2) | 180 | C(3)#5−Fe(1)−C(3) | 178.3(5) |
| C(1)−Fe(1)−C(3) | 89.20(30) | C(3)#4−Fe(1)−C(3)#3 | 178.3(5) |
| C(1)−Fe(1)−C(3)#3 | 89.20(30) | C(3)#3−Fe(1)−C(3) | 89.987(8) |
| C(1)−Fe(1)−C(3)#4 | 89.20(30) | C(3)#4−Fe(1)−C(3) | 89.989(8) |
| C(1)−Fe(1)−C(3)#5 | 89.20(30) | C(3)#5−Fe(1)−C(3)#4 | 89.988(8) |
| C(2)−Fe(1)−C(3) | 90.80(30) | C(3)#5−Fe(1)−C(3)#3 | 89.988(8) |
| C(2)−Fe(1)−C(3)#3 | 90.80(30) |  |  |
| C(2)−Fe(1)−C(3)#4 | 90.80(30) |  |  |
| C(2)−Fe(1)−C(3)#5 | 90.80(30) |  |  |

Symmetry codes: #1 −x, −y, −z; #3 y, −x, z; #4 −y, x, z; #5 −x, −y, z.

Table S4. Hydrogen bonding geometry for 2: lengths (Å) and angles ().

| D−H···A | d(D−H) | d(H···A) | d(D···A) | <(DHA) |
| --- | --- | --- | --- | --- |
| N(2)−H(2)···N(2)#13 | 0.86 | 1.69 | 2.54(3) | 180 |
| O(2)−H(2A)···N(3) | 0.85 | 1.86 | 2.70(2) | 179.3 |
| O(2)−H(2A)···N(3)#2 | 0.85 | 2.10 | 2.91(3) | 159.0 |
| O(2)−H(2B)···N(3)#11 | 0.85 | 2.10 | 2.91(3) | 158.4 |
| O(2)−H(2B)···N(3)#10 | 0.85 | 1.83 | 2.68(3) | 178.7 |

Symmetry codes: #2 −x, y, z; #10 −y+1/2, −x+1/2, −z+1/2; #11 −y+1/2, x+1/2, −z+1/2; #13 −x, −y, −z+1.

Table S5. Selected bond lengths (Å) and angles () for 3.

| 3 |  |  |  |
| --- | --- | --- | --- |
| Dy(1)−N(1) | 2.380(12) | Co(1)−C(3) | 1.904(10) |
| Dy(1)−N(1)#1 | 2.380(12) | Co(1)−C(3)#2 | 1.904(10) |
| Dy(1)−O(1) | 2.235(11) | Co(1)−C(3)#3 | 1.904(10) |
| Co(1)−C(1) | 1.860(13) | Co(1)−C(3)#4 | 1.904(10) |
| Co(1)−C(2) | 1.869(13) |  |  |
| N(1)#1−Dy(1)−N(1) | 180 | O1#3−Dy1−O1#4 | 89.969(1) |
| O1−Dy(1)−O1#2 | 89.969(1) | O(1)−Dy(1)−N(1)#1 | 90.7(7) |
| O1#2−Dy1−O1#4 | 89.969(1) | O(1)−Dy(1)−N(1) | 89.3(7) |
| O1−Dy1−O1#3 | 89.969(1) |  |  |
| C(1)−Co(1)−C(2) | 180 | C(3)−Co(1)−C(3)#4 | 178.2(5) |
| C(1)−Co(1)−C(3) | 89.1(3) | C(3)#3−Co(1)−C(3)#2 | 178.2(5) |
| C(1)−Co(1)−C(3)#2 | 89.1(3) | C(3)−Co(1)−C(3)#2 | 89.986(9) |
| C(1)−Co(1)−C(3)#3 | 89.1(3) | C(3)−Co(1)−C(3)#3 | 89.985(8) |
| C(1)−Co(1)−C(3)#4 | 89.1(3) | C(3)#4−Co(1)−C(3)#2 | 89.986(8) |
| C(2)−Co(1)−C(3) | 90.9(3) | C(3)#4−Co(1)−C(3)#3 | 89.986(9) |
| C(2)−Co(1)−C(3)#2 | 90.9(3) |  |  |
| C(2)−Co(1)−C(3)#3 | 90.9(3) |  |  |
| C(2)−Co(1)−C(3)#4 | 90.9(3) |  |  |

Symmetry codes: #1 −x, −y, −z; #2 y, −x, z; #3 −y, x, z; #4 −x, −y, z.

Table S6. Hydrogen bonding geometry for 3: lengths (Å) and angles ().

| D−H···A | d(D−H) | d(H···A) | d(D···A) | <(DHA) |
| --- | --- | --- | --- | --- |
| N(2)−H(2)···N(2)#13 | 0.85 | 1.71 | 2.56(2) | 180 |
| O(2)−H(2A)···N(3) | 0.85 | 1.83 | 2.68(4) | 179.2 |
| O(2)−H(2A)···N(3)#7 | 0.85 | 2.09 | 2.90(4) | 158.6 |
| O(2)−H(2B)···N(3)#9 | 0.85 | 2.15 | 2.95(4) | 157.8 |
| O(2)−H(2B)···N(3)#10 | 0.85 | 1.86 | 2.71(4) | 178.3 |

Symmetry codes: #7 −x, y, z ; #9 −y+1/2, x+1/2, −z+1/2 ; #10 −y+1/2, −x+1/2, −z+1/2 ; #13 −x, −y, −z+1.

Table S7. Continuous shaped measures (CShM) for 1−3 using SHAPE 2.1.

|  | 1 | 2 | 3 |
| --- | --- | --- | --- |
| HP-6 | 33.391 | 33.363 | 33.374 |
| PPY-6 | 30.016 | 30.116 | 30.072 |
| OC-6 | 0.131 | 0.079 | 0.105 |
| TPR-6 | 16.841 | 16.800 | 16.822 |
| JPPY-5 | 33.446 | 33.556 | 33.490 |

| HP-6 = (D6h) Hexagon | TPR-6 = (D3h) Trigonal prism |
| --- | --- |
| PPY-6 = (C5v) Pentagonal pyramid | JPPY-5 = (C5v) Johnson pentagonal pyramid (J2) |
| OC-6 = (Oh) Octahedron |  |

Figure S1. The disorder in the molecular structure of compound 2.

Figure S2. Powder X-ray diffraction patterns of compound 1 for the as-synthesized samples and the simulated one.

Figure S3. Powder X-ray diffraction patterns of compound 2 for the as-synthesized samples and the simulated one.

Figure S4. Powder X-ray diffraction patterns of compound 3 for the as-synthesized samples and the simulated one.

Figure S5. Field dependence of the magnetization at the temperatures of 2 K, 3 K, 5 K, 10 K and 15 K for a polycrystalline sample of 1.

Figure S6. Plots of the reduced magnetization M vs H/T at the temperatures of 2 K, 3 K, 5 K, 10 K and 15 K for a polycrystalline sample of 1.

Figure S7. Field dependence of the magnetization at the temperatures of 2 K, 3 K, 5 K, 10 K and 15 K for a polycrystalline sample of 3.

Figure S8. Plots of the reduced magnetization M vs H/T at the temperatures of 2 K, 3 K, 5 K, 10 K and 15 K for a polycrystalline sample of 3.

Figure S9. Field dependence of the in-phase (', inset) and out-of-phase ('') ac susceptibilities for 2 with f = 10, 100 and 999 Hz.

Figure S10. Field dependence of the in-phase (', inset) and out-of-phase ('') ac susceptibilities for 3 with f = 10, 100 and 999 Hz.

Figure S11. Temperature dependence of the in-phase (') and out-of-phase ('') ac susceptibilities for 3 under a 3 kOe dc field.