Supplementary file

(1) XRD analysis

Figure S1. Deconvoluted XRD diffractogram of the oleogels: (a) CR1, (b) CR2, (c) CR3, (d) CR4 and (e) CR5

Table S1. Parameters of the deconvoluted XRD diffractograms

| Formulations | Peaks | Peak position (o2θ) | FWHM | d-spacing (Å) | Crystallite size (nm) | Lattice strain |
| --- | --- | --- | --- | --- | --- | --- |
|  | Peak 1 | 20.289 | 4.749 | 5.079 | 2.060 | 0.116 |
|  | Peak 2 | 22.929 | 0.636 | 4.500 | 15.470 | 0.014 |
|  | Peak 3 | 24.201 | 1.238 | 4.267 | 7.960 | 0.025 |
| CR1 | Peak 4 | 25.269 | 0.585 | 4.089 | 16.880 | 0.011 |
|  | Peak 5 | 25.979 | 4.541 | 3.979 | 2.180 | 0.086 |
|  | Peak 6 | 28.800 | 10.152 | 3.597 | 0.980 | 0.173 |
|  | Peak 7 | 48.829 | 21.151 | 2.164 | 0.500 | 0.203 |
|  | Peak 8 | 22.714 | 3.547 | 4.542 | 2.770 | 0.077 |
|  | Peak 1 | 9.360 | 4.446 | 10.963 | 2.180 | 0.237 |
|  | Peak 2 | 18.000 | 11.100 | 5.718 | 0.880 | 0.306 |
|  | Peak 3 | 21.222 | 4.565 | 4.858 | 2.150 | 0.106 |
| CR2 | Peak 4 | 22.564 | 2.670 | 4.572 | 3.680 | 0.058 |
|  | Peak 5 | 23.743 | 1.166 | 4.348 | 8.450 | 0.024 |
|  | Peak 6 | 24.752 | 0.608 | 4.174 | 16.230 | 0.012 |
|  | Peak 7 | 25.477 | 4.038 | 4.057 | 2.450 | 0.078 |
|  | Peak 8 | 25.477 | 12.271 | 4.057 | 0.810 | 0.237 |
|  | Peak 1 | 15.156 | 4.814 | 6.783 | 2.020 | 0.158 |
|  | Peak 2 | 20.564 | 1.361 | 5.011 | 7.200 | 0.033 |
|  | Peak 3 | 22.253 | 6.775 | 4.635 | 1.450 | 0.150 |
| CR3 | Peak 4 | 22.253 | 1.978 | 4.635 | 4.970 | 0.044 |
|  | Peak 5 | 23.441 | 0.930 | 4.403 | 10.590 | 0.020 |
|  | Peak 6 | 24.448 | 0.650 | 4.225 | 15.190 | 0.013 |
|  | Peak 7 | 24.774 | 10.462 | 4.170 | 0.940 | 0.208 |
|  | Peak 8 | 32.455 | 26.455 | 3.201 | 0.380 | 0.397 |
|  | Peak 1 | 18.576 | 3.965 | 5.542 | 2.460 | 0.106 |
|  | Peak 2 | 21.642 | 18.885 | 4.764 | 0.520 | 0.431 |
|  | Peak 3 | 22.659 | 5.259 | 4.553 | 1.870 | 0.115 |
| CR4 | Peak 4 | 23.598 | 0.710 | 4.374 | 13.870 | 0.015 |
|  | Peak 5 | 24.700 | 0.679 | 4.182 | 14.530 | 0.014 |
|  | Peak 6 | 26.910 | 6.885 | 3.844 | 1.440 | 0.126 |
|  | Peak 7 | 26.910 | 1.800 | 3.844 | 5.510 | 0.033 |
|  | Peak 8 | 27.780 | 4.192 | 3.726 | 2.370 | 0.074 |
|  | Peak 1 | 13.187 | 9.615 | 7.790 | 1.010 | 0.363 |
|  | Peak 2 | 22.143 | 7.789 | 4.658 | 1.260 | 0.174 |
|  | Peak 3 | 23.341 | 4.670 | 4.422 | 2.110 | 0.099 |
| CR5 | Peak 4 | 24.046 | 0.679 | 4.294 | 14.510 | 0.014 |
|  | Peak 5 | 25.139 | 0.559 | 4.110 | 17.680 | 0.011 |
|  | Peak 6 | 27.287 | 6.415 | 3.792 | 1.550 | 0.115 |
|  | Peak 7 | 27.287 | 1.812 | 3.792 | 5.470 | 0.033 |
|  | Peak 8 | 30.350 | 9.094 | 3.417 | 1.100 | 0.146 |

(2) Crystallization kinetics

Figure S2. Crystallization profiles of the prepared oleogels fitted with exponential decay model.

(3) DSC analysis

Figure S3. Deconvoluted DSC thermograms of the prepared oleogels: (a) CR1, (b) CR2, (c) CR3, (d) CR4, and (e) CR5.

(4) Mechanical Analysis

Table S2. Stress relaxation model parameters

| Model | Model parameters | Formulations |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | CR1 | CR2 | CR3 | CR4 | CR5 |
| -- | Fo (g) | 745.545 ± 81.710a | 753.831 ± 76.540a | 1636.552 ± 483.351b | 2069.221 ± 515.664bc | 2829.952 ± 612.107c |
|  | F60 (g) | 132.694 ± 16.181a | 122.874 ± 17.255a | 366.720 ± 134.880b | 395.869 ± 109.236b | 693.765 ± 168.201c |
|  | %SR | 82.205 ± 0.733a | 83.741 ± 0.814ab | 77.874 ± 1.794c | 80.963 ± 0.571ad | 75.586 ± 1.005ce |
| Peleg's Model | k1 | 1.455 | 0.685 | 0.925 | 2.060 | 2.254 |
|  | k2 | 1.216 | 1.206 | 1.296 | 1.194 | 1.260 |
|  | R2 | 0.975 | 0.978 | 0.984 | 0.971 | 0.970 |
| Weichert Model | P0 | 0.185 | 0.168 | 0.229 | 0.198 | 0.252 |
|  | P1 | 0.251 | 0.181 | 0.222 | 0.246 | 0.194 |
|  | τ1 (sec) | 13.021 | 12.339 | 9.642 | 12.325 | 14.193 |
|  | P2 | 0.562 | 0.650 | 0.548 | 0.554 | 0.554 |
|  | τ2 (sec) | 0.454 | 0.335 | 0.390 | 0.429 | 0.439 |
|  | R2 | 0.998 | 0.999 | 0.999 | 0.998 | 0.998 |

Data is represented as mean ± standard deviation. Different small letters in the same row indicate significant differences using t-test (p < 0.05).

(5) Antimicrobial analysis

Figure S4. Antimicrobial analysis using E. coli: (a) CR1, (b) CR2, (c) CR3, (d) CR4, and (e) CR5; and Bacillus cereus: (g) CR1, (h) CR2, (i) CR3, (j) CR4, and (k) CR5.

(6) Ocular Irritation Test

Figure S5. Ocular irritation study as per Draize’s rabbit eye test using CR1D.

Figure S6. Ocular irritation study as per Draize’s rabbit eye test using CR2D.

Figure S7. Ocular irritation study as per Draize’s rabbit eye test using CR3D.

Figure S8. Ocular irritation study as per Draize’s rabbit eye test using CR4D.