## Slide 1
INFLUENCE OF THE INTERACTION BETWEEN FIBER HEMP RESIDUES AND SOIL ON THE MECHANICAL CHARACTERISTICS OF RESIDUES
Lekavičienė K., Naujokienė V., Eigirdas E.
Vytautas Magnus University, Agriculture Academy (Lithuania)
Fig. 3. Breaking time of unrolled and rolled hemp.
In order to contribute to the mitigation of climate change, the management of plant residues by reducing tillage is proposed [1,2]. However, after reducing tillage, plant residues on the surface of the soil do not lose their strong mechanical properties in a short time, so they clog the working parts of tillage machines or are inserted into the place of seed growth, thus worsening the technological process of sowing [3,4]. The force required to cut or break plant residues depends on the plant type, stem diameter, plant length, moisture, cell structure and elasticity, the time which the residue remains [5,6,7].
Growing population and consumption forces us to look to alternatives, and to make efforts and find solutions to facilitate the cultivation of fiber hemp because use fiber hemp can be for many different types of products. Therefore, it is important to look for solutions to facilitate the cultivation technologies of fiber hemp. The aim of the study was to evaluate the impact of the interaction of fibrous hemp (Cannabis sativa L.) residue and soil on the mechanical properties.
The research determined rolled and unrolled fiber hemp residues' effect on the moisture content, and mechanical characteristics. The fiber hemp is rolled with a roller after harvest in September (Fig. 1). Rolled and unrolled plant residues are left to overwinter. The mechanical characteristics of rolled and unrolled hemp in spring were determined with „Instron 5960“ equipment (Fig. 2). The breaking research was carried out with 5 mm, 8 mm, 10 mm diameter, and 100 mm length hemp carrying out five replications.
Moisture content was determined by drying hemp residues in a drying cabinet at a temperature of 105 ºC until their mass no longer changed. The resulting difference between the initial and final mass is converted into a percentage.
Data arithmetic averages, standard deviation and their intervals of confidence were determined with probability level (p < 0.05), respectively.
Experimental studies have shown a significantly higher moisture content (73%) for rolled hemp compared to unrolled hemp. Moisture of rolled fiber hemp were 48%, unrolled 13%. When fiber hemp is rolled, it mixes with the soil, so it takes longer for the moisture to decrease than unrolled hemp. Studies have shown that the hemp residues rolled takes about 39% longer time to break (Fig. 3), it extension is about 39% higher (Fig. 4), and energy required to break the 39% higher (Fig. 5) compared to unrolled hemp, which has a significantly lower moisture content.
Fig. 1. Roller.
Fig. 2. Equipment for determining the mechanical properties of plant residues “Instron 5960”.
INTRODUCTION
MATERIALS AND METHODS
RESULTS
Fig. 4. Extension of unrolled and rolled hemp.
Fig. 5. Breaking energy of unrolled and rolled hemp.
Studies have shown that rolled hemp residues left to overwinter strengthen their mechanical properties compared to unrolled. Therefore, during no tillage technologies they can be uncut and can be inserted into the plant's seedbed. In this place, conditions are unfavourable for growing seed. The research can be applied to the choice of technological processes for hemp cultivation.
1. Wang, D.; Blumfield, T.J.; Xu, Z. Long-term impacts of soil compaction and cultivation on soil carbon and nitrogen pools, foliar δ13C and δ15N as well as tree growth in a hoop pine plantation of subtropical Australia. Journal of Soils and Sediments 2020, 20, 2829–2842.;
2. Alskaf, K.; Mooney, S.J.; Sparkes, D.L.; Wilson, P.; Sjögersten, S. Short-term impacts of different tillage practices and plant residue retention on soil physical properties and greenhouse gas emissions. Soil and Tillage Research 2021, 206, 104803.3.
3. Korucu, F.; Arslan, S. Effects of direct and conventional planting on soil properties and yield characteristics of second crop maize. Tar. Bil. Derg. 2009, 15, 157–165.
4. Tourn, M.; Soza, E.; Botta, G.; Mete, A. Direct corn seedling. Effects of residue clearance on implant efficiency. Span. J. Agric. Res. 2003, 1, 99.
5. Hemmatian, R.; Najafi, G.; Samani, B.H.; Hashjin, T.T.; Khoshtaghaza, M.H. Experimental and theoretical investigation of the effects of moisture content and internodes position on shearing characteristics of sugar cane stems. J. Agric. Sci. Technol. 2012, 14, 963–974.
6. Šarauskis, E.; Masilionytė, L.; Andriušis, A.; Jakštas, A. The force needed for breaking and cutting of winter wheat and spring barley straw. Zemdirb. Agric. 2013, 100, 269–276.
7. Vaitauskienė, K.; Šarauskis, E.; Naujokienė, V.; Liakas, V. The influence of free-living nitrogen-fixing bacteria on the mechanical characteristics of different plant residues under no-till and strip-till conditions. Soil Tillage Res. 2015, 154, 91–102.
REFERENCES
CONSLUSION