## Slide 1
novel HBS and SC-PC-FD
steel beam–column connections
Arash Akbari Hamed
Mahsa Saeidzadeh
Mohammad Reza Chenaghlou
24 October 2023

## Slide 2: Introduction
Sensitivity of connections
Enhancement approaches
Novel ideas

## Slide 3: State of the art for steel connections

## Slide 4: HBS and SC-PC-fd connections
Novel Ideas
Heat-Treated Beam Section (HBS)
Self-Centering Pinned Connection with Friction Damper (SC-PC-FD)

## Slide 5: the HBS connection
Resistance furnace fabrication and heat treatment process
Heat-treatment time history

## Slide 6: the HBS connection
Status of the RBS and HBS specimens

## Slide 7: the HBS connection
The detailed status of the RBS specimen at the rotation of 0.06 rad

## Slide 8: the HBS connection
The detailed status of the HBS specimen at the rotation of 0.06 rad

## Slide 9: the HBS connection
Equivalent plastic strain and PE11 component of plastic strain values at 6% inter-story drift ratio

## Slide 10: the HBS connection
Comparison of stiffness in different inter-story drift ratios and absorbed energy of CHS and RHS

## Slide 11: the SC-PC-FD connection
Fabrication process of the experimental specimen
Overall view of the experimental specimens’ setup

## Slide 12: the SC-PC-FD connection
Status of the experimental specimens
Hysteretic curves of experimental specimens

## Slide 13: the SC-PC-FD connection

## Slide 14: HBS and SC-PC-FD connections vs. Existing Connections
Verification of FE modeling method

## Slide 15: HBS and SC-PC-FD connections vs. Existing Connections
Yielding status of considered steel beam-column connections at a rotation of 0.06 rad

## Slide 16: HBS and SC-PC-FD connections vs. Existing Connections
 | Strength [kN.m] | Ductility | Initial stiffness [kN.m/Rad] | Strength ratio | Ductility ratio | Initial stiffness ratio
WMC | 22.63 | 4.14 | 2617.96 | 1.11 | 0.28 | 1.01
PTSC | 20.65 | 11.76 | 2599.85 | 1.01 | 0.80 | 1.01
FDC | 22.80 | 5.17 | 2669.93 | 1.12 | 0.35 | 1.03
MYDC | 23.91 | 4.62 | 2681.31 | 1.17 | 0.31 | 1.04
HBS | 21.10 | 4.03 | 2604.87 | 1.03 | 0.27 | 1.01
SCPCFD | 20.41 | 14.67 | 2585.89 | 1 | 1 | 1

## Slide 17: Performance of self-centering frames

## Slide 18: Performance of self-centering frames

## Slide 19: Conclusions
HBS
Stable hysteretic curves until 0.06 rad rotation and a ductility of 4 to 6
Material yielding and local buckling only occurred around the weakened region far from the column face.
SC-PC-FD
Stable hysteretic curves until 0.07 rad rotation and a high ductility of 14
The effective participation of friction pads in energy dissipation by the obtained enclosed-area of the hysteretic curve
Stiffness change prevention at the weakened region and consequently elimination of lateral-torsional buckling limit state of the beam
Distribution of inelasticity of the bending plastic hinge over a larger area at the weakened region which causes to have less stress and strain values
Having more values of the stiffness and dissipated energy with respect to RBS connections
Flag-shaped hysteretic behavior without any residual deformation which confirms the full self-centering action.
Easy modification of the characteristics of SC-PC-FD connection by changing the amount of strand post-tensioning and pin pre-tensioning forces, the strand diameter size along with the strand relative distance.
Elimination of main members’ yielding and lateral-torsional buckling with simple constructional details

## Slide 20: Conclusions
HBS
SC-PC-FD
SC-PC-FD
HBS
This novel SCF system can thus be used as a reliable alternative seismic-resisting system to conventional MRFs in seismic-prone areas.

## Slide 21: Thanks for your attention
Any Questions?
Email: akbarihamed.a@sut.ac.ir
akbarihamed.arash@gmail.com